## Slide 1: New Ideas & Approaches to Raise CEBAF Q0 - Initial Results and Proposed Studies
Rongli Geng, Gigi Ciovati
July 15, 2015
2015 OPS StayTreat

## Slide 2: Outline
Introduction
Factor of 2 change in Q0 from evaluation at VTA to placement in CEBAF
Sources of change and mitigation
  Understanding from past and present effort
  Mitigations implemented and planned
New opportunities
  Frozen flux reduction by Cryogenic Thermal Annealing (CTA)
  Whole-module degaussing
  Impurity doping refurbishment cavities?
Proposal for new studies and tests
Conclusion

## Slide 3: Introduction
Upgrade done. CEBAF has entered into new era of operation for NP.
  320 5-cell cavities plus 80 7-cell cavities in north- & south- linacs
  High gradient (15-20 MV/m) in CW operation
    Unprecedented
    Unique large SRF linac – pushing reliability envelope
Energy reach is crucial for CEBAF capability
  Ultimate energy reach is constrained by Q0 given fixed cavity shape and cryo-plant capacity (also RF source and LLRF)
Energy efficiency is critical for sustainability
  CEBAF needs to catch up in next few years for efficiency competitiveness
    CEBAF: 2 GeV, 10 kW @ 2K
    LCLS-II: 4 GeV, 8(4) kW @ 2K
Seeking for establishment of new project to raise Q0 of installed cavities in CEBAF: (a) without moving cryomodules out of tunnel;(b) within on-going C50 refurbishment effort.

## Slide 4
Original Cavity and Cryomodule
Cryo unit
 | Design | Vertical testing | Cryomodule testing
<Eacc> | 5 | >5 | >5
Q0 at 2K at 5 MV/m | 2.4×109 | ~ 1×1010 | ~ 5×109
4x cryo unit -> cryomodule (8.25 m long)
Factor of 2 loss in Q0
Q0 met construction spec of 2.4×109

## Slide 5: Sources of Q0 Change and Mitigation
Source | Understanding | Mitigation | Mitigation implemented?
Magnetic strut springs | 302 SS, remanent magnetic flux, worse case 6 G at contact | Replace them by 316 SS springs | YES
Magnetic tuner drive shaft | 17-4 PH SS, remanent magnetic flux, worse case 1.7 G at contact | Replace them by 316 SS shaft | NO
Magnetic bearing | 440C SS, remanent magnetic flux typical 0.5 G at contact | Degauss first then re-use | YES
Confirmed magnetic sources
Source | Ruled out?
“Q-disease” from hydrogen in niobium material | YES
Window loss | TBD
Other sources
Work published at IPAC14 as a contributed talk, THOBB01
“Pursuing the Origin and Remediation of Low Q0 observed in the Original CEBAF Cryomodules”

## Slide 6: Sources of Q0 Change and Mitigation (cont.)
Source | Testing result in hand? | Further test needed? | Potential benefit
Generated flux from thermal current effect | Initial testing result measured in VTA using a 5-cell dummy cavity | YES | May lead to a “thermal therapy” of in-situ Q0 recovery in CEBAF tunnel
Additional flux trapping from repeated quenching events | NO | YES | May lead to an improved cryomodule testing procedure for full preservation of cavity Q0 from VTA to tuunel
Sources under investigation/to be investigated
Presently:
Examination of magnetic flux thermally generated inside the loop formed between niobium cavity and stainless steels rods
Developing a thermal current model for prediction of generated flux of cavity pair in a cryo-unit.
A potential “thermal therapy” is being developed for zero out the thermally generated flux.
Series test of thermal current and generated flux
using a 5-cell CEBAF cavity
Stainless steel rod
Niobium cavity
magnetometers
After 20K warm up followed by
Re-cool down
Thermally generated flux during initial cool down
Flux jump
near 9.25K,
Tc of Nb
New
Shichun Huang

## Slide 7
JLAB-TN-14-021
Additional flux trapping from repeated quenching events

## Slide 8
SRF Machine | Duty Factor [%] | Design Q0 [1010] | Surface resistance [nΩ] | Relative increase for 4 nΩ added surface resistance | Number of high Q0 cavities | Impact level
CEBAF-original | 100 | 0.24 | 114 | 4% | 338 | Negligible
CEBAF-upgrade | 100 | 0.72 | 39 | 10% | 80 | Low
XFEL | 0.65 | 1.0 | 27 | 15% | 800 | Medium
LCLS-II | 100 | 2.7 | 10 | 40% | ~300 | High
ILC-baseline | 0.65 | 1.0 | 27 | 15% | 16000 | Medium
ILC- low loss | 0.65 | 2.0 | 14 | 30% | 16000 | High
Impact Factors

## Slide 9: New Opportunities
Frozen flux reduction by CTA
Whole-module degaussing
Impurity doping of re-furbished cavities

## Slide 10
1-Cell Cavity Testing of CTA
LSF1-3
1.3 GHz
LSF Shape
Large-Grain Nb
Cavity processing:
BCP 60 um + 800Cx2hr + BCP 20 um + 120Cx9hr
30% increase in Q0

## Slide 11
Chart: LSF1-3 partial warm to 20 K then re-cool down

## Slide 12
Whole-module degaussing
De-magnetize whole cryomoudle
  Could lead to a solution applicable to cryomodules placed in CEBAF without moving them out of tunnel.
Feasibility test with a cryo-unit or a quarter module
A. Crawford, Superconducting RF Cryomodule Demagnetization, arXiv:1503.04736

## Slide 13: Impurity Doping of Re-furbished Cavities
Impurity doping (Ti, N) has shown benefit of raising Q0.
A workable procedure is now available in-house for nitrogen doping due to work for LCLS-II.
A number of 9-cell XFEL/ILC cavities have been treated with nitrogen doping and tested at JLAB with good Q values up to the regime of 20 MV/m.
A 7-cell C100-style was nitrogen doped and tested horizontally in a one-cavity cryomodule, with good Q values.
Therefore…

## Slide 14: Impurity Doping of Re-furbished Cavities (cont.)
At September 22, 2014 C50-12 pre-kickoff meeting, a decision was made to test Nitrogen doping on a CEBAF 5-cell cavity.
The goal is to raise cavity Q0 in a CEBAF re-work cryomodule beyond what can be imagined before by exploitation of nitrogen doping technique that was made available in-house for LCLS-II Q0 R&D.
Cavity IA009 was chosen for this study.

## Slide 15
Triple Q0
New goal:
Q0=2E10
@ 12.5 MV/m
Original C50 goal:
Q0=6.8E9
@ 12.5 MV/m
Achieved Q0
In C50-1…11

## Slide 16: IA009 Performance Evolution since Re-baseline

## Slide 17: Discovery of Surface Defects
4 mm fusion zone
Pit ~400 µm dia.
Connected with extended bark regions
Pit ~100 µm dia.
Outstanding defects in fusion zone
of equator weld of cell #4

## Slide 18: Expanded Inspection of Surface Defects
Only Pit and large flaw counted

## Slide 19: Conclusion on Preliminary 5-Cell N-doping
First attempt in raising Q0 by N-doping (IA009) is not successful, as a result of “grave” Fusion Zone Defect (FZD).
Optical inspection of 4 more 5-cell cavities revealed similar FZD’s in similar amount.
FZD’s can be classified into three types: (1) pit; (2) ripple; (3) “large flaw”. They are believed to originate from material/fabrication and therefore can be considered “genetic”.
FZD is rarely observable on modern-day Nb cavities.
It seems that “any attempt to further raise the Q0 of these cavities by re-processing may face a brick wall”.
  Nature FZD and their interplay with N-doping deserve studies.
  Cure FZD by barrels polishing may help and should be evaluated.

## Slide 20: Proposal for New Studies and Tests
Systematic VTA cavity testing for frozen flux effect.
  Test the CTA procedure for recovering Q0 of cavities under the standard cavity pair configuration. (High impact potential)
    Verify the thermal current model that has been developed from one 5-cell dummy cavity test.
    Develop a CTA recipe of “thermal therapy” to be applied in-situ over all 5-cell cavities currently placed in tunnel.
  Complete the unfinished C50-12 activities. (Impact the future re-furbishment cryomodules)
    Progressive component addition to cavity pair to pin-point magnetized components.
    Experiment “local shielding” over the center cells.
    Assess window loss contribution.

## Slide 21: Proposal for New Studies and Tests (cont.)
Test the feasibility of “whole module” de-magnetization.
  Test with dummy cryo-unit.
    Series tests with progressively added components around cavity.
    Assess shielding factors of the inner shield and the outer shield
    Characterize the magnetization of the shielding itself.
  Cryogenic test of a cavity pair in a short cryomoudle
    Mini-test of CTA.
    Study added frozen flux from repeated quench events.

## Slide 22: Proposal for New Studies and Tests (cont.)
Further evaluation of nitrogen-doping for raising Q0 5-cell cavities, including possible re-doping after barrel polishing.
  Two cavites in hand:
    IA008 (N-doping completed)
    IA011
  A clear conclusion on N-doping is useful
    Positive answer sets solid ground for possible future path of Nb3Sn re-treatment.
    Negative answer sets solid ground for possible future path of “LG cell transplant”
Fundamental studies of defects in IA009
  Dissect cavity, make 5 each 1-cell cavities, test with T-mapping, cut out quench area for material studies.
  Recycle end groups for “C75” cavities with transplanted cells.

## Slide 23: Conclusion
The low Q0 issue of 5-cell CEBAF cavities remains outstanding.
  Understanding of Q0 damage from magnetized components in hand, one change implemented in C50-11. One more change is to be implemented in C50-12.
The effort in raising Q0 of placed cavities in CEBAF has led us to explore inexpensive solutions applicable in-situ for raising average Q0.
  Cryogenic Thermal Annealing.
  Whole-module degaussing.
The effort in raising Q0 for C50 refurbishment by N-doping 5-cell cavities met the issue of genetic FZDs. Further studies needed.
Effort in Q0 improvement and field emission reduction is related.
Proposal is to establish a new project, whose objective is to raise Q0 of installed cavities in CEBAF: (a) without moving cryomodules out of tunnel;(b) within on-going C50 refurbishment effort.
A detailed cost of the proposed studies is being developed (< $150K).

## Slide 24
Backup Slides

## Slide 25: IA009 Actions since 5/5/15
Cavity vented, removed from test stand, fully dis-assembled.
Optical inspection of equator regions.
  Cell number starting at input power coupler side
  Angle definition: 0°= 12 o’clock, direction=clock-wise

## Slide 26
4 mm fusion zone
Pit ~400 µm dia.
Connected with extended bark regions
Pit ~100 µm dia.
Outstanding defects in fusion zone
of equator weld of cell #4

## Slide 27: Cell #1 Equator Weld
Φ=174°
Φ=346°
Pits (3 in total, smaller than average)

## Slide 28: Cell #1 Equator Weld
Φ=56°
Φ=159°
speckles (clustered in a few regions, only cell showing this)
Nitrogen-rich islands due to insufficient surface removal?

## Slide 29: Cell #2 Equator Weld
Φ=185°
Φ=263°
Pits (13 in total, 2 typical examples shown)

## Slide 30: Cell #2 Equator Weld
Φ=14°
Φ=32°
Large flaws

## Slide 31: Cell #3 Equator Weld
Φ=215°
Φ=332°
Pits (14 total, largest shown)
Curved linear feature
(ripple of molten Nb?)

## Slide 32: Cell #4 Equator Weld
Φ=0°
Φ=35°
Pits (45 total, a few typical shown)

## Slide 33: Cell #4 Equator Weld
Φ=15°
Φ=73°
Pits next to ripple

## Slide 34: Cell #4 Equator Weld
Φ=52°
Φ=334°
Large flaws

## Slide 35: Cell #4 Equator Weld
Φ=62°
Φ=200°
Pits (4 total, largest shown)
Curved linear feature
(ripple of molten Nb?)

## Slide 36: 5/14/15 Conclusion
Post VTA optical inspection revealed surprisingly large number of defects (pits, ripples and large flaws).
Cell #2 & #4 are the worst – both have large flaws
Cell #1 & #5 are the best; #3 in the middle.
The heavy defect in cell #2 & #4 is consistent with previous finding of cell #2/4 being the most lossy; is also consistent with previous finding of cell #2/4 are among candidate cells responsible for quench at 9 MV/m.
“Cloudy” speckles observed on cell #1 equator weld surface. We suspect these are nitrogen-rich islands due to insufficient EP removal.

## Slide 37: 5/14/15 Conclusion (cont.)
Based on good correlation between pass-band measurements and optical inspection results, we conclude both the premature quench and the strong Q-slope of IA009 after nitrogen doping was caused by grave defects in fusion zone of cell #2/4 equator welds.
From RG’s past experience, there is little chance of further improving the cavity performance by another EP.
Based on optical inspection data of IA009 (2015) and IA015 (2008), we conclude the “fusion zone defect (FZD)” is a genetic character in all original CEBAF cavities, due to the then cavity EBW technology. Therefore, any attempt to further raise the Q0 of these cavities by re-processing may face a brick wall. We propose to terminate the N-doping CEBAF cavity experiment. Instead, start to evaluate a cure to pit first.
We seem to have a case of insufficient EP removal in cell #1 of a CEBAF 5-cell cavity.

## Slide 38: Actions since May 14
Cavity | Last surface treatment and performance | Note
IA011 | Unknown (most likely BCP) | Cavity received from LP
IA080 | Unknown (most likely BCP) | Cavity dis-assembled from a cryomodule (FEL?) to be re-worked and become C50-12. Cavity have “large grains” all over places – apparently heat treated to high temperature (at least 1250 °C) in its past life.
IA355 | Unknown (most likely BCP) | ibid
IA008 | Nitrogen doping (no cryogenic RF test after nitrogen doping) | Pre-nitrogen doping processing history unknown. Latest cold test on 4/8/2013; 3/12/2013; 10/15/2008
Carried out optical inspection of four 5-cell CEBAF cavities

## Slide 39
Only Pit and large flaw counted

## Slide 40: IA008 (Nitrogen doped)
Cell 4 Φ=334°
Cell 2 Φ=132°
pit
Large flaw

## Slide 41: IA080 (removed from module to be re-worked and become C50-12, “Large grain”)
Cell 1 Φ=204°
Cell 2 Φ=146-148°
pit
Large flaw

## Slide 42: IA355 (removed from module to be re-worked and become C50-12, “Large grain”)
Cell 4 Φ=215°
Cell 3 Φ=154°
pit
Large flaw

## Slide 43: IA011
Cell 4 Φ=88°
Cell 2 Φ=355°
pit
Pre-cursor large flaw?
No apparent large flaw observed
BCP etching of inner surface seems much less than other inspected cavities
  Visible molten pool ripples
  Visible “blisters” on fusion zone surface