## Slide 1: C75 options
F. Marhauser, J. Henry, R. Rimmer,
J. Benesch

## Slide 2: Options for “C75”
Goal is to investigate something between C50 and C100 with more “bang for the buck”
Cost like C50, performance like C100
“magic bullet”: some process to transform old cavities
  N2 Doping, Nb3Sn, ???
New cavities in old CM
  Add cost, but gain performance*
  Could fix coupling kicks
  Significant engineering required
  What about “cell transplant”?
New less expensive C100 CM
  Major re-engineering needed. Synergy with MEIC?
* Need to find and fix the cause of Q loss to make this worthwhile

## Slide 3: FEL HC design study
For FEL upgrade we looked at a new high-current 5-cell cavities that would fit in old cryounits
Also for new CEBAF cryounit (same insertion length)

## Slide 4: 6-cell C75 cavity
Squeeze 6-cell cavity into space in pair
  Eliminate separate helium vessel hubs
  Use C100 center type waveguide interface
  Use C100 type HOM cans instead of waveguides
Significant engineering needed to make it real
  New tuner required? (Rock-crusher or blade type?)
  Separate helium vessels

## Slide 5: “J100”
Jay’s 12 GeV proposal:
  6 x 9-cell cavities
  ~18.5 MV/m average
  Stretched CEBAF type pairs, extended vessels
  Higher power ~17 kW FPC, klystrons (but fewer)
What about J75?
  ~14 MV/m, ~13 kW tubes, 12 GeV LLRF

## Slide 6: CEBAF energy maintenance options
Summary of options and estimated costs
 | cavities | cells/cav | cav length m | Act. length m | fill factor % | voltage (MV) | volts/cav (MV) | gradient (MV/m) | klystron power | unit cost (FY16 M$) | voltage gain (MV) | V/$
C50 | 8 | 5 | 0.5 | 4 | 48.1 | 50 | 6.25 | 12.5 | 6 | 1.51 | 20 | 13.3
C100 | 8 | 7 | 0.7 | 5.6 | 64.4 | 100 | 12.5 | 17.9‡ | 13 | 4.77 | 70 | 14.7
C75† | 8 | 5 | 0.5 | 4 | 48.1 | 75 | 9.4 | 18.8‡ | 8 | 1.91 | 45 | 23.6
C75†* | 8 | 6 | 0.6 | 4.8 | 57.8 | 75 | 9.4 | 15.6 | 8 | 2.31* | 45 | 19.5
J100* | 6 | 9 | 0.9 | 5.4 | 65.0 | 100 | 16.7 | 18.5‡ | ~17 | ??? | 70 | ???
J75* | 6 | 9 | 0.9 | 5.4 | 65.0 | 75 | 12.5 | 13.9 | 13 | ??? | 45 | ???
*Engineering required at additional cost (not included)
‡Digital LLRF required
†New cells or new processing required to achieve higher Q’s and gradients

## Slide 7: Opt. 3:High Current (HC) Cavity for C50 Cryomodules?
HC 5-cell cavity using C50 HOM and FPC endgroup - “HC50”
OC 5-cell cavity

## Slide 8: VTA test 1497 MHz HC 5-cell cavity
Large grain with damaged cell from CBP, final BCP
Q0 ~ 1.1e10 up to 20 MV/m

## Slide 9: Cavity Parameters
Parameter | Unit | C50 | HC50
Frequency @ 2 Kelvin | MHz | 1497 | 1497
R/Q (β = 1) | Ω | 482.5 | 525.4
G | Ω | 274.0 | 275.6
R/Q*G | Ω2 | 132205 | 144802
tube/iris ID | mm | 70/70 | 70/70
TE11/TM01 cutoff | GHz | 2.51/3.28 | 2.51/3.28
cell-to-cell coupling | % | 3.15 | 3.15
Uacc (nominal, on crest) | MV | 6.25 | 6.25
Lactive (nominal) | mm | 499.855 | 491.600
Eacc (nominal @ 50 MeV) | MV/m | 12.50 | 12.71
Epeak/Eacc |  | 2.56 | 2.45
Bpeak/Eacc | mT/(MV/m) | 4.56 | 4.18
Epeak | MV/m | 32.0 | 31.1
Bpeak | mT | 57.0 | 52.3
Pcav (@ Q0 = 6.8e9) | W | 11.9 | 10.9
PCM (@ Q0 = 6.8e9) | W | 95.2 | 86.9
At same Q0 about 1 W reduction of dynamic losses per cavity at 2 K (~10%) at 50 MeV based on cavity design

## Slide 10: Cavity Parameters
Parameter | Unit | C50 | HC50
Frequency @ 2 Kelvin | MHz | 1497 | 1497
R/Q (β = 1) | Ω | 482.5 | 525.4
G | Ω | 274.0 | 275.6
R/Q*G | Ω2 | 132205 | 144802
tube/iris ID | mm | 70/70 | 70/70
TE11/TM01 cutoff | GHz | 2.51/3.28 | 2.51/3.28
cell-to-cell coupling | % | 3.15 | 3.15
Uacc (nominal, on crest) | MV | 6.25 | 6.25
Lactive (nominal) | mm | 499.855 | 491.600
Eacc (nominal @ 50 MeV) | MV/m | 12.50 | 12.71
Epeak/Eacc |  | 2.56 | 2.45
Bpeak/Eacc | mT/(MV/m) | 4.56 | 4.18
Epeak | MV/m | 32.0 | 31.1
Bpeak | mT | 57.0 | 52.3
Pcav (@ Q0 = 1.1e10) | W | 7.4 | 6.7
PCM (@ Q0 = 1.1e10) | W | 58.9 | 53.7
At same Q0 about 1 W reduction of dynamic losses per cavity at 2 K (~10%) at 50 MeV based on cavity design

## Slide 11: Dynamic RF losses
Parameter | Unit | C50 | HC50 | ΔPRF (W) | ΔPRF , max (W)
Eacc (nominal @ 50 MeV) | MV/m | 12.5 | 12.7 | - | -
Pcav(@ Q0 = 6.8e9) | W | 11.9 | 10.9 | 1.0 | -
Pcav (@ Q0 = 1.1e10) | W | 7.4 | 6.7 | 0.64 | 5.2
1.04 W/cav. reduction at same low Q0 (8.3 W per CM)
0.62 W/cav. reduction at same high Q0 (5.2 W per CM)
5.19 W/cav. max. reduction with Q0 gain (41.5 W per CM)
Parameter | Unit | C50 | HC50 | ΔPRF (W) | ΔPRF , max (W)
Eacc (nominal @ 70 MeV) | MV/m | 17.5 | 17.8 | - | -
Pcav (@ Q0 = 6.8e9) | W | 23.3 | 21.3 | 2.0 | -
Pcav (@ Q0 = 1.1e10) | W | 14.4 | 13.2 | 1.3 | 10.2
2.04 W/cav. reduction at same low Q0 (16.4 W per CM)
1.26 W/cav. reduction at same high Q0 (10.1 W per CM)
10.17 W/cav. max. reduction with Q0 gain (81.4 W per CM)
max.
max.
50 MeV gain
70 MeV gain

## Slide 12: What about HOMs?
“HC50”
C50
Can now model in CST Microwave Studio including HOM loads

## Slide 13: C50-style load
Include material properties in calculation instead of perfect match
material data (I.E. Campisi 1993)
model data (ε‘, ε‘‘)

## Slide 14: HOM Damping
Damping slightly improved for crucial dipole modes
Modes below HOM waveguide cutoff rely on evanescent field and FPC mode damping

## Slide 15: TE111 HOMs below HOM Waveguide Cutoff
1st TE111 mode pair (π/7): ~1725 MHz
2nd TE111 mode pair (2π/7): ~1760 MHz
FPC TE10 cutoff: 1.1 GHz
more vertically polarized
more horizontally polarized
more vertically polarized
more horizontally polarized
scale similar throughout (electrical RF field)

## Slide 16: HOM Damping (with FPC damping)
Damping by FPC has impact on modes close to BBU threshold
damping through FPC waveguide included
Monopole Impedances (Ohms)

## Slide 17: HOM Damping (with FPC damping)
Damping by FPC has impact on modes close to BBU threshold
damping through FPC waveguide included

## Slide 18: C50 external HOM filters
This was one reason to utilize the CM-external CEBAF filters

## Slide 19: Conclusions
Numerous options for improved cost-effectiveness
Magic bullet (still looking…)
Cell transplant
  minimum perturbation
  Best near term “bang for the buck”?
New cavities
  engineering required
  Can fix other problems
New cryomodule
  more engineering required
  May have synergy with MEIC
  Possibly cost–effective long term

## Slide 20: Proposal
Build two “HC50” cavities using in-stock ingot material and existing spare end groups
  We have the dies
  We have the material but needs slicing (~15k)
Process and test in VTA
If good insert into next available C50
Cost ~50k, mostly shop, e-beam welding and chemistry/VTA

## Slide 21
Back up

## Slide 22: CEBAF SRF Workshop (April 2014)
C20: met Q0 = 2.4e9 at 5 MV/m at 2K  45 W dynamic load per CM
C50: Q0 target 6.8e9 at 12.5 MV/m at 2.1 K ~100 W dynamic per CM (M. Drury, PAC07, WEPMS059)
C50-11 Q0 Analysis (Rongli Geng): No cavity reached target Q0 in CEBAF tunnel during commissioning, on average factor 2 lower Q0
Observation: Q0 = 5e9 at 6 MV/m similar to 1992 commissioning, i.e. no improvement by refurbishment at 6 MV/m
But Q0 > 1e10 at 12.5 MV/m in VTA)

## Slide 23: CEBAF SRF Workshop (April 2014)
At same Q0 about 1 W reduction of dynamic losses per cavity at 2 K (~10%) at 50 MeV based on cavity design
C50-11 Q0 Analysis (Rongli Geng)