## Slide 1: CERN Alkali Antimonide Experience
Christoph Hessler
On behalf of the CERN lasers and photocathode team
Photocathode Physics for Photoinjectors (P3) Workshop,
17 - 19 October 2015, Jefferson Lab, Newport News, USA

## Slide 2: Outline
Overview on CLIC photoinjector activities
Why do we study alkali antimonide cathodes?
Photocathode production
Alkali antimonide lifetime studies in RF and DC gun
XPS surface analysis studies
Outlook

## Slide 3: CLIC

## Slide 4: Photoinjectors at CTF3
Photoinjector laser lab (1st floor) and optical transfer line to PHIN and CALIFES
Dedicated photoemission laboratory for photocathode production, testing and R&D
PHIN
CLIC Test Facility 3 (CTF3):

## Slide 5: Photoinjector Parameters
 | Main beam | Drive beam | 
Parameter | CALIFES (CTF3) | PHIN (CTF3) | CLIC requirem.
Charge per bunch (nC) | 0.6 | 2.3 (9.2) | 8.4
Macro pulse length (μs) | <0.2 | 1.2 (1.6) | 140
Bunch spacing (ns) | 0.66 | 0.66 | 2.0
Gun RF / bunch rep. rate (GHz) | 3 / 1.5 | 3 / 1.5 | 1 / 0.5
Number of bunches in macro pulse | 1 – 300 | 1800 (2400) | 70000
Macro pulse rep. rate (Hz) | 5 | 5 (5) | 50
Charge per macro pulse (μC) | <0.18 | 4.1 (5.5) | 590
Beam current in macro pulse (A) | 0.9 | 3.5 | 4.2
Bunch length (ps) | 10 | 10 | 10
Charge stability | <3% | <0.25% (<1%) | <0.1%
Cathode lifetime (Cs2Te) | 1 y (QE>0.3%) | >50 h (QE>3%) (>300 h) | >150 h (QE>3%)
Cathode type | Cs2Te (in-situ, dual layer) | Cs2Te, Cs3Sb (co-deposition) | To be defined
Norm. emittance (μm) | <20 | <25 (14) | <100
O. Mete et al., “Production of long bunch trains with 4.5 µC total charge using a photoinjector”, Phys. Rev. ST Accel. Beams 15 (2012), 022803.

## Slide 6: Long Train Harmonics Generation
Degradation of UV beam has been observed for long pulse trains due to photo-elastic effects caused by two-photon absorption in the FHG crystal.
Problem does not exist for SHG.
Possible solutions:
  Usage of photocathodes sensitive to visible light.
  New harmonics generation schemes with multiple crystals.
10us, 4.4mJ
80us, 25mJ
140us, 41mJ
FHG, BBO 12 mm
Figures courtesy M. Martyanov

## Slide 7: Photocathode Production and R&D
Dedicated photoemission laboratory available at CERN for photocathode production and R&D.
Equipped with preparation system for co-evaporation of Cs and Te/Sb.
70 keV DC gun and diagnostic beam line for measuring the photocathode properties.
Transport of photocathodes under vacuum to PHIN photoinjector, CERN XPS laboratory and LAL (Orsay) possible. And soon to ASTeC Daresbury (special samples only).
Achieved quantum efficiency (QE): >20% (Cs2Te), 7.5% (Cs3Sb)
Te/Sb evaporator
Cs dispenser
Masks

## Slide 8: Preparation System and Test Beam Line
LASER:
Q-switched Nd:YAG λ=532 nm or 266 nm
CATHODE position during PRODUCTION
electron beam
CATHODE position during TEST
Bunch charge measured by:
Wall Current Monitor (WCM)
Fast Current Transformer (FCT)
Faraday Cup (FC)
DC gun
Preparation chamber
Beam line

## Slide 9: Co-Deposition Setup
Substrate: Copper with diamond powder polished surface
Substrate is heated to 125⁰C for Cs3Sb, and not heated for Cs2Te.
Thickness monitors: Quartz microbalances for Cs and Te/Sb. Masks allow to measure both evaporation rates separately.
Online QE measurement: Main tool for optimizing the deposition process → mandatory for co-deposition
Laser beam
Shutter
Evaporators
Te/Sb
microbalance
Cs microbalance
Plug
position
Ø ~ 19 mm
Te/Sb evaporator
Cs dispenser
Masks
SAES®getters
E. Chevallay, “Experimental Results at the CERN Photoemission Laboratory with Co-deposition Photocathodes in the Frame of the CLIC Studies”, CTF3 Note 104, 2012

## Slide 10: Co-Deposition Process
Co-deposition: Cs and Sb (or Te) evaporated at the same time. The metallic elements can mix together in the vapour phase.
The evaporators power is adjusted in order to reach a maximum value of the QE.
Average pressure during the process ~1E-8 mbar
Courtesy I. Martini

## Slide 11: Deposition Results for Cs3Sb
After stopping the evaporation, the QE of Cs3Sb cathodes initially continues to increase during beam production in DC gun (not observed for Cs2Te).
Reason for this behavior still unclear, maybe due to re-organization of Cs and Sb atoms.
QE mapping shows a uniform photoemissive layer.
No. | Initial QE (%) | Max QE (%) | Evaporated Cs (nm)* | Evaporated Sb (nm)* | Final stoich. ratio*
178 | 0.3 | 0.5 | 120 | 18.4 | 2.9
179 | 1.4 | 2.3 | 156 | 24.5 | 1.74
180 | 0.6 | 1.0 | 52 | 14.4 | 3.1
187 | 0.3 | 0.4 | 67.6 | 4.7 | 18.9
188 | 1.3 | 2.2 | 152 | 17.8 | 8.84
189 | 2.3 | 4.4 | 64 | 15 | 1
191 | 5.4 | 7.5 | 156 | 14 | 1.7
192 | 2.0 | 2.7 | 9.7 | 3.5 | 0.66
193 | 4.2 | 5.8 | 10.8 | 7.6 | 0.65
194 | 2.7 | 4.5 | 18.7 | 20.7 | 0.9
199 | 3.5 | 5.2 | 269 | 22.7 | 2.9
200 | 3.4 | 5.5 | 83.3 | 23.5 | 0.98
Continuous beam operation
Chart: y[mm]
| -12 | -11 | -10 | -9 | -8 | -7 | -6 | -5 | -4 | -3 | -2 | -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11
-12 | 0.052513 | 0.055827 | 0.053644 | 0.055688 | 0.057277 | 0.058345 | 0.060502 | 0.060058 | 0.064452 | 0.063364 | 0.067958 | 0.066271 | 0.065877 | 0.064765 | 0.065289 | 0.06291 | 0.063019 | 0.060388 | 0.057375 | 0.057407 | 0.057782 | 0.055996 | 0.056828 | 0.055875
-11 | 0.053483 | 0.057516 | 0.058018 | 0.056086 | 0.06045 | 0.062696 | 0.064813 | 0.065675 | 0.069172 | 0.073541 | 0.075139 | 0.079996 | 0.083537 | 0.078478 | 0.075538 | 0.071084 | 0.068533 | 0.064847 | 0.061519 | 0.061221 | 0.059659 | 0.058046 | 0.055822 | 0.05356
-10 | 0.05519 | 0.057535 | 0.059958 | 0.062715 | 0.061728 | 0.066811 | 0.069393 | 0.080094 | 0.093364 | 0.10814 | 0.11923 | 0.12665 | 0.12687 | 0.1231 | 0.11131 | 0.10173 | 0.082006 | 0.076634 | 0.066656 | 0.065964 | 0.062088 | 0.060703 | 0.059682 | 0.058109
-9 | 0.055057 | 0.059736 | 0.060878 | 0.060667 | 0.068674 | 0.078336 | 0.094724 | 0.12135 | 0.15841 | 0.1917 | 0.21917 | 0.22724 | 0.21974 | 0.21023 | 0.19212 | 0.16859 | 0.13242 | 0.099596 | 0.084509 | 0.069421 | 0.064616 | 0.062112 | 0.060508 | 0.060546
-8 | 0.058984 | 0.06032 | 0.061526 | 0.069641 | 0.073223 | 0.10085 | 0.14472 | 0.20542 | 0.29627 | 0.36506 | 0.44504 | 0.45657 | 0.44506 | 0.40267 | 0.33608 | 0.27816 | 0.21226 | 0.16906 | 0.12091 | 0.087051 | 0.075141 | 0.066593 | 0.060747 | 0.060449
-7 | 0.059376 | 0.063749 | 0.064114 | 0.073266 | 0.092389 | 0.15711 | 0.2575 | 0.40271 | 0.59304 | 0.72333 | 0.87345 | 0.94944 | 0.91442 | 0.82499 | 0.67687 | 0.50631 | 0.33909 | 0.25061 | 0.19051 | 0.14042 | 0.089319 | 0.073391 | 0.067066 | 0.060185
-6 | 0.061128 | 0.063731 | 0.072934 | 0.08462 | 0.13823 | 0.27017 | 0.48415 | 0.7524 | 1.0697 | 1.2682 | 1.4184 | 1.4578 | 1.4183 | 1.3429 | 1.1892 | 0.96499 | 0.58998 | 0.36171 | 0.26835 | 0.20079 | 0.12753 | 0.08577 | 0.071445 | 0.061887
-5 | 0.06538 | 0.068414 | 0.078116 | 0.10651 | 0.20157 | 0.44707 | 0.77866 | 1.1372 | 1.4762 | 1.6352 | 1.6954 | 1.6805 | 1.6544 | 1.5894 | 1.4963 | 1.3171 | 0.98158 | 0.59842 | 0.36038 | 0.26647 | 0.18264 | 0.11088 | 0.07696 | 0.068597
-4 | 0.062401 | 0.068648 | 0.084289 | 0.13479 | 0.29604 | 0.65631 | 1.0545 | 1.4696 | 1.7066 | 1.7708 | 1.7425 | 1.7712 | 1.7459 | 1.7114 | 1.6276 | 1.5516 | 1.2887 | 0.9163 | 0.53113 | 0.31428 | 0.24988 | 0.14312 | 0.087163 | 0.068372
-3 | 0.064615 | 0.073005 | 0.09427 | 0.17154 | 0.38748 | 0.84788 | 1.2785 | 1.6732 | 1.7888 | 1.8426 | 1.7908 | 1.8149 | 1.7616 | 1.7423 | 1.6968 | 1.6269 | 1.4632 | 1.1677 | 0.73639 | 0.42036 | 0.30309 | 0.19824 | 0.11084 | 0.073388
-2 | 0.067977 | 0.073652 | 0.10126 | 0.19954 | 0.45317 | 0.94512 | 1.422 | 1.7174 | 1.8222 | 1.8508 | 1.8756 | 1.8798 | 1.8515 | 1.7932 | 1.7331 | 1.6725 | 1.5751 | 1.3521 | 0.88242 | 0.49841 | 0.32635 | 0.23615 | 0.12273 | 0.078404
-1 | 0.065055 | 0.077708 | 0.10635 | 0.21584 | 0.51188 | 1.0402 | 1.5224 | 1.7662 | 1.8542 | 1.8541 | 1.8834 | 1.906 | 1.9135 | 1.8534 | 1.8232 | 1.7595 | 1.6826 | 1.4862 | 1.0397 | 0.59239 | 0.3434 | 0.26249 | 0.14068 | 0.081502
Max. achieved QE = 7.5%.
No obvious correlation between QE and the final stoichiometric ratio or the evaporated quantity.
Courtesy I. Martini
I. Martini et al., Proc. of IPAC’13, Shanghai (2013), p. 413.

## Slide 12: Produced Co-Deposition Cathodes
Courtesy E. Chevallay

## Slide 13: Summary: Preparation System
Main advantages of CERN preparation setup:
  Online QE monitoring allows precise tuning of evaporation rates to achieve good QE values.
  Availability of DC gun and test beam line at the preparation system allows an immediate control of the QE in a reliable way (incl. QE map).
  DC gun allows the initial operation of Cs3Sb cathodes to increase their QE.
  Transport of cathode samples under UHV possible to PHIN photoinjector, CERN XPS lab, LAL and soon to ASTeC Daresbury lab for surface studies.
Room for improvements:
  One complete equipped evaporator setup lasts only for ~3 cathodes. → New evaporator setups has been designed for double capacity SAES Cs dispensers, for Alvatec Cs dispensers and for 3 component cathodes.
  For changing evaporators and cathode substrates the preparation chamber must be opened and afterwards baked, which in total takes several weeks. → To improve situation a load-lock system has been studied.
  Vacuum mirror in preparation chamber gets coated with the time and needs to be exchanged frequently.

## Slide 14: PHIN Layout
FCT: Fast current transformer VM: Vacuum mirror SM: Steering magnet BPM: Beam position monitor MSM: Multi-slit Mask OTR: Optical transition radiation screen
MTV: Gated cameras SD: Segmented dump FC: Faraday cup
VW: Vacuum window
VW
Mode of operation:
One PHIN run per year (~4 weeks)

## Slide 15: Vacuum Improvement at PHIN
7e-10 mbar
1.3e-10 mbar
Dynamic vacuum level:
4e-9 mbar
Static vacuum level:
2.2e-10 mbar
March 2012
March 2011
Step 1: Activation of NEG chamber around gun
2e-10 mbar
2.4e-11 mbar
July 2013
Step 2: Installation of additional NEG pump
Step 3: Separation of Faraday cup by vacuum window
August 2015
Same minimum vacuum level, but also for long train operation

## Slide 16: Cs3Sb Lifetimes after 1st Vacuum Improvement
Measurements taken during PHIN run March 2012 after activation of NEG chamber.
Excellent lifetimes obtained, much better than expected.
Long-time operation over 10 days with one cathode!
Operation of 1.2 µs long trains yield similar lifetime as for short trains.
Lifetimes similar as for Cs2Te at that time (for same setup without vacuum window) and within CLIC specifications.
2.3 nC, 350 ns, l=524 nm
2.3 nC, 1200 ns, l=524 nm
1/e lifetime 168 h
(corresponds to 270 h
above 0.5% QE)
1/e lifetime 135 h
2012
2012
9e-10 mbar
1e-9 mbar

## Slide 17: Impact of Vacuum on Cs3Sb Cathode Lifetime
Comparison with earlier measurements of Cs3Sb cathodes with UV light and worse vacuum conditions before the 1st step of vacuum improvement (same beam parameters).
Lifetime has drastically improved from 26 to 185 h.
Improved vacuum condition due to activation of NEG chamber around the gun.
1/e lifetime 185 h
1 nC, 800 ns, l=524 nm
1/e lifetime 26 h
1 nC, 800 ns, l=262 nm
7e-10 mbar
4e-9 mbar
March 2012
March 2011

## Slide 18: Cs3Sb Lifetimes after 2nd Vacuum Improvement
Investigation of Cs3Sb lifetimes after installation of additional NEG pump:
Dynamic pressure: 2.3e-10 mbar
1 nC, 800 ns, Cs3Sb #200
Despite better vacuum level the lifetime is significantly shorter.
This can be explained with a problem of the phase: The phase was jumping by ~180 degrees several times a day, which caused strong breakdowns.
Strong QE decrease started after a phase jump.
2014
C. Hessler et al., “Recent Results on the Performance of Cs3Sb Photocathodes
in the PHIN RF-Gun”, Proc. of IPAC’15, Richmond (2015), p. 1699.

## Slide 19: Cs3Sb Lifetimes after Installation of Vacuum Window
2.3 nC, 350 ns, l=524 nm
Cs3Sb #207
2.3 nC, 1.2 µs, l=524 nm
Cs3Sb #207
Phase was strongly drifting and therefore (occasionally) corrected manually and with new klystron phase loop.
Vacuum conditions very stable, only very rarely breakdowns.
1/e lifetime ~100 h, corresponds to lifetime of 170 h above QE=0.5%
Not as good as in 2012, maybe related to poor laser spot shape
Phase loop switched on
2016
2016

## Slide 20: Comparison with Cs2Te Lifetime
Measurement taken after separation of Faraday cup from the rest of the beam line by a vacuum window.
Operation with 1.6 µs (beyond PHIN specs), 2.3 nC/bunch and 0.8 Hz rep rate.
2.3 nC, 1.6 µs, 0.8 Hz, Cs2Te #203
2015
Vacuum at the exit of the gun stayed at low e-10 mbar level, whereas the vacuum in the new Faraday cup sector increased up to 4e-6 mbar.
No real decrease of the QE visible over 100h of beam operation!
Oscillations on the measured QE curve are due to problems with the temperature stability in the laser lab.
The phase was slowly drifting, probably also due to the problems with the temperature stability.
C. Hessler et al., “Study of the Performance of Cs2Te Cathodes in the PHIN RF
Photoinjector using Long Pulse Trains”, Proc. of IPAC’16, Busan (2016), p. 3960.

## Slide 21: Cs3Sb Lifetime Studies in DC Gun
Measurement in DC gun with 1 kHz / 2 kHz laser beam and Cs3Sb cathodes :
Total integrated charge produced: 321 mC (cathode #188), 35 C (cathode #202).
For low charge lifetime is significantly longer than in PHIN with same average current.
For high charge vacuum is still better than in PHIN, but lifetime worse.
1 µA average current, 1 nC/bunch
120 µA average current, 60 nC/bunch
2015
2013
Cs3Sb #188
Cs3Sb #202
I. Martini et al., “Studies of Cs3Sb Cathodes for the CLIC Drive Beam Photoinjector Option”, Proc. of IPAC’13, Shanghai (2013), p. 413.

## Slide 22: XPS Surface Analysis Studies of Photocathodes
Surface analysis of photocathode materials with XPS and their impact on the cathode performance studied in collaboration with CERN vacuum group.
New UHV carrier vessel (designed by and built in collaboration with LAL) allows to transfer cathodes under vacuum from production laboratory to the XPS setup.
XPS measurement allows material characterization of the surface. Together with qualitative elemental composition also chemical and quantitative information can be obtained (not straightforward).
  In this study a correlation between the chemical composition of the surface and the QE has been found. The poor photoemissive properties (of used cathodes) are accompanied by surface contamination and not good stoichiometry of the cathodes composition.
Transfer vessel
Courtesy I. Martini
I. Martini et al., “X-ray Photoemission Spectroscopy Studies of Cesium Antimonide Photocathodes for Photoinjector Applications”, Phys. Proc. 77 (2015) 34 - 41.

## Slide 23: XPS Analysis of Cs3Sb Cathodes
Courtesy I. Martini
Cs3Sb cathode #202 after production:
  Sb-rich phase
  O 1s peaks could be explained by Cs3O11 and H2O
After operation in DC gun:
  Sb-rich peak has increased
  Oxygen and carbon contamination is present and can be explained by CO32-: Cs has probably reacted with CO2 to Cs2CO3
  Cs3O11 or H2O not excluded
fresh
used
I. Martini, “Characterization of Cs-Sb cathodes for high charge RF photoinjectors”, PHD Thesis, Politecnico di Milano, 2016

## Slide 24: XPS Analysis of Cs3Sb Cathodes
Cs3Sb cathode #199 after operation in PHIN RF gun:
  Oxygen is the only contaminant.
  4 different states of Sb: Cs3Sb, alkali-deficient component, metallic Sb, Sb2O3
  O 1s level → Cs3O11 , Sb2O3
  Strong QE degradation is related to the oxidation.
  Sb-rich phase could either be created during production (no XPS measurement of this cathode before usage in PHIN available) or due to high energy ions/electrons impinging the cathode surface.
Courtesy I. Martini
fresh
used
I. Martini, “Characterization of Cs-Sb cathodes for high charge RF photoinjectors”, PHD Thesis, Politecnico di Milano, 2016

## Slide 25: Conclusion
Cs3Sb seems to be less robust than Cs2Te and more sensitive to non-optimal operation conditions.
For obtaining good lifetimes with Cs3Sb cathodes it is important to have the following conditions:
  Excellent vacuum conditions.
  A stable phase between the RF arriving in the gun and the laser arriving in the gun (no phase jumps, no slow drifts).
  To be in the linear charge extraction regime of the gun. Otherwise the non-extracted electrons cause desorption in the gun, which affects the cathode health.
  Probably a good laser beam shape.
In a stable environment, which is currently not available at CTF3, a sufficient performance with Cs3Sb cathodes might be still achievable.
More studies would be needed.

## Slide 26: Outlook
  CTF3 will be closed end of this year.
  PHIN program has come to its end. PHIN will be used for AWAKE project. → No real possibility to continue then CLIC drive beam photoinjector studies at PHIN due to different time structure of electron beam.
  Continue photocathode studies on a lower level. Photocathodes still needed for AWAKE, but with other properties.
  Final proof of feasibility of a photoinjector for CLIC drive beam anyway cannot be achieved with PHIN, due to its different parameters.
  New 1 GHz RF gun specially designed for the CLIC requirements needed.
  Probably new ideas needed, how to make photocathodes more robust.
Different macro-pulse repetition rates: 0.8 – 5 Hz (PHIN) 50 Hz (CLIC)

## Slide 27: AWAKE Project
Proton driven plasma wake-field acceleration experiment.
Electron gun needed for witness beam.
Installation at the former CNGS underground area.
Challenging space constraints.
Laser
dump
e-
SPS
protons
10m plasma
SMI
Acceleration
Proton
beam
dump
RF gun
Laser
p
Proton diagnostics
BTV,OTR, CTR
e- spectrometer
Laser room
Proton beam line
Electron beam line
RF gun
Klystron
Plasma cell
Experimental diagnostics

## Slide 28: AWAKE Electron Gun
Electron beam parameter requirements:
PHIN gun was chosen for AWAKE.
Challenging to achieve 1 nC bunch charge, small emittance and short bunch length at the same time with copper cathodes (Ablation seems to be an issue).
Parameter | Baseline | Range to check
Beam Energy | 16 MeV | 10- 20 MeV
Energy spread (s) | 0.5% | < 0.5% ?
Bunch Length (FWHM) | 10 ps | 0.3-10 ps
Beam Focus Size (s) | 250 µm | 0.25 – 1 mm
Normalized Emittance (rms) | 2 mm mrad | 0.5 - 5 mm mrad
Bunch Charge | 1 nC | 0.1 - 1 nC
Photocathode type | Cs2Te | Cu (or other metal) ?

## Slide 29: Acknowledgement
Collaborating CERN groups:
Lasers and photocathode section, equipment control section, vacuum group, beam instrumentation group, RF group, CTF3 operation team, and many others
Collaborating institutes:
… and thank you for your attention!
LA3NET is funded by European Commission
under Grant Agreement Number GA-ITN-2011-28919

## Slide 31
Backup Slides

## Slide 32: Motivation for a Drive-Beam Photoinjector
To generate the 12 GHz time structure of the drive beam, several fast 180 degree phase switches are needed, which is presently done by a sub-harmonic bunching system.
However, this system generates parasitic satellite pulses, which produce beam losses.
  Reduced system power efficiency
  Radiation issues due to the beam losses of the satellite pulses
These problems can be avoided using a photoinjector, where the phase-coding can be done on the laser side and only the needed electron bunches are produced with the needed time structure.
Satellite-free beam production at PHIN using laser phase-coding based on fiber-modulator technology has been demonstrated in 2011.
M.Csatari Divall et al., “Fast phase switching within the bunch train of the PHIN photo-injector at CERN using fiber-optic modulators on the drive laser”, Nucl. Instr. And Meth. A 659 (2011) p. 1.
 Satellites <0.1%
Figure courtesy M. Divall

## Slide 33: CTF3 Beam Combination Scheme

## Slide 34: Challenges for CLIC Drive-Beam Photoinjector
Achieve long cathode lifetimes (>150 h) together with high bunch charge (8.4 nC) and high average current (30 mA)
Produce UV laser beam with high power and long train lengths (140 µs)
  UV beam degradation in long trains
  Thermal lensing and heat load effects?
High charge stability (<0,1%)
→ Vacuum improvement, new cathode materials
→ Usage of Cs3Sb cathodes sensitive to green light → New UV conversion schemes with multiple crystals
→ Study the dynamics of laser system with full CLIC specs
→ Feedback stabilisation, → New fiber-based laser front end
Photocathode R&D
Laser R&D
Photoinjector optimization and beam studies

## Slide 35: Laser System
100W
3-pass amplifier
2-pass amplifier
3.5kW
8.3kW
7.8kW
14.8mJ in 1.2μs
2ω
3.6kW
4.67mJ
in 1.2μs
4ω
1.25kW
1.5mJ in 1.2μs
(=800nJ / laser pulse)
To CALIFES
photoinjector
To PHIN
Photoinjector /
Future 1 GHz gun
2ω
4ω
450μJ in 100ns
(=3μJ / laser pulse)
3-pass amplifier
1.5 GHz
Synched HighQ oscillator
Cw
HighQ pre-amplifier
500 MHz synched
Fiber oscillator
100 W burst fiber pre-amplifier
Phase coding setup
10W
New fiber-based front-end
M. Petrarca et al., “Study of the Powerful Nd:YLF Laser Amplifiers for the CTF3 Photoinjectors”, IEEE J. Quant. Electr. 47 (2011), p. 306.

## Slide 36: PHIN and CLIC Parameters
 |  | DRIVE beam | 
Electrons |  | PHIN | CLIC
 | charge/bunch (nC) | 2.3 | 8.4
 | train length (ns) | 1200 | 140371
 | bunch spacing(ns) | 0.666 | 1.992
 | bunch length (ps) | 10 | 10
 | bunch rep rate (GHz) | 1.5 | 0.5
 | number of bunches | 1802 | 70467
 | machine rep rate (Hz) | 5 | 100
 | margine for the laser | 1.5 | 2.9
 | charge stability | <0.25% | <0.1%
 | Cathode lifetime (h) at QE > 3% | >50 | >150
Laser in UV | laser wavelegth (nm) | 262 | 262
 | energy/micropulse on cathode (nJ) | 363 | 1988
 | energy/micropulse laserroom (nJ) | 544 | 5765
 | energy/macrop. laserroom (uJ) | 9.8E+02 | 4.1E+05
 | mean power (kW) | 0.8 | 2.9
 | average power at cathode wavelength(W) | 0.005 | 41
 | micro/macropulse stability | 1.30% | <0.1%
Laser in IR | conversion efficiency | 0.1 | 0.1
 | energy/macropulse in IR (mJ) | 9.8 | 4062.2
 | energy/micropulse in IR (uJ) | 5.4 | 57.6
 | mean power in IR (kW) | 8.2 | 28.9
 | average power on second harmonic (W) | 0.49 | 406
 | average power in final amplifier (W) | 9 | 608

## Slide 37: RF Lifetime of Cs3Sb Cathodes
Fast and slow decay visible as during beam operation.
In both cases longer lifetimes as during beam operation.
Lower vacuum level than during beam operation.
Conclusion: RF has a non-negligible influence on lifetime, but it is not the dominant factor.
Dynamic vacuum level: 2.5e-10 mbar
Dynamic vacuum level: 3e-10 mbar
Courtesy I. Martini
2014
2014
Fresh cathode
Cathode #200 (Cs3Sb)
Used cathode
Cathode #199 (Cs3Sb)

## Slide 38: Dark Current Studies
Field emission contribution from gun cavity (Cu) and cathode.
Cs3Sb cathodes (F~2 eV) produce higher dark current than Cs2Te (F~3.5 eV) and copper (F~4.5 eV). → Higher vacuum level for Cs3Sb than Cs2Te under same beam conditions.
The low dark current measured with copper confirms that the major contribution is coming from the cathode.
Courtesy I. Martini

## Slide 39: Cs2Te Lifetimes after 1st Vacuum Improvement
Lifetime measurements before and after the activation of the NEG chamber surrounding the gun cavity:
Cathode #185
Substantial improvement of dynamic vacuum level has resulted in drastic increase of 1/e lifetime from 38 to 250 h.
Corresponds to total cathode lifetime of 300 h above 3% QE.
l=262 nm
l=262 nm
C. Hessler et al., “Lifetime Studies of Cs2Te Cathodes at the PHIN RF Photoinjector at CERN”, Proc. of IPAC’12, New Orleans (2012), p. 1554.

## Slide 40: Cs2Te Lifetimes after 2nd Vacuum Improvement
After the installation of an additional NEG pump:
Double exponential fit represents well the data
Lifetime similar to previous measurement.
Cs2Te is not ultra-sensitive against non-optimal vacuum conditions
Dynamic pressure: 1.5e-9 mbar 3e-10 mbar
2014
2011
2.3 nC, 350 ns, Cs2Te #185
2.3 nC, 350 ns, Cs2Te #198
t2 = 300 h

## Slide 41: 5 Hz Operation with Cs2Te Cathode
Operation with 1.6 µs (beyond PHIN specs), 2.0 nC/bunch and 5 Hz rep rate.
2.0 nC, 1.6 µs, 5 Hz, Cs2Te #203
2015
QE seemed initially to decrease, but could be restored by changing the phase. → Evident that phase is drifting.
Also in this measurement, QE seems to be constant.
C. Hessler et al., “Study of the Performance of Cs2Te Cathodes in the PHIN RF
Photoinjector using Long Pulse Trains”, Proc. of IPAC’16, Busan (2016), p. 3960.

## Slide 42: XPS Analysis of Cs2Te Cathode
Courtesy I. Martini
Cs2Te cathode #203 after production:
  No oxygen or oxide contamination visible.
  Good stoichiometry n(Cs)/n(Te)=~2
  Copper from substrate visible
After operation in PHIN:
  TeO3 and metallic Te were formed during degradation process
  Larger quantity of Cu visible, probably coating has been partially removed by ion bombardment.
I. Martini, “Characterization of Cs-Sb cathodes for high charge RF photoinjectors”, PHD Thesis, Politecnico di Milano, 2016