## Slide 1: Simulation photo-emission from K2CsSb photocathode
Erdong Wang on behalf of electron source group
BNL

## Slide 2: Outline
Motivation
A preliminary analytical model
Monte-Carlo simulation
Three step model
Simulation results
Compare to experiment
Schottky effect

## Slide 3: Motivation
We observed strong QE decay when cool down the cathode to 77K.
Schottky effect was observed in 704MHz gun beam test.
To understand the photoemission and cathode performance inside the gun.
Spectrum response
Schottky effect
QE change at different temperature

## Slide 4: An analytical model
1. Assumed a Maxwell-Boltzmann distribution,
With kBT equals to σ
PHYSICAL REVIEW B 66, 115102(2002)
2. Due to low laser power, the conduction band has sufficient states to accept the excited electrons.
3. Scattering or collision is not considered explicitly during the transport step. However, the tail in the density distribution takes these effects into consideration implicitly.
4. the energy is conserved. Momentum conservation is not considered here.

## Slide 5: Results
Electron distribution above the conduction band
Fitting parameters for absorption:
B. K. Chang, et al., Proc. SPIE 1982, Photoelectronic Detection and Imaging: Technology and Applications 174 (1993)
By fitting the analytical model with the experimental data (297K to 166K), we got:
Varshni. Y. P. physica (1967) 34 149-154

## Slide 6: Monte-Carlo simulation
To understand the K2CsSb photocathode photoemission, we developed a python-based 2.5 D Monte-Carlo simulation code based on Spicer’s three step model. To reduce the assumptions in analytical model.
Using referenced density of states .
Considering carrier scattering and the electron-phonon scattering
Considering momentum conservation.
Could we know the thermal emittance and temporal response from the code?
How the thickness effect the QE?
This code pre-set parameters came from many references.

## Slide 7: Electrons excitation
We used K2CsSb density of state. The energy distribution of excited electron is DoSVB DoSCB(hv)
ERL 2015
CsK2Sb photon absorption coefficients
L.Kalarasse et al., J. Phys. Chem. Solid. 71, 1732 (2010)
PHYSICAL REVIEW B 66, 115102(2002)
J. Phys. Chem. Solid. 71, 1732 (2010)

## Slide 8: Initial electrons distribution
2.3 eV
6 eV
532nm

## Slide 9: Some useful data
K. L. Jensen, et al., J. Appl. Phys 104, 044907 (2008)
Effective mass
Eg(eV) | Ea(eV) | 
1.1 | 0.65 | NRL
1.2 | 0.7 | Ghosh C and Varma B P. J. Appl. Phys, 1978, 49 (8): 4549-4553
1.2 | 0.7 | CPC(HEP & NP), 2012, 36(6): 531–537
1.6 | 0.2 | A. R. H. F. Ettema , PHYSICAL REVIEW B 66, 115102 ~2002
1 |  | Nathan, R., Mee, C. H. B.: Int. J. Electron. 23 (1967) 349
1.2 |  | Sommer, A. H.: Photoemissive Materials, John Wiley, New York 1968
1.4 |  | Kalarasse et al, Journal of Physics and Chemistry of Solids 71 (2010) 314–322
W. E. Spicer, SLAC Report NO.SLAC-PUB-6306(1993).
e-e scattering

## Slide 10: Phonon scattering in electrons transport
Electron phonon scattering:
Electrons scatter from one valley to another by absorbing or emitting an optical phonon of energy.
Ek’ = Ek+-hω where hw is the phonon energy (0.027eV)
Electron will not loss energy in scattering once the energy of the electron is less than one phonon energy above the minimum of the conduction band.
Each scattering-> change energy-> change angle-> update (px, py,pz)->update (y,z)
V. Beguchev J. Phys. : Apl. Phys. 26 (1993) 4499-4502

## Slide 11: Electron –electron/hole scattering
Ee-ECB>Ebandgap
If the energy of electrons is higher than the minimum of the conduction band by n E,E:[Eg,Eg+VB width] it is possible that e-e scattering can happen up to n times.
The surface defects could result in p-doping, and then the Fermi level could lie closer to the maximum of the valence band, enabling holes to exist in the valence band.
the electron will lose energy in the range of zero to the width of the valence band from the DoS of K2CsSb to the hole.
Electron-hole scattering:
Electron-electron scattering:

## Slide 12: Emission
Vacuum
Cathode
If the electron’s energy is less than the electron affinity, electrons come back and encounter another diffusion iteration.
If the electron’s energy is more than the electron affinity, consider the transverse momentum continuity.
py,out
py,in
pin
pout
CB
VB
Cathode
Vacuum

## Slide 13: QE , thermal emittance vs wavelength
Thermal Emittance:
QE: # emitted electrons / # incident photons
e-e scattering energy loss:
n * energy gap+width; n=1,2…
e-h scattering energy loss:
0~1.2 eV, VB width
e-p scattering:0.027eV
The EA is 0.5 eV by fitting.
e-e and e-h scattering : continuous increase
e-e scattering: QE drop at high photon side.

## Slide 14: QE vs thickness
For a thickness ≥ 20 nm, the QE is independent of the cathode’s thickness.
Three cathodes were made in Sb thickness of 1.3nm, 15nm and 41nm. We also tried 60nm of Sb, QE is about 10%.

## Slide 15: Thickness vs temporal response
For the typical 50 nm thickness cathode, the simulated response time is 170 fs (90% of the electrons emitted) from the curve

## Slide 16: QE in 77K

## Slide 17: Schottky effect compensates the band gap change
Surface barrier change due to Schottky effect:
K2CsSb relative permittivity: 9.2
L. Kalarasse, B. Bennecer Journal of Physics and Chemistry of Solids Volume 71, Issue 12, December 2010, Pages 1732–1741
With 20MV/m gradient , from the Schottky effect induced potential change is above 0.08eV
Peak current 1.65A
Gradient 12 MV/m
If cathode at 300K, no Schottky effect

## Slide 18: Summary
The QE degradation due to cold cathode was studied. Our conclusion is that QE decay is induced by band gap(ionization energy) change. We observed the Schottky effect by scanning the RF phase.
A preliminary analytical model was developed.
One Monte-Carlo code was developed to simulate photoemission from the multi-alkali photocathode.
The performance of considering e-h ,e-e and e-p scattering match to our spectrum response curve and thickness dependence.
The code could estimate the temporal response.
It could generate particles for Parmela or Astra simulation.
Thanks to J. Smedley and D. A. Dimitrov on cathode modeling discussion!

## Slide 19
Thanks for you attention!