## Slide 1: Limits on emittance from solid photocathodes due to surface non-uniformities
- Siddharth Karkare
Physical Roughness
Chemical roughness
Quantum scale effects
Acknowledgements –
Ivan Bazarov (Cornell)
Howard Padmore (LBNL)
Zihao Ding (LBNL)
Susanne Schubert (LBNL)
Jun Feng (LBNL)
Notes: We saw several ways to obtain ultra low emittances (tips, ultracold atoms etc). In this talk, I will give a perspective about what problems we should expect while attempting to achieve ultralow emittances from solid state photocathodes. Strategies to reduce emittance, then talk about various factors that will limit emittance – physical roughness, chemical roughness and quantum scale effects.

## Slide 2: Where we are?
25-40 meV – near threshold
Metals
  Very low QE<10-7
Alkali-antimonides
  Low QE <10-4.
GaAs/(Cs,O)
  Very long response time
Practically used in most photoinjectors
1 eV
100 meV
1 meV
10 meV
(1.4 μm/mm)
(0.44 μm/mm)
(0.14 μm/mm)
)
(0.04 μm/mm)
ULTRACOLD ELECTRONS

## Slide 3: Strategies to reduce emittance
Disordered surfaces –
Disordered over layers on ordered materials (GaAs(Cs/O))
Polycrystalline/amorphous materials (alkali antimonides, polished metals)
if  0
Strategy: Operate at near threshold and cryo-cool cathodes
Both assume isotropic emission of electrons 
Physical and chemical roughness both will be an issue
Emission best explained by 3-step model
Dowell’s theory for polycrystalline metals and alkali antimonides
Monte-Carlo simulations for GaAs(Cs/O)
Notes: Ordered surfaces – Conservation of transverse momentum, small transverse effective mass – are physically atomically smooth by definition, may still have chemical roughness- may show directed emission (eg – narrow cone from GaAs)

## Slide 4: Strategies to reduce emittance
Ordered surfaces –
Can obtain LEED pattern, Clean auger spectrum
Have not been demonstrated in guns so far
Emittance given by band-structure –
Use low transverse effective mass
Surface states
Hole-like bands
Physical roughness by definition not an issue for most ordered materials
Chemical roughness may be present due to varying surface terminations

## Slide 5: Limits on emittance from solid photocathodes due to surface non-uniformities
- Siddharth Karkare
Physical Roughness
Chemical roughness
Quantum scale effects
Notes: We saw several ways to obtain ultra low emittances (tips, ultracold atoms etc). In this talk, I will give a perspective about what problems we should expect while attempting to achieve ultralow emittances from solid state photocathodes. Strategies to reduce emittance, then talk about various factors that will limit emittance – physical roughness, chemical roughness and quantum scale effects.

## Slide 6: Physical roughness
First discussed by Bradley – Slope effect and Field Effect
For disordered surfaces
– isotropic emission
– near 0 K.E at emission
 Negligible slope effect
Consider only field effect
D.J. Bradley et al., J. Phys. D: Appl. Phys 10, 111 (1977)

## Slide 7: Field effect
Calculate electron trajectories in roughness distorted field to obtain increase in MTE
for

## Slide 8: Modelling field effect
Possible to calculate this for any surface by decomposing the field into Fourier components
T. Gorlov, Journal of Electrostatics 65, 735 (2007)
S. Karkare et al., Proceedings of 2011 Particle Accelerator Conference, New York, NY, USA, THP192
Accelerating field
Distortions due to
surface roughness
>>

## Slide 9: Alkali antimonide example
Co-deposition – 0.6 nm rms
UHV-AFM measurements
Sequential deposition – 2.5 nm rms
Electric field | 5 MV/m | 20 MV/m | 100 MV/m
Rough cathode (sequential deposition) | 16.6 meV | 66.6 meV | 333 meV
Smooth cathode (Co-deposition) | 2.1 meV | 8.3 meV | 41.5 meV
For ultra-cold electrons (~2 meV)
Need atomically smooth cathodes!!
~ 100K
~ 25K

## Slide 10: Limits on emittance from solid photocathodes due surface non-uniformities
- Siddharth Karkare
Physical Roughness
Chemical roughness
Quantum scale effects
Notes: We saw several ways to obtain ultra low emittances (tips, ultracold atoms etc). In this talk, I will give a perspective about what problems we should expect while attempting to achieve ultralow emittances from solid state photocathodes. Strategies to reduce emittance, then talk about various factors that will limit emittance – physical roughness, chemical roughness and quantum scale effects.

## Slide 11: Chemical roughness
surface adsorbates
different grain orientations
different surface terminations
Kelvin Probe Force Microscopy on CsKSb
Measured at LBNL
Energy Resolved or Tunable wavelength PEEM
+Renault et al. Surf. Interface Anal. 2006; 38: 375–377
~0.5 V variations on clean polished Cu
Surface potential (V)

## Slide 12: Modelling chemical roughness effect
x,y
z
Electric field
is potential variation
is periodicity
and
Say V, nm
MV/m
= 17 meV @ MV/m
= 8 meV @ MV/m
Karkare and Bazarov, Phys. Rev Applied, 4, 024015 (2015)

## Slide 13: Complications in modelling
For - Emitted electrons can re-enter the cathode
Electron emission is also non-uniform –
  Low work function regions emit more electrons
  Increased space charge effects
Can result in electric fields inside
cathode surfaces
More complications if physical
and chemical roughness are
present
Karkare et al. Phys. Rev Applied, 4, 024015(2015)

## Slide 14: Limits on emittance from solid photocathodes due surface non-uniformities
- Siddharth Karkare
Physical Roughness
Chemical roughness
Quantum scale effects
Notes: We saw several ways to obtain ultra low emittances (tips, ultracold atoms etc). In this talk, I will give a perspective about what problems we should expect while attempting to achieve ultralow emittances from solid state photocathodes. Strategies to reduce emittance, then talk about various factors that will limit emittance – physical roughness, chemical roughness and quantum scale effects.

## Slide 15: Quantum scale effects
100 meV electrons  Wavelength > 4 nm
10 meV electrons  Wavelength > 10 nm
For surface variations with period of few nm quantum interference matters
e-
1 nm
Scattered electrons
For example –
Sub-nm scale surface roughness can act as a diffraction grating to scatter emitted electrons

## Slide 16: GaAs example
V
0
zmin
zmax
GaAs
Vacuum
GaAs
Vacuum
Interface
S(z) is the heavy-side function
Simplified surface – no Cs barrier, no work function variation
1 nm
Karkare and Bazarov, Phys. Rev Applied, 4, 024015 (2015)

## Slide 17: GaAs example
1 nm
Scattered electrons
Sub-nm scale roughness can be due to surface reconstructions, atomic steps or surface defects
Can explain experimental results
Karkare and Bazarov, Phys. Rev Applied, 4, 024015 (2015)

## Slide 18: Conclusions
To achieve 1-2 meV scale MTE need atomically smooth cathodes
Chemical roughness or work function variations can be a major obstacle
Need to measure chemical roughness on cathode surfaces and develop simulations to calculate its effects on electron emission
Understand quantum scale effects in photoemission