## Slide 1: Vacuum considerations for JLEIC beamline and Interaction Region Marcy L. Stutzman
Notes: Title Page Design 3

## Slide 2: General considerations for beamline vacuum design
Static vacuum design
  Materials: material, heat treat, surface preparation
  Pumping systems: distributed and lumped pumps
Dynamic vacuum design
  Electron stimulated desorption, secondary electron yield
  Photon stimulated desorption
    Beamline shape for PSD reduction as needed

## Slide 3: Modeling available for both static vacuum and PSD
Molflow+ and Synrad modeling software developed by Roberto Kersevan
Jason Carter, ANL, used Molflow+/Synrad to model static and dynamic vacuum for APS upgrade
CAD designs of beamline are combined with pumping speeds and outgassing rates of elements yield expected pressure

## Slide 4
How SynRad works
Magnetic elements in orange, program generated synchrotron fan in green, surface hit points in red
Magnetic elements generate synchrotron rays within 3D space
BEAM
DIRECTION
APS-U storage ring vacuum system design using SynRad/MolFlow+ with photon scattering
Jason Carter, AVS 2015 presentation

## Slide 5
Coupled simulations
Coupling feature translates SynRad flux density rates (photons/cm2/s) to photon stimulated desorption, PSD, outgassing (mbar*L/cm2/s)
Translations based on conditioning time and PSD yield measurements for various vacuum materials
Jason Carter, AVS 2015 presentation

## Slide 6: What is needed to use modeling software?
Understanding of materials properties for beamline
  Outgassing rates
  Pump speeds
  Electron/Photon stimulated desorption
Detailed CAD design of the interior of the vacuum space
Accelerator vacuum community are researching these issues
→ This talk summarized recent workshop

## Slide 7: Summary of the International Workshop on Functional Surface Coatings and Treatments for UHV/XHV Applications
Workshop hosted by Daresbury Laboratory, September 2015
Coatings
  TiN coatings
  Carbon coatings
  Non-evaporable Getter (NEG) coatings
  Surface texturing effects
Tests
  Outgassing/pumping
  Electron/Photon stimulated desorption
  RF surface resistivity
Participants from
  Argonne (US)
  Brookhaven (US)
  CERN (EU)
  Cornell (US)
  Daresbury/Cockcroft/Astec (UK)
  DESY (Germany)
  IHEP (China)
  LNF-INFN (Italy)
  JLab (US)
  KEK (Japan)
  LBNL (US)
  MAX IV (Sweeden)
  Pohang (Korea)
  SNS (US)
  SAES Getters (pump company)
  VACOM (pump company)
Presentations available under “program” link at
https://www.cockcroft.ac.uk/events/FSC/index.html

## Slide 8: Static vacuum design
Conductance to pumping elements
Reduced outgassing materials
Modeling in Molflow+ or similar can determine requirements for pump sizes

## Slide 9: Dynamic vacuum
Measurements of Secondary Electron Yield
Measurements of Electron/Photon Stimulated Desorption (ESD/PSD)
Effect of Coatings and surface treatments
  Carbon (amorphous or HOPG)
  Titanium Nitride (TiN)
  Non-evaporable getters (NEG)
  Surface patterning/grooves
Beampipe design for discrete/distributed pumping

## Slide 10: Secondary Electron Yield: electron cloud, vacuum excursions
Shigeki Kato, KEK

## Slide 11: Patterning of surfaces
Reza Valizadeh, Daresbury
Laser patterning
L. Olano Garcia, CSIC, Spain
wet chemical deposition

## Slide 12: SEY: Laser Engineered Surface
Laser engineered surface (LESS)
Sergio Calatroni, CERN
Relatively new approach

## Slide 13: TiN Coatings on Aluminum and grooved aluminum: SEY Kyo Shibata SuperKEKB

## Slide 14: SEY summary
Bare metals tend to have peak SEY >1, can lead to electron cloud
Coatings (carbon, TiN) or patterning (LESS, grooves) will reduce SEY
Historical measurements of NEG coatings gives SEY slightly >1, new work proceeding on optimizing NEG films
Importance of materials properties (Hydrogen content), standardization of testing protocol (normal vs. grazing incident electron beam)

## Slide 15: Pressure increase due to SEY
Shibata, KEK: scrubbing needed for TiN coated pipes in SuperKEKB

## Slide 16: Carbon Coatings vs. NEG coatings: Photon Stimulated Desorption Yasunori Tanimoto, KEK
a-Carbon excellent for photon stimulated yield of secondary electrons
However, other gasses desorbed from a-Carbon make it bad for the vacuum (compared to NEG coating)

## Slide 17: Distributed NEG pumping
Antechamber designs: NEG strips integrated into beampipe
LEP: early implementation
SuperKEK: recent design

## Slide 18: NEG coatings
Non-evaporable getter can be coated onto the beampipes
  Provide distributed pumping
  Reduce ESD/PSD
Drawbacks
  Higher cost than some other coatings
  Requires in-situ heating for activations
Structure
  columnar vs. amorphous?
  Composition: binary-quartenary to optimize activation temperature, pump speed (Daresbury)
Excellent option for areas where discrete pumping impossible

## Slide 19: NEG coating for MaxIV: various shapes
Straight segments: ESRF
Curved sections: industry contractor
Special shapes: collaborate with CERN

## Slide 20: NEG coating: long thin pipes
LBNL: Narrow chambers
SAES getters: 10 mm – 4 mm
See morphology from twisted wires
Need alloy wire (Andre Anders)
SAES can achieve good adhesion and morphology even on challenging thin pipes

## Slide 21: JLEIC vacuum design
Vacuum design must
  Limit outgassing
  Mitigate ESD, PSD, SEY
  Optimize pumping systems
Goal: P~1x10-9 Torr
Sources of dynamic vacuum loads?

## Slide 22: Summary
Molflow+: static vacuum modeling
SynRad: model of vacuum events due to beam
Beam related pressure mitigation
  Coatings (TiN, carbon, NEG)
  Morphology (grooves, laser patterning)
  Antechambers to provide pumping, mitigate PSD
Vacuum system design must take into account
  Outgassing
  ESD, PSD, SEY induced vacuum
  Pump design (distributed and lumped)