## Slide 1: Superferric Magnets for MEIC
Peter McIntyre
October 8, 2015
Peter McIntyre
Texas A&M University

## Slide 2: Superferric Magnets for the Ion Ring and Booster
R = 155.5 m
Arc, 261.7
IPs
disp. supp./
geom. match #1
disp. supp./
geom. match #1
det. elem.
disp. supp.
rm.+
SRF
beam exp./
match
el. cool.
ions
Ion Ring– 128 arc half-cells
Booster – 32 arc half-cells
Superferric magnets have been designed for the requirements of arc half-cells:
Ion Ring: 8-100 GeV protons: 0.25 -- 3 T dipoles, 52 T/m quads
Booster: 0.2-8 GeV protons: 0.24 – 3 T dipoles, 6 T/m quads

## Slide 3: Half-cell cryostat geometry for Ion Ring arcs
= leads
= fixed anchor to support post
= sliding anchor to support post
= sliding shroud section of vacuum vessel
F
S
F
F
F
S
S
11.4 m overall half-cell length
Dipole aperture requirement: betatron amplitude (15 s) @ injection: ±3 cm
dispersion of ±0.5% momentum spread: ±1 cm sagitta (with 4 m dipole length): ±1.8 cm
±5 cm
Quad aperture radius requirement: 4 cm
Each half-cell contains two 4 m dipoles, one 0.8 m quadrupole, 1 sextupole to correct body sextupole in dipoles (Neuffer):

## Slide 4
Superferric Magnets – Cost Minimum up to ~4 T
3 T SSC dipole
2 T pipe dipole for VLHC
1 T strong-focusing cyclotron
3 T proton gantry for particle beam therapy
4.5 T for 100 TeV hadron collider
2 T FAIR dipoles

## Slide 5: MEIC Arc dipole
The biggest challenge is to create a 10 cm x 6 cm aperture with the field quality needed for high-luminosity collisions with long luminosity lifetime – dynamic aperture

## Slide 6
Chart: Load Lines
| 0.5 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
NbTi short sample @ 4.5K | 40677.1463 | 37055.3026 | 31492.2055 | 26676.7997 | 22797.0368 | 17875.9938 | 13691.6668 | 9603.3735 | 5583.6757 | 1618.8544 | 0
Bmax in coil | 750 | 1500 | 3000 | 4500 | 6000 | 7500 | 9000 | 10500 | 12000 | 13500 | 15000 | 16500 | 17250
Bbore | 750 | 1500 | 3000 | 4500 | 6000 | 7500 | 9000 | 10500 | 12000 | 13500 | 15000 | 16500 | 17250
short sample in coil | 19750
short sample in bore | 19750
Multipoles vs. field and load lines for MEIC dipole design.
Injection @ 8 GeV collision @ 100 GeV
20 s contours,
± sagitta
10 s contours,
± sagitta
Green is good!
The fields seen by the ion beams…

## Slide 7: Cable-in-Conduit: Dubna to GSI to MEIC
The SIS-100 ring uses superferric dipoles operating at 1.8 T.
Its conductor is a semi-rigid cable-in-conduit, in which the helium cryogen flows internally so that the magnet is not immersed in liquid helium.
Cable-in-conduit makes a much simpler end geometry for a large-bore dipole. The windings can be supported in a reinforced polymer structure, with tight precision.

## Slide 8: We follow the Dubna/GSI CIC strategy with a few improvements for higher-field operation
15 NbTi/Cu wires are cabled onto a perforated spring tube.
The cable is inserted in a sheath tube, and the sheath is drawn onto the cable to just compress the wires against the spring tube.

## Slide 9: Superferric Dipoles: How we build them
3. Insert the SS beam tube, seal the ends, and epoxy impregnate the gap between segments and beam tube.
Fabricate inner form segments from 4”-thick G-11 fiber-reinforced epoxy slab.
Assemble stack of segments for dipole body, using the CIC channels for alignment.
Strategy:
All cables are positioned sandwiched between layers of precision-machined structure.
Ends are formed to the side of the dipole, then popped into place in the structure layer.
Overall coil assembly is preloaded within steel flux return, all windings immobilized.

## Slide 10: Assembly/alignment / epoxy impregnation of beam tube & winding structure

## Slide 11
All ends are formed with 2” radius bends.
1. Bend a U with the correct horizontal spacing.
Bend the U to form a 90° ear, with offset for layer-layer transitions.
3. ‘Odd-man’ turns require forming a ‘dog-bone’ end.
Forming the flared ends requires production tooling
We have validated that bends preserve internal structure, do not damage NbTi wires.
See videos of the real tools making these bends at https://goo.gl/VoSDOS

## Slide 12: Mockup Winding – Layer 1 wound

## Slide 13: Measurement of cable positions for Layer 1
1
2
5
6
4
3
3
4
5
6
7
8
9
10
11
12
13
16
Right
left
1
2
15
14

## Slide 14: Error matrix from magnetic model: bn, an from .001” error on each cable x,y

## Slide 15: Measure cable positions for Layer 1
Extract random multipoles from cable placements in Layer 1:
Preliminary cable placement measurements for Layer 1:

## Slide 16: Next: the complete fabrication
Body segments assembled on beam tube, jig-located, epoxy-impregnated
SS bars, end frames installed, ready to wind first layer
First layer wound
Second layer wound
Third layer wound
Cable frame complete, End covers installed
Ti channels, SS top/bottom skins installed
Flux return halves installed and closed, SS shells welded

## Slide 17: Quench Protection
Quench heater foils are bonded in a 10 cm end segment of the G-11 structure on both ends of the dipole.
Every cable turn is driven normal in ~10 ms by a current pulse to the heater foils.
Chart: Peak Temperature
Chart: MIITs
Maximum pressure during quench in the 250 m length CIC of a 4 m dipole = 41 bar

## Slide 18: Provision for differential contraction, preload against Lorentz forces in body
Horizontal contraction
Chart: Central Multipoles Cold+Forces @2cm
| 0.18723999999999999 | 0.37462000000000001 | 0.74938000000000005 | 1.1240699999999999 | 1.4982899999999999 | 1.86812 | 2.2139000000000002 | 2.51946 | 2.7833600000000001 | 3.0171700000000001 | 3.2340200000000001 | 3.44123 | 3.54284
b2 | 0.23362 | 0.2032 | 0.15959 | 0.12656 | 0.16161 | 0.6489 | 0.71925 | 0.12544 | -0.71964 | -0.42286 | 0.8218 | 2.5409 | 3.5519
b4 | -1.0319 | -1.0328 | -1.0316 | -1.0301 | -1.0276 | -1.0507 | -1.0782 | -1.0287 | -0.83787 | -0.66137 | -0.50464 | -0.35998 | -0.29151
b6 | 1.0677 | 1.067 | 1.0666 | 1.0664 | 1.0653 | 1.068 | 1.0971 | 1.1826 | 1.2908 | 1.3972 | 1.4938 | 1.5805 | 1.6206
b8 | -0.33758 | -0.33744 | -0.33741 | -0.33747 | -0.33733 | -0.33692 | -0.33898 | -0.35037 | -0.36819 | -0.38702 | -0.40512 | -0.4221 | -0.43011
Orient G-11 with fabric perpendicular to beam tube axis – small contraction.
Locate Ti U-channels to compensate differential contraction – warm-cold ~+.002”
Locate SS/mica paper slip plane between G-11 and steel flux return.
Ti
G-11
316 SS
Steel

## Slide 19: CIC winding limits temperature rise in event of heat from beam losses
Simulated temperature distribution in the presence of 1 W heat deposition in a MEIC dipole winding.
4.5 K
4.4
4.3
4.2
CIC structure controls Lorentz stress, prevents coil motion, error fields
Y displacement (RT – 3 T) .001”
X displacement (RT – 3 T) .001”
Multipole effects <0.2 units

## Slide 20: Half-cell cryostat
Support load from 5 reentrant feet.
Supports integrate provisions for precise positioning & internal alignment of all elements.
50 K shield, MLI, and top-half shell go on after all alignment. Ports for checking alignments.
Static heat loads ~0.5 W to 4.5 K, 50 W to 50 K.

## Slide 21: Booster (8 GeV, gt = 16.8 i)
injection
extraction
RF cavity
Crossing angle:
79 deg.
Injection: multi-turn 6D painting
  0.22-0.25 ms long pulses ~180 turns
  Proton single pulse charge stripping at 285 MeV
  Ion 28-pulse drag-and-cool stacking at ~100 MeV/u
  Ion energies scaled by mas-to-charge ratio to preserve magnetic rigidity
Ekin = 285 MeV – 7.062 GeV
Ring circumference: 273 m
(≈ 2200/8)
21
275.087
0
40
0
5
-5
BETA_X&Y[m]
DISP_X&Y[m]
BETA_X
BETA_Y
DISP_X
DISP_Y
Straight
Inj. Arc (2590)
Straight (RF + extraction)
Arc (2590)
Bogacz

## Slide 22: Booster arc magnets
For planning purposes we could provide the required fields and apertures for the Booster magnets by building Ion Ring arc dipoles and quads with appropriate lengths:
Dipole 1.2 m Quad 0.4 m
It may likely prove to be the case that making the dipoles of a common design is less expensive than making dedicated designs with smaller quad gradient.

## Slide 23: Current Status of Development
We have built a 1.2m mockup winding:
  Developed all tooling for coil fabrication.
  Fabricated all G-11 piece-parts for 3-layer structure.
  Use Cu-Ni tube drawn to same size as CIC.
  Wind the three-layer structure to evaluate methods.
  Map locations of all cables, predict random multipoles.

## Slide 24
Fabricate CIC cable
Build laminated flux return
QC cable positions of all turns in dipole
Texas A&M group will propose NP funding for fabrication of a 1.2 m model dipole
Assemble winding in flux return, preload
Measure cable positions under preload
Ready to test model dipole in 2017

## Slide 25
JLEIC External Review:
What would be cost impact of 100 GeV ions?
What would a 6 T CIC dipole look like?

## Slide 26: 6 T CIC dipole
Design field B0 | 3 T | 6 T
Coil current | 13.7 kA | 17.2 kA
Coil field @ B0 | 3.5 T | 6.9 T
Bore field @ SS | 3.8 T | 6.2 T
# turns in coil | 24 | 54
Cable: |  | 
# strands | 15 | 14
strand dia. | 1.2 mm | 1.5 mm
total s.c. area | 8 cm2 | 27 cm2
Flux return size | 20 cm | 33 cm
Magnet cost for a CIC dipole is proportional to # turns, flux return size.
On that basis, 6 T dipoles would cost ~2.25 x cost of 3 T.
Compare to cos q, for which cost ~ B2.

## Slide 27: 6 T coil structure is same as for 3 T CIC dipole, but 5 layers instead of 3 layers
So building/testing a 3 T model dipole would go far toward validating the 6 T cousin.

## Slide 28: Continuous Tube-Forming of Sheath on Cable-in-Conduit
Hyper Tech developed a Continuous Tube Forming and Filling machine for continuous multifilament wire encapsulation and laser welding of in-situ MgB2 wire and multifilament cable.
HyperTech is adapting their CTFF process to continuously form the sheath cable onto long lengths of NbTi CIC.
Key challenge: demonstrate that the laser-weld is He-tight warm and cold.
Related SBIR project

## Slide 29: Compression-molded fiber-reinforced polymer parts for the CIC winding structure
RockWest fabricates FRP components by compression-molding. They have experience with cryo-compatible FRP materials, and holding tight dimensional tolerance.
Expensive at the front end to develop molds, perfect fab process for the desired parts.
Payoff is per-piece cost thereafter is ~$10,000 for 4 m body structure, vs.
~$20,000 for 4 m body structure using NC-machined G-11 parts.