## Slide 1
Sam Posen
TTC High Q0 Meeting
18 May 2016
Cavity Treatment for High Q0 in Realistic Magnetic Fields

## Slide 2: Flux Expulsion
Need to preserve high Q0 from vertical test into cryomodule
When flux from background magnetic field is trapped, Q0 is degraded
Important recent results:
  Spatial thermal gradients during cooldown can significantly improve expulsion of magnetic flux
  Flux expulsion behavior can be substantially enhanced through UHV furnace treatment
Expulsion
Trapping

## Slide 3: This Study
Critical questions for this study:
What is the effect of realistic applied fields (e.g. LCLS II spec <5 mG) on Q0?
Can UHV furnace treatment substantially mitigate the effect?

## Slide 4: This Study
Critical questions for this study:
What is the effect of realistic applied fields (e.g. LCLS II spec <5 mG) on Q0?
Can UHV furnace treatment substantially mitigate the effect?
Two single cell 1.3 GHz cavities for this study – fabricated by AES with RRR Nb from Ningxia:
TE1AES024 – LCLS II baseline recipe: bulk EP, degas and nitrogen-dope 2/6 at 800 C, 5 micron EP
TE1AES025 – Modified LCLS II recipe: 900 C furnace treatment, bulk EP, degas and nitrogen-dope 2/6 at 800 C, 5 micron EP

## Slide 5
External
field coils
0.2
0.4
0.8
1.0
1.2
1.4
1.6
1.8
2.0
0.0
0.6
Bz/Bz0
Fluxgate magnetometer
Temperature
sensor
Bz0

## Slide 6: Flux Expulsion
Poor expulsion: BSC/BNC ~ 1.3
Good expulsion: BSC/BNC ~ 1.6
Magnetometers
Thermometers
Magnetometers
Thermometers

## Slide 7: Flux Expulsion Results

## Slide 8: RF Results – 2.0 K

## Slide 9: RF Results – 2.0 K
Substantial Q0 degradation
No degradation observed!
Only difference: 900 C 3 h before bulk EP – big effect!

## Slide 10: RF Results – 1.5 K

## Slide 11: RF Results – 1.5 K
Substantial Q0 degradation
No degradation observed!
Only difference: 900 C 3 h before bulk EP – big effect!

## Slide 12: Summary
Two cavities nearly identical except for 900 C 3 hr treatment before bulk EP
The cavity with 900 C 3 hr treatment shows much stronger flux expulsion
The cavity without 900 C 3 hr treatment shows substantial degradation due to trapped flux after cooling in a field of 5 mG, even with ΔT~5 K
The cavity with 900 C 3 hr treatment shows no observable degradation even with ΔT~2 K
Even when we deliberately tried to cool the cavity slowly, it expelled the majority of applied field!