## Slide 1
Martina Martinello
High Q TTC Meeting,19 May 2016
Surface resistance studies as a function of the mean free path

## Slide 2: Surface Resistance Contributions
Trapped flux surface resistance:
BCS surface resistance:

## Slide 3: Trapped Flus Surface Resistance
The trapped flux surface resistance depends on:
    The amount of trapped flux
          External magnetic field ()
          Level flux expulsion during SC transition
    Surface treatment (mean free path, )

## Slide 4: Trapped Flux Surface Resistance
In order to estimate :
Slow cooldown with
In order to estimate :
Cavity cooled in compensated field ( ) OR
Fast cooldown with efficient flux expulsion

## Slide 5: Trapped Flux Sensitivity
How much the cavity dissipated per amount of trapped flux:

## Slide 6: Sensitivity vs mean free path
2/6 N-doping

## Slide 7: Trapped Flux Sensitivity Field Dependence

## Slide 8: Sensitivity Summary
Bell-shaped trend of sensitivity as a function of mean free path
Sensitivity is lower at both very low value (120 C bake) and very large value (EP) of mean free path
Over-doped cavities fall at the maximum of the curve
LCLS-II doping recipe ( 2/6 N-doping ) minimizes trapped flux sensitivity of N-doped cavities
Sensitivity increases with the accelerating field

## Slide 9: BCS vs mfp
N-doping allows to tune the mean free path and reaching the theoretical minimum of RBCS vs mean free path
Different theoretical curves for standard Nb cavities and N-doped cavities
  → Mean free path is not the only parameter changing with N-doping
  → N-doped cavities may have larger than standard Nb cavities

## Slide 10: Q-factor vs mfp
Adding together all the contributions, it is possible to predict the Q-factor as function of mean free path for different amount of trapped flux

## Slide 11: Q-factor vs mfp
Adding together all the contributions, it is possible to predict the Q-factor as function of mean free path for different amount of trapped flux

## Slide 12: Q-factor vs mfp
Adding together all the contributions, it is possible to predict the Q-factor as function of mean free path for different amount of trapped flux

## Slide 13: Q-factor vs mfp
Adding together all the contributions, it is possible to predict the Q-factor as function of mean free path for different amount of trapped flux

## Slide 14: Q-factor vs Trapped Flux for different surface treatments
12
15

## Slide 15: Conclusions
N-doped cavities are closed to both minimum of BCS and maximum of sensitivity
Light N-doping allows lower sensitivity and still low BCS
The 2/6 N-doping recipe gives the highest Q-factor at 2 K and 16 hMV/m as long as the trapped field is less than 10 mG
Further optimization still possible towards even lighter N-doping

## Slide 16: Thank you for your attention