## Slide 1: RF dissipation due to nonlinear dynamics of Josephson vortices in polycrystalline TFSRF structures
Ahmad Sheikhzada and Alex Gurevich
Physics Department and Center for Accelerator Sciences
Old Dominion University
Supported by U.S. Department of Energy under grant No. DE-SC0010081
Sheikhzada, A. and Gurevich, A. Sci. Rep. 5, 17821 (2015)
A. Sheikhzada and A. Gurevich, Physica C 506, 59-68 (2014)
7th International Workshop on Thin Films and New Ideas for Pushing the Limits of RF Superconductivity

## Slide 2: Outline
Grain boundaries are current blocking planar defects which can limit the SRF performance of promising polycrystalline materials Nb3Sn, NbN and pnictides.
Polycrystalline thin film coatings
Reduced field onset of dissipation due to penetration of Josephson vortices under strong rf fields.
Numerical simulation of nonlinear dynamics of Josephson vortices driven by strong rf currents
Rf power as a function of field amplitude
Cherenkov instability of Josephson vortices
Contribution to the high field Q-slope
S. Posen & M. Liepe, TUIOC03 (2014)
SEM of Nb3Sn surface

## Slide 3: Grain Boundaries as Josephson Junction
2D planar defects between two crystalline grains.
  Reduce current density,
  Facilitate flux penetration,
  Interface GB resistance
Bulk depairing current density at which the cooper pair breaks.
Ginzburg-Landau parameter
decays with misorientation angle.
GB can be modeled as long Josephson junction.
Weakly coupled GBs
Strongly coupled GBs

## Slide 4: Josephson junction
Two Bulk superconducting electrodes separated by a nonsuperconducting layer.
Cooper pairs may tunnel through barrier layer giving rise to a supercurrent .
Weak superconducting region, SIS, SNS,…
Current and voltage across JJ depend on phase difference between electrodes
DC effect ()
AC effect ()
V

## Slide 5: Long Junction()
&
Solution is kink (Josephson vortex) forming a long current loop along JJ moving with velocity and subjected to Lorentz contraction.
Josephson magnetic penetration depth .
Low junction .
(Swihart velocity of small EM waves)
As increases the vortex Shrinks at and Expands at
Sine-Gordon Eq.

## Slide 6: S-G, DC dynamics

## Slide 7: S-G, AC dynamics

## Slide 8: Vortex penetration
AC field application:
DC field application:

## Slide 9: Power Dissipation
Quadratic function of field amplitude, .
Step-like feature associated to one additional vortex penetration
Power changes with square root of frequency, .

## Slide 10: Surface Resistance
JJ junction model by Halbritter (2006):
Simulations show that is not linear in and .
1
3

## Slide 11: Strongly coupled GBs
For large currents the width of Josephson vortex shrinks and .
In superconductors with large G-L parameter , .
GBs for Nb3Sn
S-G is no longer valid and relation between field and phase in general becomes nonlocal.
New Abrikosov-Josephson (A-J) core length.
logarithmic
exponential

## Slide 12: Nonlocal electrodynamics of strongly coupled GBs
Extreme nonlocality (, ):
This describes the important field range
,
(, for Nb3Sn)
  Large damping
  A-J vortex like J-V expands at large damping and shrinks at small ones.
J
l
A-J
Gurevich, Physica C 243, 191(1995)
A
Normal core
No core
J core

## Slide 13: Experimental observations of AJ vortices
Transport measurements on grain boundaries, thin film junctions and layered superconductors
STM imaging of AJ vortices in monolayer step junctions

## Slide 14: Cherenkov radiation
A charged particle moves with velocity greater than the phase velocity of light in a medium leaves behind electromagnetic radiation.
Electron passes through water in an underwater nuclear reactor emits Cherenkov radiation.
wikipedia.org/wiki/Cherenkov_radiation

## Slide 15: Cherenkov radiation by Vortices
Sine-Gordon equation is Lorentz invariant
Nonlocal equation is not Lorentz invariant.
A vortex moving with a constant velocity produces Cherenkov radiation.
Radiation occurs for
where decreases with .
For small perturbations in phase
at ,

## Slide 16: Instability of underdamped J vortex
Trailing tale of Cherenkov radiation with the amplitude increasing with
Instability occurs as a junction critical nucleus with appears behind a moving vortex
Cascade of v-av pairs
Formation of an expanding phase pile, initial phase difference is preserved
Vortices at the edges move close to Swihart velocity or even higher

## Slide 17: Instability in various geometries
bulk junction, ,
, and
nonlocal limit of a bulk junction with
at .
thin film edge junction taken at
, and .
thin film overlap junction , and .
We have observed the vortex fragmentation instability for different JJ geometries.

## Slide 18: I-V characteristics
Radiation friction
Ohmic
friction
Small currents→ Ohmic friction force
Large currents→ Cherenkov radiation friction force
Instability at currents well below
Similar behavior in different geometries

## Slide 19: Effect of Finite Thickness of SRF Coating
Thin film slab
  Small screening over the thickness
  Cherenkov radiation + effect of the edges
  When current exceeds , vortices can penetrate and start moving under the bias current .
  Vortices can also be produced by point defects that locally reduces .

## Slide 20: Dynamics
Overdamped
  Penetration of single vortices
  No radiation
  Vortex expands as current increases.
  At large currents the junction turns to a small contact in which phase slip occur.

## Slide 21: DC dynamics
-point defect

## Slide 22: Ac field
Vortex penetration and radiation
dissipation

## Slide 23: conclusions
Grain boundaries are current blocking planar defects which can limit the SRF performance of promising polycrystalline materials Nb3Sn, NbN and pnictides.
New instability of JV resulting from Cherenkov radiation ultimately drives the entire GB into resistive state.
Instability happens at currents well below and is most pronounced in thin films at low temperatures.
Surface resistance is a nonlinear function of field amplitude and current due to penetration and annihilation of vortices.
Contribution to high field Q-slope.

## Slide 24: Thank you!

## Slide 25: Numerical estimation
Nb3Sn ,

## Slide 26: S-G, low damping
Medium damping
annihilation
Ohmic dissipation is small
Vortices gain inertia
Low damping
Collision become elastic in such a way that vortices don’t annihilate and simply go through
No vortex exit

## Slide 27: Surface Resistance
How a vortex dissipates?
When a vortex moves it induces electric field which couples to normal current and results in dissipation of energy.
Dissipation due to vortex dynamics in GBs contribute to residual resistivity .
Power dissipation in SRF materials and cavities