## Slide 1: Advances in Materials Characterization for SRF Thin-Films Research and Development
Jay Tuggle*
Grigory Eremeev, Ari Palczewski, Charles Reece, Uttar Pudasaini, Michael Kelley
*Virginia Polytechnic Institute and State University

## Slide 2: Secondary Ion Mass Spectrometry (SIMS)
What is SIMS
Ion bombardment
Secondary ions can be extracted and detected

## Slide 3: Secondary Ion Mass Spectrometry (SIMS)
Dynamic Magnetic Sector (Cameca 7fGeo)

## Slide 4: SIMS-So what’s the hard stuff
  Quantification is difficult
    Matrix effects
Problem Elements (Atmospherics)
Time
  Good Vacuum
  Tuning
Preferential sputtering
  Depth resolution
  BCP vs NP
Chart: Nitrogen Implant

## Slide 5: SIMS-So what’s the hard stuff
Chart: Nitrogen Concentration
Chart: Nitrogen Concentration
  Quantification is difficult
    Matrix effects
Problem Elements (Atmospherics)
Time
  Good Vacuum
  Tuning
Preferential sputtering
  Depth resolution
  BCP vs NP

## Slide 6: SIMS-Nitrogen Doping
Depth Profiles of nitrogen under different N-Doping conditions

## Slide 7: SIMS-Nb3Sn
Chart: B1-9 Depth Profile
  Depth profiling Cl after deposition
  MCs+ technique

## Slide 8: EBSD
What’s it good for?
  Phase ID, size and shape of grains, orientation information
  Preferred orientation
What’s the hard part?
  Time
  Insulating materials
  Any kind of sample drift
  Sample Prep
    10nm-20nm information depth
    Material dependent

## Slide 9: EBSD-Nb3Sn
Not just qualitative, but quantitative

## Slide 10: EBSD-Nb3Sn
Not just qualitative, but quantitative

## Slide 11
FIB-Nitrogen Doping
Platinum
Nitrides
Niobium
3.2µm
Cross section of N-Doped sample

## Slide 12
XPS-Nb3Sn Depth Profile
Chart: Conc. Vs Sputter Time
-Sputter Argon 5kv 3mmx3mm
200um 50W15kv Analysis Spot

## Slide 13
Acknowledgements
Co-Authored by Jefferson Science Associates, LLC under U.S. DOE Contract No. DE-AC05-06OR23177
We are grateful for support from the Oﬃce of High Energy Physics, U.S. Department of Energy under grant DE-SC0014475 to the College of William & Mary.
Jay Tuggle*
Grigory Eremeev, Ari Palczewski, Charles Reece, Uttar Pudasaini, Michael Kelley
*Virginia Polytechnic Institute and State University
Questions/Comments