## Slide 1
Magnetron sputtering:
New developments of a mature film deposition technique
André Anders
Senior Scientist, Lawrence Berkeley National Laboratory
Berkeley, California
aanders@lbl.gov
Acknowledgments:
This presentation includes results of several members of and visitors to the Plasma Applications Group, including Yuchen Yang, Xue Shoe, Matjaz Panjan, Joakim Andersson, and others. Work at LBNL is supported by the U.S. Department of Energy under Contract No. DE-AC02-05CH11231.
7th International Workshop on Thin Films and New Ideas for Pushing the Limits of RF Superconductivity
July 27-29, 2016
Thomas Jefferson National Accelerator Facility, Newport News, VA

## Slide 2: The Sputtering Process
This image, and the following, are from D. Depla, et al. (Ed.), Reactive Magnetron Sputtering, Springer, 2008
light ion
heavy ion

## Slide 3: Sputtering Yield
Example: Ar+  Cu
in the relevant ion region between 100 and 1000 eV, yield ~ (ion energy)1/2
Maximum at about 10 keV

## Slide 4: Energy of Sputtered Atoms: Thompson Distribution: log scale
5 keV Ar+  Cu

## Slide 5
Motion of electrons in a magnetron’s E x B field
−
+
–
Slide design by Matjaz Panjan.

## Slide 6
A. Anders, Surf. Coat. Technol. 205 (2011) S1.

## Slide 7: Magnetrons
examples are from Gencoa.com
planar, round
dual, planar, rectangular
dual, cylindrical, rotating

## Slide 8: Structure Zone Diagram for Sputtered Films
Thornton, J. Vac. Sci. Technol. 11 (1974) 666

## Slide 9: A Generalized Structure Zone Diagram including the Effects of Plasma Assistance to Film Growth
A. Anders, Thin Solid Films 518 (2010) 4087
derived from Thornton’s diagram, 1974
E* = normalized kinetic energy
t* = normalized film thickness
T* = normalized temperature and potential energy

## Slide 10: Unbalanced Magnetron: A first step to using the plasma of the magnetron to assist film growth
Unbalanced magnetic field allows electrons and ions to escape from target region, providing a means of ion assistance to film growth
ne ~ 1012 cm-3, for up to a distance of 10 cm.
B. Windows and N.Savvides, J. Vac. Sci. Technol. A 4, 453 (1986)
6 cm

## Slide 11
1990s: i-PVD
Magnetron Discharge with Auxiliary Ionization
ICP
S. M. Rossnagel and J. Hopwood, Appl. Phys. Lett. 63 (1993) 3285-3287
Ionized Physical Vapor Deposition; Vol., ed. by J. A. Hopwood (Academic Press, San Diego, CA, 2000).

## Slide 12: 1977: Early Report on Self-Sputtering
N. Hosokawa, T. Tsukada, T. Misumi, J. Vac. Sci. Technol. 14 (1977) 143.
Self-sputtering = sputtering of a target by ions of the target material

## Slide 13: Turning the Magnetron into a Plasma Source
V. Kouznetsov, et al., Surf. Coat. Technol. 122, 290-293 (1999)
from the seminal (but not first) HiPIMS paper

## Slide 14: HiPIMS: ionization of the sputtered atoms
2” magnetron
Ion collector
Copper Target in Argon
J. Andersson and A. Anders, Phys. Rev. Lett. 102 (2009) 045003.
ionized copper

## Slide 15
C. Reinhard et al., Thin Solid Films 515 (2007) 3685.
HiPIMS contains mainly singly charged metal ions
Arc contains multiply charged metal ions
Conventional sputtering contains neutral metal atoms

## Slide 16: Runaway of Self-Sputtering
Look for this small change in voltage but huge effect in current!
Copper target,
2” magnetron
A. Anders, et al., J. Appl. Phys. 103 (2008) 039901

## Slide 17
N. Hosokawa et al., Proc. 8th Vac. Con., (1980) 11; A. Anders, Appl. Phys. Lett. 92 (2008) 201501
A. Anders, Surf. Coat. Technol. 205 (2011) S1.
target
substrate
atoms to substrate
ions to substrate
Sustained self-sputtering
Probability for ions to return to the target
Ionization
probability
self-sputtering yield
Self-sputtering runaway

## Slide 18: Electric Field in Magnetic Presheath Leads to High Return Probability
Plasma potential in front of a racetrack of a magnetron (Nb sputtered in Ar), measured with an emissive probe  Average ion acceleration is mostly toward to target
Plasma potential
with respect to ground, (V)
Distance r from
target center, (mm)
Distance z from
target surface, (mm)
“racetrack”
“magnetic
presheath”
J. Sanders, et al., Rev. Sci. Instrum. 82 (2011) 093505; A. Rauch et al., J. Appl. Phys. 111 (2012) 083302.

## Slide 19: Self-Sputter Yields
(for research on Pseudosparks)
A. Anders, et al., IEEE Trans. Plasma Sci. 23 (1995) 275
Ag
Cu
is a necessary but not sufficient condition for sustained self-sputtering
Note:
carbon cannot go in sustained self-sputtering

## Slide 20: Runaway can be observed for all target materials
Runway in current is observed even for targets with extremely small self-sputtering yield, which initially was unexpected.
graphite target in argon
A. Anders, et al., J. Phys D: Appl. Phys. 45 (2012) 012003.

## Slide 21: Generalized Flux Model for HiPIMS
A. Anders, et al., J. Phys D: Appl. Phys. 45 (2012) 012003.

## Slide 22: Evidence for Gas-Recycling Model for low yield targets like carbon
after runaway to high power, argon emission remains dominant:
A. Anders, et al., J. Phys D: Appl. Phys. 45 (2012) 012003.
Below runaway, at low power
above runaway, at high power
Look for C+/Ar+ intensity ratio

## Slide 23: HIPIMS of Niobium: Self-Sputtering AND Gas Recycling
HIPIMS with Nb target ,  5 cm
A. Anders, Surf. Coat. Technol. 205 (2011) S1.
in 0.25 Pa of Ar
in 0.50 Pa of Kr

## Slide 24: Localization of Ionization and Self-Organization
A. Anders, et al., J. Appl. Phys. 111 (2012) 053304
observed by several groups in the last years

## Slide 25: Self-organization and Turbulence
A. Anders, et al., J. Appl. Phys. 111 (2012) 053304
ALL of those images were taken with Nb target, 0.27 Pa Ar, 50 µs pulse, 350 A peak.
Each image is from a different pulse  similarities and differences suggest that structures
show some interaction (self-self-organization)
show strong changes, evolution, turbulence

## Slide 26: Side-on view frame image
A. Anders, et al., J. Appl. Phys. 111 (2012) 053304
plasma flare
trailing the
ionization zone
v
(10 ns snapshot)

## Slide 27: Frame and Streak Camera Combination
A. Anders, et al., J. Appl. Phys. 111 (2012) 053304.
end-on view
frame image
end-on view
streak image
velocity of ionization zones:
just under 10,000 m/s,
depends on material.

## Slide 28
Streak image sequence, 20 ms sweep time
z, (mm)
20
10
0
A. Anders, et al., J. Appl. Phys. 111 (2012) 053304
time

## Slide 29: Example of Streak Image, 20 ms sweep time
z, (mm)
20
10
0
often greater tilt early in pulse: lower current, lower plasma density, slower flare
flare originates at the ionization zone
time

## Slide 30: High Resolution Streak Image
the greater the tilt the slower the speed in z-direction
greatest visible light intensity is at about z = 8 mm
P.A. Ni, et al., Appl. Phys. Lett. 101 (2012) 224102.

## Slide 31: Spectroscopic Imaging: End-on view through Spectral Filter.  Evidence for Concentration of Ionization.
Al, 0.25 Pa Ar, 100 A, 150 ns snapshots
300-800 nm
Al I,
from 3.14 eV
Al II,
from 15.06 eV
Ar II,
from 19.22 eV
Ar I
from 13.3 eV
ionization occurs primarily in the ionization zones, little elsewhere
the higher the upper excitation level the more focussed appears the plasma
A. Andersson, et al., Appl. Phys. Lett. 103 (2013) 054104.

## Slide 32
top collector
bottom collector
electrons
Nb ions
y
x
drift
z
Niobium HiPIMS discharge
U = 390 V
Iav = 1.25 A
P = 450 W
M. Panjan, et al., Plasma Sources Sci. Technol., 23 (2014) 025007.
Ionization zones and transport of charged particles

## Slide 33: Measurements of Ion Energy Distributions
We use EQP300 by Hiden Ltd.; scan mass up to 300 amu and energies up to 1 keV (neg. and pos. ions)
Instrument transmittance function has a greater acceptance cone angle for small (especially < 10 eV) ion energies
acceptance
cone
entrance
aperture
ion energy filter
quadrupole mass spectrometer

## Slide 34
Niobium Ion Energy Distribution Function, measured azimuthally
A. Anders, et al., Appl. Phys. Lett. 103 (2013) 144103;
M. Panjan, et al., Plasma Sources Sci. Technol. 23 (2014) 025007.

## Slide 35: Examples of Ion Energy Distribution Measurements
M. Panjan, et al., Plasma Sources Sci. Technol. 23 (2014) 025007.
HiPIMS

## Slide 36: Energizing Electrons in the Sheath Versus in Presheath
Penning-Thornton paradigm: , electron heating from secondary electrons
However, electron current in the presheath is much greater and than in the sheath  energy dissipation and electron heating can be greatest in the presheath
C. Huo, et al., Plasma Sources Sci. Technol. 22 (2013) 045005.
some notable voltage drop here

## Slide 37: Localized Energizing of Drifting Electrons
A. Anders, Appl. Phys. Lett. 105 (2014) 244104.
electrons drift according to the local E and B fields
ions are not magnetized, therefore follow E-field
direction along racetrack
NOT TO SCALE
target
x
equipotential lines
with potential hump
in ionization zone
E x B drift
of electrons
B
hump
z
flare

## Slide 38
A. Anders, Appl. Phys. Lett. 105 (2014) 244104.
Light can be seen as strongly related to the potential hump structure
side-on view
end–on view

## Slide 39: Also in dcMS: Ionization Zones are Regions of Elevated Potential  Ions gain extra energy
M. Panjan, et al., Plasma Sources Sci. Technol. 23 (2014) 025007.
majority is thermal
energetic tail
(not Thompson distribution!)
dcMS

## Slide 40
A. Anders, et al., IEEE Trans. Plasma Sci. 42 (2014) 2578.
Nb in Ar
Ionization zones exist:
even DC at low current, all the way to 4 mA!
also in reactive systems
with much slower motion than HiPIMS

## Slide 41: Transitions from DC to HiPIMS
Y. Yang, et al., Appl. Phys. Lett. 106, 124102 (2015); Y. Yang, et al., Appl. Phys. Lett. 105, 254101 (2014)
Low, < 1 A
Around 16 A
High, > 6 A
Discharge current
DCMS
PMS
HiPIMS
HiPIMS
>200 A
Transition region with
quasi-stationary spokes
Transition region of
spoke mode to spoke-free mode

## Slide 42: Multi-Probe Experiment to Measure Instabilities
Fast shutter
ICCD camera
Port for gas inlet
Port for
Vacuum gauges
N
N
S
Magnetron
Power
feedthrough
Probes
To camera control
Window
with shutter
3
5
1
7
8
4
2
6
Target
Front view
Set of floating potential probes
Y. Yang, et al., Appl. Phys. Lett. 108 (2016) 034101.

## Slide 43: Detection of Breathing Mode
0.1 Pa
All 8 probes show in-phase oscillations of floating potential
0.4 Pa
Cr target, non-reactive PMS, current ~ 6 A
Y. Yang, et al., Appl. Phys. Lett. 108 (2016) 034101.

## Slide 44
Evolution of Ionization Zones
seen for DC Magnetron Discharges (3” Nb in Ar)
Y. Yang, et al., Appl. Phys. Lett. 105 (2014) 254101.
time
sweep 200 µs
examples of streak camera images, illustrating zone stability vs. change

## Slide 45: Transition Region between HiPIMS and dc
Reversal of direction!
from E x B to - E x B
at about 6 A.
Image 20 ns each
Y. Yang, et al., Appl. Phys. Lett. 105 (2014) 254101.
Au

## Slide 46: Custom Movable, Cylindrical Magnetrons for SRF 1.3 GHz Cavities
A. Anders, et al., 15th Int. Conf. on RF Superconductivity, Chicago, Il, 2011. http://accelconf.web.cern.ch/AccelConf/SRF2011/papers/tuioa06.pdf

## Slide 47
magnetron
ion trajectory
possible collision
cavity
sheath
plasma
Cylindrical Magnetron - Cavity as Anode
A. Anders, et al., 15th Int. Conf. on RF Superconductivity, Chicago, Il, 2011. http://accelconf.web.cern.ch/AccelConf/SRF2011/papers/tuioa06.pdf

## Slide 48
ion trajectory
possible collision
cavity
sheath
nearly
perpendicular
incidence!
plasma
Vbias
magnetron 1
magnetron 2
Dual Magnetron: Most effective for a Biasing Approach: Affecting Ion Energies and Trajectories
A. Anders, et al., 15th Int. Conf. on RF Superconductivity, Chicago, Il, 2011. http://accelconf.web.cern.ch/AccelConf/SRF2011/papers/tuioa06.pdf

## Slide 49: CrN Glancing Angle Deposition
Inclination of columns is reduced at high target current densities due to high ion-to-neutral ratio
DCMS
0.1 Acm-2
0.2 Acm-2
0.6 Acm-2
0.9 Acm-2
1.7 Acm-2
G. Greczynski, et al., Thin Solid Films 519 (2011) 6354.
biased substrate
E
ion
neutral

## Slide 50: HIPIMS Coatings Technology for SRF Cavities
dual cylindrical magnetron in at relatively low power sputtering mode
Dominated by argon emission
dual cylindrical magnetron in high power mode (above runaway threshold)
Dominated by niobium emission
Relatively straight forward to include NbN and Nb/NbN multilayers
One could use two different materials with two asymmetrically operating magnetrons to produce Nb3Sn, NbTi alloys, Mg2B, and multilayer structures

## Slide 51: Summary
For Nb and other targets: self-sputtering AND gas recycling
Magnetron Sputtering since 1970s
Dual HiPIMS for SRF
Ionization in “spokes”, transport in flares
Kinetic and potential energy affects microstructure
Ionization in HiPIMS affect microstructure