## Slide 1: Pulsed Energetic Condensation of Nb Thin Film Cavities at JLab
Matthew Burton
The College of William & Mary
Department of Physics

## Slide 2: Acknowledgements
Research Group:
  Melissa Beebe (W&M), Ari Palczewski (JLab), Larry Phillips (JLab), Charlie Reece (JLab) and Ale Lukaszew (W&M)
The College of William & Mary
Thomas Jefferson National Accelerator Facility (JLab)
  SRF Institute
Olga Trofimova and the Applied Research Center (ARC) at Jefferson Lab

## Slide 3: Outline
Background
  Energetic Condensation
    High-Power Impulse Magnetron Sputtering (HiPIMS)
  JLab Deposition System
Current Work with HiPIMS: Nb Thin Film Cavities
  Goals
  Small Sample Studies
  Cavity Results
Future Work

## Slide 4: Energetic Condensation
Energetic condensation has been shown to yield films with improved:
  Microstructure
  Surface morphology
  Superconducting properties
  New frontier of film deposition that has not been strongly pursued within the SRF field
High Power Impulse Magnetron Sputtering (HiPIMS)
  Method which utilizes extremely high peak power densities on sputtering targets
  Power densities too high for continuous operation, but can be pulsed
  Yields a plasma with a large fraction of the sputtered metal being ionized (up to 90%)
    Compared to DCMS with max ion percentage of ~5%
Helmersson et al., Ionized Physical Vapor Deposition (IPVD): A review of Technology and Applications

## Slide 5: HiPIMS at JLab
Developed a vacuum system specifically designed for cavity depositions
  Can isolate cavity from system under vacuum while cleaning sputtering target
  Can deposit small samples separate from cavity depositions in order to do measurements
  Can remove cavity from system under vacuum and test without ever exposing to air (oxidizing)
Built a custom HiPIMS pulsing system with corresponding power supply
  Gives complete control over process
System currently being recommissioned after design upgrade

## Slide 6: Current Work
Goals:
  Create Nb thin film cavities using HiPIMS technique
  Exhibit cavity performance with high quality factor (Q)
  Show cavity performance with no or suppressed Q-slope
Small Sample Studies:
  Perform measurements not possible on cavities (due to geometrical constraints)
  Perform correlation studies between deposition parameters and film properties
Cavity Studies:
  Perform RF measurements on Cavities deposited using HiPIMS
  Correlate small sample film properties with cavity performance as feedback

## Slide 7: Small Sample Studies
Samples grown on Cu substrates
  Mechanically and Electrically Polished
X-Ray Diffraction:
  Probes microstructure of the film
  Gives out of plane lattice parameter (a) and grain size
Atomic Force Microscopy:
  Creates an image of the film surface
  Gives roughness (Rq) information and power spectral density (PSD)

## Slide 8: Small Sample Summary
Sample | Voltage (-V) | Peak Current (-A) | Peak Power (kW) | Temperature(°C) | Bias (-V) | Thickness (nm) | Lattice Parameter (nm) | Grain Size (nm) | RMS Roughness (nm)
A | 360 | 115 | 41.4 | 350 | 100 | ~1000 | 0.3318 | 26.748 | 20.44
B | 390 | 185 | 72.15 | 350 | 100 | ~1000 | 0.3326 | 26.6208 | 27.86
C | 411 | 232 | 95.35 | 350 | 100 | ~1000 | 0.3325 | 24.1682 | NA
D | 360 | 304 | 109.44 | 350 | *90 | ~1000 | 0.3309 | 30.5636 | 19.41
E | 435 | 312 | 135.72 | 350 | 100 | ~1000 | 0.3318 | 26.6661 | 20.75
*Bias was setup using a different scheme for this sample to reproduce previously used cavity deposition bias design

## Slide 9: X-Ray Diffraction (XRD)
XRD data courtesy of Melissa Beebe

## Slide 10: XRD Results
Bulk lattice parameter for Nb is
0.3304 nm (Red Dotted Line)
See most “bulk like” lattice parameter around 110kW peak power
Films exhibit very good microstructural properties
Bulk Nb

## Slide 11: Atomic Force Microscopy (AFM)
AFM scans the surface of a sample using Van Der Waals force between a tip and the sample to create and image
Qualitatively smooth surface with well defined grain texture similar to the copper substrate
Some samples exhibit what appears to be pitting, perhaps from the substrate preparation
AFM Images Courtesy of Olga Trofimova and the ARC

## Slide 12: AFM Results
Values taken from 50x50µm scans
Roughness reaches a minimum around 110kW peak power
Overall, the roughness is very low

## Slide 13: Cavity Results
Nb Cavity Results:
  Baseline measurement was after plasma etch and HFx10
  Cavity baked at 350C for 24hrs and deposited ~1µm film at 350C
  Cavity exhibits high Q greater than or equal to the original bulk Nb cavity
  Q-Slope still present in film
  Radiation onset expected since cavity had no HPR after coating just a nitrogen blow-off after a dirty vent up
Results confirm capability of system to deposit a high RF performing Nb film
RF Measurements Performed by Ari Palczewski at JLab

## Slide 14: Cavity Issues
One main issue remaining is the quality of the base copper cavities
  We have encountered issues with proper preparation and welding of the cavity during its creation
  These issues could explain the lower than expected performance of the cavities
  Recently finished editing the Cu cavity preparation and welding procedure
  New Cu cavities in process of being created using new procedure
  See Josh Spradlin’s talk Friday morning for more detailed information

## Slide 15: Future Work
Finish recommissioning cavity deposition system & reproduce successful Nb/Nb cavity deposition results using new system design
Deposit Nb films on suitable copper cavities
Perform more small sample studies to determine the effects of other parameters (bias, pulse shape, temperature and pressure) on resulting film properties and their crossover
Deposit cavities at studied parameter areas to determine effect on RF properties of cavities
Perform reactive HiPIMS studies using nitrogen gas to study materials beyond Nb for SRF applications (such as NbN)

## Slide 16: SRF (Superconducting Radio Frequency)
Used at Particle Accelerators (JLab, CERN…etc.)
Utilizes Superconducting Resonant Cavities (Nb)
Antenna Emits at Resonant Frequency of Cavity to establish Mode and Amplify Field
Images: jlab.org
Images: wikipedia.com

## Slide 17: Issues with Bulk Nb Cavities
Expensive & difficult to make
Poor thermal conductance (cooling issues)
Complicates overall system by imposing material and design restrictions

## Slide 18: Thin Films for SRF Cavities
SRF is a Surface Phenomena with ~1µm surface penetration
Enables cavities to be made of cheaper more suitable materials
Historically, Cu has been material most used due to:
  High thermal conductance
  Relatively low cost
  Easy to manipulate

## Slide 19: Early Work
CERN first to push thin film SRF cavities
  LEP accelerator
Deposited Films with DC Magnetron Sputtering (DCMS)
  Form of low energy condensation
Cavities had high initial Q value, but suffered from a “Q-slope”
  Efficiency of cavity decreased dramatically with increasing applied power
  Limited maximum energy of accelerator
  If LEP had no Q-slope HIGS found decades earlier
S. Calatroni, Physica C 441, 95 (2006).

## Slide 20: Transition Temperature (Tc)
Superconductivity is characterized by an abrupt second order transition from a normal conducting state to a superconducting state at the “Critical or Transition” temperature, which is, mainly, material dependent.
Placeholder for future RRR Tc data
Tc data courtesy of Josh Spradlin and the SRF Institute at JLab