## Slide 1
SUPERCONDUCTING THIN FILMS FOR SRF CAVITIES
Stuart Wilde
STFC Daresbury Laboratory and Loughborough University
Dr Reza Valizadeh and Dr Oleg Malyshev
STFC Daresbury Laboratory
Dr Boris Chesca
Loughborough University

## Slide 2
Magnetron Sputtering
Used in industry to produce thin films
Has already been used successfully to coat SRF cavities

## Slide 3
High Impulse Magnetron Sputtering
Current on the black axis
Voltage on the red axis
Average current for both DC and HiPIMS is similar
Peak current for HiPIMS up to 2 orders of magnitude higher than DC
Higher plasma current at target surface increases target ion to neutral ratio
Allows for ion assisted deposition

## Slide 4
Experiment: To analyse the morphological and superconducting properties of HiPIMS films with changing temperature and / or DC substrate bias
Samples were deposited at room temperature, 500 °C, 700 °C and 800 °C
Films deposited with either a grounded substrate or substrate biased to -20, -50, -80, -100 and -120 V DC at each temperature
Films then analysed using XRD, SEM, EBSD, and DC SQUID magnetometry (support for XRD and DC SQUID provided by G. B. G. Stenning at STFC ISIS Laboratory)

## Slide 5
HiPIMS niobium on copper
Niobium thin films were deposited on polycrystalline Cu
Constant HiPIMS settings
Pulse width of 100 μs
Repetition rate of 200 Hz
Average current of 600 mA
Peak current of 40 A
Kr sputter gas constant at 500 mTorr

## Slide 6
Room temp
500 °C
XRD of all films grown at 500 °C and below have Nb (110) preferred grain orientation

## Slide 7
700 °C
800 °C
Nb (200) begins to grow at 700 °C
Largest relative Nb (200) peak sizes occur at 0 V bias
Nb (110) and (200) varies when bias is applied

## Slide 8
Lattice Constant
Lattice Constant was calculated to be longest for RT and 500 °C
Shorter lattice constants at highest temperatures

## Slide 9
Room temperature
500 °C
DC SQUID Magnetometry

## Slide 10
700 °C
800 °C

## Slide 11
700 °C shows FFP at -80 V. This was also the highest field recorded for any film at 580 Oe
DC SQUID and penetration field

## Slide 12
Summary showing peak at 80 / 100 V DC Bias

## Slide 13
Ideal Meissner state
Measured SQUID curve
Alternative look at the SQUID curves.
SQUID curves have been compared to their ideal case with no magnetic penetration
Each measured curve was fitted with a 2nd order polynomial fit
Fraction of the non-Meissner sample volume was calculated
H Field
Moment

## Slide 15
800 °C -120 V Bias
700 °C and 800 °C at high bias show textured film surface
Possibly pitting of substrate or film delamination
Images of all films required to make definite conclusions
SEM

## Slide 16
700 °C -100 Bias
800 °C – 80 V Bias
Grains appear bigger at 800 °C
Thickness of both films is approx. 1.3 micron
Only 2 films so far imaged in cross section
No delamination seen in either image

## Slide 17
EBSD
Sample deposited at 800 °C with -80 bias
Some single grains are as thick as the film
Largest grains approx. 4 μm
Majority of the grains were in the (110) orientation

## Slide 18
700 °C and -100 V Bias
Grain orientation dictated by the orientation of the underlying copper substrate
EBSD Performed by Dr K. Dawson
The University of Liverpool

## Slide 19
Surface resistance measurements
Sample deposited at 500°C with -100 V Bias.
Sample tested at 3.9 GHz
Thickness of film approx. 4 micron
Surface resistance measurements performed at Cornell University by J. T. Maniscalco

## Slide 20
Sample deposited at 800 °C without bias showed very poor RF performance.
Rs was in μΩ region
Superconductivity extinguished at 30 - 40 mT
Unsure of the reason for such poor performance
Further analysis needed!

## Slide 21
Coherence length can be calculated by applying a magnetic field then measuring Tc
is the gradient of Tc plotted against field strength for different applied fields
Mean free path can then be calculated from the coherence length of the sample and that of pure niobium
Future Analysis
I+
I-
V+
V-
B Field
Use four point probe in uniform magnetic field to measure mean free path of a superconductor

## Slide 22
RRR in magnetic field
Mean free path calculated for only 2 samples so far
800 °C no bias = 350 Å
800 °C -20 V Bias = 280 Å
RRR= 39
RRR= 43
Resistance (Ω)
More data points required to improve accuracy

## Slide 23: Acknowledgments
Reza Valizadeh
Oleg Malyshev
Gavin Stenning
Shrikant Pattalwar
Ninad Pattalwar
Adrian Hannah
Boris Chesca
Karl Dawson