## Slide 1: CVD / PECVD Superconductive materials for RF cavities
Paolo Pizzol
University of Liverpool / STFC – Daresbury Lab

## Slide 2: Outline
Superconductivity Radio Frequencies and Niobium
Chemical vapour depositions
Experimental results and planned work

## Slide 3: Outline
Superconductivity Radio Frequencies and Niobium
Chemical vapour depositions
Experimental results and planned work

## Slide 4: Niobium - Limits
Niobium SRF cavities are the state of the art for accelerating charged particles, but:
copper has a better thermal conductivity than Nb
à easier to cool down
à cheaper
a thin film of Nb requires less material
...
à cheaper

## Slide 5: PhD Topic
Problem:
Modern accelerators have reached the maximum gradient achievable by using Nb as a bulk.
Over the limit of » 45 MV/m the superconductivity breaks down!
Aim of this study:
Developing CVD / PECVD deposition techniques to coat copper cavities with an uniform Niobium superconductive thin layer

## Slide 6: Outline
Superconductivity Radio Frequencies and Niobium
Chemical vapour depositions
Experimental results and planned work

## Slide 7: Chemical Vapor Deposition (CVD)
The chemical precursors are introduced together in the reaction chamber
Fast: micrometers thick depositions in a few hours
Challenging to control the film uniformity
Niobium chemistry requires high temperatures to work well
Precursors

## Slide 8: The chemical side
Precursors under study
Niobium Pentachloride (V):
  Chosen to obtain metallic Nb layer
  Reacts with plasma of H+ to create thin film
  Crystalline solid, vapour pressure at 150 °C to perform ALD
  Very sensitive to moisture, hydrolyzes in NbOCl4
  Requires high substrate temperature to reduce Cl contamination in the film (at least 500 °C)
Tris(diethylamido)(tert-butylimido)niobium (V)
  Chosen to obtain NbN layer
  Reacts with N2 plasma to create thin film
  Liquid, good vapour pressure at 104 °C to perform ALD
  Sensitive to heating, start decomposing at 130 °C
  Doesn’t require a high deposition temperature (250 °C) à Suitable for deposition on copper

## Slide 9: Experimental setup
Cold wall reactor.
Heater capable of T > 700 C.
2 bubbler lines for precursor delivery.
Hydrogen, Nitrogen and Ammonia Gas lines.

## Slide 10: Experimental setup
In house designed bubblers to hold the precursors.
Bubbler preparation and filling done in glovebox on site.

## Slide 11: Outline
Superconductivity Radio Frequencies and Niobium
Chemical vapour depositions
Experimental results and planned work

## Slide 12: Outline
Superconductivity Radio Frequencies and Niobium
Chemical vapour depositions
Experimental results and planned work
  Niobium
  Niobium Nitride
  Niobium Titanium Nitride

## Slide 13: Nb coated Cu disc

## Slide 14: Nb coated Cu disc

## Slide 15: Nb coated Cu disc

## Slide 16: Selected Area e- Diffraction

## Slide 17: TEM cross section of Nb film

## Slide 18: TEM study – Elemental maps

## Slide 19: Niobium XRD
Phase: Cubic
Average Grain size: 14 nm
Phase: Cubic
Average Grain size: 26 nm

## Slide 20: Nb coated Cu disc
Thicker sample (2 mm)
Superconductive
RRR of best sample of 31 – thin films fall in the 0 – 50 range.

## Slide 21: Thin film etched with nitric acid

## Slide 22: SQUID measurements

## Slide 23: Nitrides of Nb. Why?
To verify the multilayer hypotesis, we decided to explore the deposition of nitrides of Nb.

## Slide 24: Niobium Nitride
Attempted to deposit Niobium Nitride with Nitrogen plasma. Maybe successful, but machine failure destroyed the sample.
Installed Ammonia gas line to obtain NbN

## Slide 25: Niobium Nitride

## Slide 26: Niobium Nitride

## Slide 27: Niobium Nitride

## Slide 28: Niobium Nitride
Phase: Cubic
Average Grain size: 25 nm

## Slide 29: EBSD on NbN
  EBSD attempted on NbN film (100mm substrate).
  Image looks pixelated due to very small size of grains.
Film
  NbN
  NbN

## Slide 30: SAED

## Slide 31: SAED

## Slide 32: Niobium Titanium Nitride
Installed second bubbler line to deposit multiprecursor films:
  NbTi
  NbTiN
  Nb3Sn
  Nb3Ge

## Slide 33: Niobium Titanium Nitride

## Slide 34: Niobium Titanium Nitride

## Slide 35: Niobium Titanium Nitride

## Slide 36: Niobium Titanium Nitride
Phase: Cubic
Average Grain size: 21 nm

## Slide 37: Planned future work
Install plasma source to reduce deposition temperature.
SRF properties testing.
Upgrade to ALD to verify conformality and multilayering of S-I-S systems.

## Slide 38: Thank you for your time