## Slide 1: Growth of MgB2 Films on Large Area Cu Discs and RF Characterization
Wenura Withanage
Advisor – Prof. Xiaoxing Xi

## Slide 2: Outline
Superconducting MgB2
Motivation & Goal
Hybrid physical chemical vapor deposition (HPCVD) of MgB2 at Temple University
MgB2 growth on metal substrates
MgB2 growth on 2” ceramic substrates
MgB2 growth on Cu substrates by other groups
MgB2 deposition on 2” Cu discs
Results
Summary
References

## Slide 3: Superconducting MgB2
Hexagonal structure
Xi et al, Physica C 456, 22 (2007)
1 μm
Zeng et.al., Nature Materials, Vol.1, 2002
Discovered in 2001
High transition temperature(Tc) ~39 K
Has a hexagonal structure
http://www.ccas-web.org/superconductivity/#image1

## Slide 4: Motivation & Goals
MgB2 is one of the most promising superconducting material for SRF applications
- high Tc (39 K) - low residual resistance
- non weak link behavior between the grain boundaries
MgB2 coated Cu cavities will have high thermal conductivity
Less expensive alternate for commonly used Nb bulk cavities
Developing a recipe to grow MgB2 on large area Cu discs
RF characterization of the MgB2 coated Cu discs
Coating MgB2 on the inner walls of a 3 GHz Cu cavity
Motivations
Goals

## Slide 5: HPCVD of MgB2 at Temple University
get rid of oxygen
prevent oxidation
make high Mg
pressure possible
pure source of B
B supply (B2H6 flow rate) controls growth rate
Pure source of Mg
high enough T
for epitaxy ~ 730 C
Substrate
H2 (~40 Torr)
B2H6 (~ 2 - 40 sccm)
Mg
Sample
holder sits
on the
resistive
heater
Pressure – Temperature phase diagram for Mg – B system
Liu Z K, Schlom D G, Li Q and Xi X X 2001
Thermodynamics of the Mg–B system: implications
for the deposition of MgB2 thin films Appl. Phys. Lett.

## Slide 6: MgB2 growth on Metal substrates using HPCVD
MgB2 was grown on metal substrates
Deposition temperature ~ 700 C
300 nm MgB2 were grown
Tc ~ 39 K
Chenggang Zhuang · Teng Tan · Alex Krick ·
Qingyu Lei ·Ke Chen · X.X. Xi
J Supercond Nov Magn (2013) 26:1563–1568
Mg readily reacts with Cu at high temperature
MgCu2 and Mg2Cu

## Slide 7: MgB2 Film growth on 2” ceramic substrates
HPCVD setup was scaled up to accommodate 2” substrates
2” sapphire discs were coated successfully
Tc ~ 39 K
Teng Tan, Chenggang Zhuang, Alex Krick, Ke Chen, and X. X. Xi
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 23, NO. 3, JUNE 2013
7

## Slide 8: MgB2 growth on Cu substrates by other groups
M. Ranot and W. N. Kang, Current Applied Physics 12 (2), 353 (2012).
(a)
(b)
(c)
(d)
MgB2 coated Cu tapes by using HPCVD

## Slide 9: MgB2 deposition on 2” Cu discs
~450 C
H2(10 Torr)
B2H6(10 ~ 20 sccm)
2” copper substrate
Molybdenum susceptor
Mg
Resistive
heating
Mg vapor reacts and forms alloy with Cu starting around 450 C at 10 Torr ( Copper surface color changes to silverfish)
Mg vapor pressure is low at low temperatures
Coating whole 2” area uniformly challenging
Challenges in growing MgB2 on Cu
Scaling Up for 2” Cu discs and Reducing the growth Temperature
HPCVD system is modified to accommodate thick 2” Cu disc
Deposition conditions were optimized for Cu substrates

## Slide 10: MgB2 deposition on cu discs
1. MgB2 coatings on Nb buffered Cu discs
100 nm of Nb layer was sputtered on the Cu discs
MgB2 depositions were carried on Nb buffered Cu discs
XRD data showed the MgCu2 alloy presence in the samples
SEM images showed the hexagonal structure
Samples showed transition temperature(Tc) close to 38 K
Polished Cu
Unpolished Cu
10

## Slide 11
2. MgB2 Growth on bare Cu discs
Mg-Cu alloy formation through the Nb layer
MgCu2 alloy promotes the growth of MgB2 phase at low temperature( ~ 400 C)1, 2
MgB2 was grown on Cu directly
Transition temperature (Tc) ~ 38 K
Polished Cu
Unpolished Cu
11

## Slide 12: results
Copper cavity
Loop antenna
Sapphire puck
Sample
Q vs T graphs gives us information about Tc and indicate the quality in a RF field compared to a reference sample
MgB2 films on copper show Tc around 38 K
18.4 GHz

## Slide 13: Q vs T and Rs vs T measurements carried out at jlab
MgB2 on Nb buffered Cu discs were measured
7.4 GHz
13

## Slide 14: Q vs T measurements carried out using Cryogenic RF measurement system at SLAC
Films showed Tc close to 37.5 K
Best MgB2 samples on Cu discs shows comparable Q with Nb reference samples and higher Q than copper reference sample.
Cu cavity results
Nb cavity results
11.4 GHz
14

## Slide 15: Future work
Study the cross section and film thickness
Improve the process
Field measurements
Moving to the Cu cavity

## Slide 16: Acknowledgement
My advisor and group members
Dr. Alireza Nassiri
Dr. Paul Welander
Dr. Grigory Eremeev
Dr. Anne – Marie

## Slide 17: References
M. Ranot and W. N. Kang, Current Applied Physics 12 (2), 353 (2012).
Y. Z. Wang, C. G. Zhuang, J. Y. Gao, X. D. Shan, J. M. Zhang, Z. M. Liao, H. J. Xu, D. P. Yu, and Q. R. Feng, Journal of the American Chemical Society 131 (7), 2436 (2009).
B. P. Xiao, G. V. Eremeev, M. J. Kelley, H. L. Phillips, C. E. Reece Proceedings of LINAC2012, Tel-Aviv, Israel
Jiquan Guo, Sami Tantawi, David Martin, Charles Yoneda Proceedings of 2011 Particle Accelerator Conference, New York, NY, USA
Chenggang Zhuang · Teng Tan · Alex Krick , Qingyu Lei ·Ke Chen · X.X. Xi
J Supercond Nov Magn (2013) 26:1563–1568
Teng Tan, Chenggang Zhuang, Alex Krick, Ke Chen, and X. X. Xi
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 23, NO. 3, JUNE 2013

## Slide 18
Where –
A – is a constant depends on penetration depth, coherence length, Fermi velocity and mean free path
f – Frequency k – Boltzmann constant
T – Temperature - Energy gap
RBCS =

## Slide 21
MgCu2 alloy peak
MgCu2 peak
MgCu2 alloy, MgB2 and Cu peaks overlap
XRD data of MgB2 samples on
Nb buffered Cu discs

## Slide 22
Back to Mg – B phase diagram

## Slide 23
H
Sample being tested
11.4 GHz
E
SLAC system
Back to SCLAC results