## Slide 1: Increase in vortex penetration field on bulk Nb coated with a MgB2 thin film without an insulation layer
Teng Tan--Institute of Modern Physics, CAS
M. A. Wolak, X. X. Xi--Temple University
L. Civale, T. Tajima--LANL

## Slide 2: Outlines
Motivations
Experiments
Results and Discussions
Conclusions

## Slide 3: Outlines
Motivations
Experiments
Results and Discussions
Conclusions

## Slide 4: Motivations (VP on Film/Cavity)
A SC thin film coated ellipsoid can provide such conditions.
Vortex penetration causes loss.
Use thin film/S-I-S structure to protect the SRF cavities from VP.
Prove the effectiveness of thin film: H//, only on one side.
Strong vortex dissipation
Gurevich, APL 88, 012511 (2006)
H

## Slide 5: Motivations (Film on an Ellipsoid)
An ellipsoid in H//axis has uniform magnetization.
H//surface everywhere. Mimicking the inner surface of SRF cavities.
Strongest H at equator.
H0
Heq
H
H’ =
N is the demagnetization factor

## Slide 6: Motivations (MgB2 thin films)
Higher Tc, comparing with Nb and Nb3Sn.
Hc and Hsh are close to Nb3Sn, higher than Nb.
Lower Hc1 is covered by thin film structure.
Larger l is good for thin film coated SRF cavity.
Material | Tc [K] | ρn (μΩcm) | Hc(0) [T] | Hc1(0) [T] | Hc2(0) [T] | (0) [nm] |  [meV]
Nb | 9.23 | 2 | 0.2 | 0.18 | 0.28 | 40 | 1.5
Nb3Sn | 18 | 20 | 0.54 | 0.05 | 30 | 80-100 | 3.1
MgB2 | 40 | 0.1-10 | 0.43 | 0.03 | 7 | 100~140 on metal | 1.8/7.2

## Slide 7: Theory (H// on one side)
Gurevich, APL 88, 012511 (2006)
Multilayer S-I-S
S. Posen PR applied 4, 044019 (2015)
Hsh and thin limit
Gurevich, AIP Advances 5, 017112 (2015);
Optimal dm.
J limit
Hc1 limit

## Slide 8: Theory (MgB2 on Nb)
T. Kubo MgB2/I/Nb, Bc(MgB2)=320 mT (2014 private comm.)
λ=140nm
λ=100nm

## Slide 9: Theory (MgB2 on Nb no I layer)
MgB2/Nb, Bsh(MgB2)=320 mT Bsh(Nb)=240 mT
lMgB2 = 100 nm
lMgB2 = 140 nm

## Slide 10: Outlines
Motivations
Experiments
Results and Discussions
Conclusions

## Slide 11: Experiments (Sample preparation)
1 2 3 4
Ellipsoids are machined from rods.
Calculations:
2c
2b
2a
2c = 8 mm
2a = 2b = 5 mm
Demag factor : Nc = 0.2186
Nb=Na=0.3907
Volume = = 0.01047 cm3
m/H0 = = 0.01066 emu/Oe
Heq/H0 = 1.28 when H0//c axis

## Slide 12: Experiments (Sample preparation 2)
MgB2 thin films by HPCVD
B2H6 + H2
Ellipsoid
SiC Reference Sample
Nb0
Nb200
3 successive depositions to deposit a shell,
A reference sample is put aside of the ellipsoid in the first deposition.
Sample is marked with “Nb + reference sample thickness”. Actual thickness of the shell is expected to be 1~1.5 times larger.
Samples: Nb0
Nb100
Nb200

## Slide 13: Experiments (Hvp measurement)
Measurements performed at LANL.
Hvp is first measured with m-H method.
Similar to thin film Hc1 measurement. ZFC then magnetization
Vortex penetration signified by m-H curve deviates from linear relationship.
H
VP at H0 reaches Hvp.
Hvp ~ 1700 Oe at 5 K for Nb0.
Method idea: Constant T, measure Hvp.
T
Nb200 ellipsoid
Example curves: Nb200.

## Slide 14: Experiments (Hvp measurement 2)
Sample ZFC then warm up in field.
VP at Hvp decrease to H0. Shown by Dm.
Method idea: Constant H, measure T correspond to the fixed Hvp.
Hvp = 1500 Oe at 5.21 K for Nb200
Nb200 ellipsoid
H
T
Sample curve measured on Nb200,
150 mT field applied after ZFC to 3 K.

## Slide 15: Outlines
Motivations
Experiments
Results and Discussions
Conclusions

## Slide 16: Results (Hvp-T from M-H)
Nb200 Tc 38.2 K
Nb0 Tc 9.3K

## Slide 17: Results (Hvp-T from M-T)

## Slide 18: Discussions (method comparison)
M-H has large noise at H > 1500 Oe due to magnet ramping.
M-T is a better alternative.

## Slide 19: Discussions (compare with theory)
Our results agree with the curves for Bsh(MgB2)=320 mT and different lMgB2. With thicker film closer to the limit.
2600 Oe
2.3 K
2600 Oe
2.8 K
2800 Oe
3000 Oe
Measurement
Linear Extrapolation to 0 K
lMgB2 = 100 nm
lMgB2 = 140 nm

## Slide 20: Supplementary: Field Penetration
Can we prove the shielding effect of S-I-S structure?
MgB2/Nb structure is not working: no place for the B probe.
B = ?

## Slide 21: Supplementary: Field Penetration
Can we prove the shielding effect of S-I-S structure?
MgB2/Nb structure is not working: no place for the B probe.
If we took out the SC core and only left a SC shell: MgB2/Mo
Mo100, Mo200, Mo300
B = 4pm/V

## Slide 22: m-H measured MgB2/Mo Hvp
Hvp: Mo200>Mo100≈Mo300

## Slide 23: Maximum DH
x
y
z
Field cool,
Vortex penetration,
no SC current.
Increase field,
Vortex frozen,
SC current increase until Ic
Further increase field,
Vortex enters again,
SC current remain Ic
400 Oe over 200 nm, J ~ 107 A/cm2

## Slide 24: Maximum DH
Field cool,
Vortex penetration,
no SC current.
Increase field,
Vortex frozen,
SC current increase until Ic
Further increase field,
Vortex enters again,
SC current remain Ic

## Slide 25: Outlines
Motivations
Experiments
Results and Discussions
Conclusions

## Slide 26: Conclusions
We increase the Hvp by ~600 Oe by coating it with a thin superconducting film that screens vortex penetration. Hsh(0) of MgB2 has to be > 3000 Oe.
It is technically possible to deposit a thin MgB2 film with appropriate properties for this purpose on curved bulk Nb via HPCVD. Making it possible for MgB2 covered Nb cavity.
The shielding effect of S-I-S structure is proved. Maximum DH ∝ Jd.
The actual Hvp enhancement depends on Hsh of the film, depairing J, film quality, and maybe more.

## Slide 27: Acknowledgements
Thanks for your attention
Welcome Collaboration!