## Slide 1: Review of muSR studies for SRF applications
Tobias Junginger

## Slide 2: Acknowledgement
Experimentalists: D. Bazyl, R. Dastley, M. Dehn, D. Azzoni Gravel, S. Gehdi, Z. He, R. Kiefl, P. Kolb, R. Laxdal, Y. Ma, D. Storey, E. Thoeng, W. Wasserman, L. Yang, Z. Yao, H. Zhang (TRIUMF)
Support from Triumf Centre for Molecular & Materials Science: D. Arseneau, B. Hitti, G. Morris, D. Vyas (TRIUMF)
Support at PSI: A. Suter (PSI)
Sample Providers: D. Hall, M. Liepe, S. Posen (Cornell), A. Valente-Felenciano (JLAB), T. Tan, W. Withanage, M. Wolak, X. Xi (Temple University), G. Terenziani, S. Calatroni (CERN)
Affiliations as of time of collaboration

## Slide 3: μSR Facilities Around the World

## Slide 4: μSR Facilities Around the World
Summary:
muSR is a technique that allows to measure localized magnetic fields. Using this technique we show:
1. A layer of higher Tc material on niobium can push the field of first flux entry from a field consistent with Hc1 to a field consistent with Hsh.
2. For multilayer systems without insulator there is a wide range proximity effect to be considered
3. There is strong evidence for magnetic impurities on the surface of Nb/Cu samples

## Slide 5: Outline
Introduction to muSR
Using muSR as a local magnetometer (TRIUMF)
  Inducing superheating in niobium by thin film coating
Low Energy muSR (PSI)
  Proximity effects in NbTiN/Nb and NbTiN/AlN/Nb samples
  Magnetic Impurities in Nb/Cu films
Summary
Outlook
  BetaNMR

## Slide 6: Muon production and decay
Muons are 100% spin polarized with kinetic energy of 4.1MeV
Muons are deposited ~100micron deep in a sample (bulk probe) – spin precesses with frequency dependent on local magnetic field
Muon decays in 1/2=2.2µsec - emits a positron preferentially along the µ+ spin direction

## Slide 7: Muon Spin Rotation – muSR
Muons are deposited one at a time in a sample
Muon decays emitting a positron preferentially aligned with the muon spin
Right and left detectors record positron correlated with time of arrival
The time evolution of the asymmetry in the two signals gives a measure of the local field in the sample
Left detector
Right detector

## Slide 8: Magnetic Volume Fraction
Non-magnetic with
magnetic impurities
Uniformly weakly magnetic
Static distribution of random fields

## Slide 9: Using muSR as local magnetometer
Meissner state
Intermediate state
Vortex state
Normal state
A sample is cooled in zero field - asymmetry measurements are taken as a function of applied magnetic field
The relative asymmetry at t=0 gives a measure of the volume fraction sampled by the muons that does not contain magnetic field
A variety of samples and sample geometries have been characterized in this way

## Slide 10: The field of first entry and the role of pinning in different geometries
Transverse coin samples are sensitive to pinning - delays flux break in to the centre
Parallel coin geometry is insensitive to pinning
Ellipsoid samples are less sensitive
All three geometries are useful to characterize the material

## Slide 11: The field of first entry and the role of pinning in different geometries
Stronger pinning
800C baked samples – pinning is clearly seen in different Hentry between transverse, parallel coin and ellipsoid geometry
Weak pinning
1400C heat treatment for three geometries
virtually eliminates pinning from the Nb
Hentry is equal for all geometries
Effect of pinning
Our baseline substrate for thin film tests is 1400°C annealed niobium
The parallel field configuration is used to determine the field of first entry
Measurements in transverse geometry measure the pinning strength

## Slide 12: Testing coated samples with muSR as a local magnetometer
Nb
Parallel field configuration. Field will first break in at the corners at 0.82 Hentry and move to the center at 0.91 Hentry. Only the field in the center is probed
Above Tc of niobium we measure the field of first entry of the coating only, below Tc of niobium we measure the higher Hc1 or Hsh
B
20mm
Muons
Muons are implanted
100 μm deep in the bulk
Coatings are between 50nm and 3.5µm

## Slide 13: Nb3Sn on Nb Ellipsoid results
Material | Hnucleate (0) [mT] | Tc [K]
Niobium | 227 | 9.36
Nb3Sn | 37.1 | 17.3
Below 9.25K we seem to measure Hsh of niobium, above 9.25K Hc1 of Nb3Sn.
 If the film induces superheating in niobium this should be independent on thickness

## Slide 14: Testing coated samples (MgB2)
Chart: Magnetic Field [mT]
| 0 | 114.28370129922507 | 142.9944436723994 | 148.73659214703426 | 154.47874062166915 | 160.22088909630401 | 163.09196333362144 | 165.96303757093889 | 168.8341118082563 | 171.70518604557373 | 177.44733452020859 | 180.31840875752604 | 183.18948299484347 | 188.9316314694783
Niobium 1400°C annealed | 1 | 0.99547 | 0.98702 | 0.98489 | 0.97444 | 0.97818 | 0.97449 | 0.98284 | 0.97947 | 0.9656 | 0.51367 | 0 | 0 | 0
MgB2 (150 nm) on Nb | 1 | 0.99744 | 1.0141 | 1.0236 | 0.99134 | 0.97169 | 0.92001 | 0.76376 | 0.4968 | 0.19399 | 0 | 0
MgB2 (50 nm) on Nb | 1 | 0.97941 | 0.98469 | 0.95067 | 1.0026 | 0.97938 | 0.95713 | 0.68238 | 0.63673 | 0.31235 | 0.15491 | 0.047274 | 0 | 0
MgB2 (300nm) on Nb | 1 | 1.0008 | 1.01 | 1.0119 | 0.96228 | 0.57785 | 0.27764 | 0.093951 | 0 | 0

## Slide 15: Testing coated samples (MgB2)
Chart: Magnetic Field [mT]
| 0 | 114.28370129922507 | 142.9944436723994 | 148.73659214703426 | 154.47874062166915 | 160.22088909630401 | 163.09196333362144 | 165.96303757093889 | 168.8341118082563 | 171.70518604557373 | 177.44733452020859 | 180.31840875752604 | 183.18948299484347 | 188.9316314694783
Niobium 1400°C annealed | 1 | 0.99547 | 0.98702 | 0.98489 | 0.97444 | 0.97818 | 0.97449 | 0.98284 | 0.97947 | 0.9656 | 0.51367 | 0 | 0 | 0
MgB2 (150 nm) on Nb | 1 | 0.99744 | 1.0141 | 1.0236 | 0.99134 | 0.97169 | 0.92001 | 0.76376 | 0.4968 | 0.19399 | 0 | 0
MgB2 (50 nm) on Nb | 1 | 0.97941 | 0.98469 | 0.95067 | 1.0026 | 0.97938 | 0.95713 | 0.68238 | 0.63673 | 0.31235 | 0.15491 | 0.047274 | 0 | 0
MgB2 (300nm) on Nb | 1 | 1.0008 | 1.01 | 1.0119 | 0.96228 | 0.57785 | 0.27764 | 0.093951 | 0 | 0
Chart: MgB2 (300nm) on Nb
| 6.7319211102994894E-2 | 0.32459196493791082 | 0.77249846603360139
 | 212 | 148 | 50
Again temperature dependence as expected for niobium

## Slide 16: Testing coated samples (Nb3Sn and MgB2)
Chart: Film Thickness [nm]
| 2000 | 2000 | 1000 | 3500 | 2000
Nb3Sn | 239 | 243 | 255 | 245 | 223
MgB2 | 240 | 223 | 229
Factor of 70
Theoretical
Hsh of Nb

## Slide 17: Testing coated samples (Nb3Sn and MgB2)
Chart: Film Thickness [nm]
| 2000 | 2000 | 1000 | 3500 | 2000
Nb3Sn | 239 | 243 | 255 | 245 | 223
MgB2 | 240 | 223 | 229
Factor of 70
Theoretical
Hsh of Nb
Hsh=237(11)

## Slide 18: Testing coated samples (Nb3Sn and MgB2)
Chart: Film Thickness [nm]
| 2000 | 2000 | 1000 | 3500 | 2000
Nb3Sn | 239 | 243 | 255 | 245 | 223
MgB2 | 240 | 223 | 229
Factor of 70
Theoretical
Hsh of Nb
No clear trend for field of first entry on material or thickness.
Conclusion: Superheating is induced in niobium
Hsh=237(11)

## Slide 19: Outline
Introduction to muSR
Using muSR as a local magnetometer (TRIUMF)
  Inducing superheating in niobium by thin film coating
Low Energy muSR (PSI)
  Proximity effects in NbTiN/Nb and NbTiN/AlN/Nb samples
  Magnetic Impurities in Nb/Cu films
Summary
Outlook
  BetaNMR

## Slide 20: Low energy muons
Low energy muons can be stopped in a variable depth between 0 and ~100nm
Ideal for testing layered structures
Parallel fields limited to 25mT
Has been applied to test two samples
  NbTiN(80nm) on Nb
  NbTiN(80nm)/AlN(20nm) on Nb

## Slide 21: Field parallel to sample surface – Meissner Screening NbTiN (80nm) on Nb
λ=223(7) nm
Magnetic field decays with a single exponential
223(7) nm is short for NbTiN
Proximity effect?
2.2K
V. Cherkez et al.- PHYSICAL REVIEW X 4, 011033 (2014)

## Slide 22: Field parallel to sample surface – Meissner Screening NbTiN (80nm) on Nb
λ=223(7) nm
Naive treatment
London theory, no proximity effect
Experiment
Magnetic field decays with a single exponential
223(7) nm is short for NbTiN
Proximity effect?
2.2K
T. Kubo arXiv:1410.1248

## Slide 23: Field parallel to sample surface – Meissner Screening NbTiN (80nm) on Nb
Fit
cosh(x/λ0)/cosh(d/(2 λ0))
λ0=204(18); d=135(11)
Either the NbTiN layer is significantly thicker than 80 nm or long range proximity effect

## Slide 24: Field parallel to sample surface – Meissner Screening NbTiN (80nm) on Nb
11 K
λ0=204(18); d=135(11)
8 K
λ0=190(15); d=157(13)
At 8 K a vortex must have entered the niobium

## Slide 25: Comparison to SIS Multilayer
Nb-NbTiN
Nb-AlN-NbTiN
8 K
λ0=190(15); d=157(13)
8 K
λ0=380(100); d=98(13)
For multilayer systems without insulator there is a wide range proximity effect to be considered.

## Slide 26: Outline
Introduction to muSR
Using muSR as a local magnetometer (TRIUMF)
  Inducing superheating in niobium by thin film coating
Low Energy muSR (PSI)
  Proximity effects in NbTiN/Nb and NbTiN/AlN/Nb samples
  Magnetic Impurities in Nb/Cu films
Summary
Outlook
  BetaNMR

## Slide 27: Fluctuating Random Fields
Slow Fluctuations
Main effect is relaxation of the ⅓ tail at long times, because 1/3 of the muons see a field in spin direction and do not process
Fast Fluctuations
No recovery. For faster fluctuations slower depolarization (motional narrowing)
Polarization function for different fluctuation rates. The “0” function corresponds to a Gaussian distribution of random fields.

## Slide 28: Evidence for Magnetic Impurities in Nb on Cu samples
HIPIMS
dcMS
HIPIMS shows strong fluctuations
  Muon diffusion?
  Magnetic Impurities?
Magnetic Impurities supported by zero bias peaks observed with point contact tunneling (PCT) from ANL (T. Proslier)
Zero bias peaks
muSR
PCT
PCT

## Slide 29: Additional tests with a nitrogen overlayer
We grew a nitrogen overlayer on the sample
Stop the muon in the nitrogen but close to the niobum surface
In nitrogen the muon is known to be static
Deviations from the static Kubo-Tuyabe function will give evidence for magnetic impurities

## Slide 30: Measurements with N2-overlayer
There is no muon diffusion in the N2-overlayer
If there are no magnetic impurities in the Nb a staticGssKT function would fit the data
Static Kubo-Toyube*exp(-λ/t)β
Static muon – Gaussian Field Distribution
No magnetic impurities
Systematic deviations

## Slide 31: New beta-NMR beamline at TRIUMF for SRF studies
Beta-NMR @ TRIUMF is a unique facility to characterize magnetic properties of materials at surfaces and film interfaces
Similar to muSR but uses radioactive ions like 8Li implanted in bunches not one by one
Like LEmuSR it can probe the superconductor through the London layer and depth profile thin films
New high field spectrometer is being installed to allow high field (near Hc1) parallel to sample face (to replicate rf fields)
TRIUMF will provide a unique facility in the world for diagnosing new treatments (doping), new materials (Nb3Sn) and new structures (SIS layers)
Existing low field spectrometer
New high field spectrometer

## Slide 32: Summary
muSR is a technique that allows to measure localized magnetic fields. Using this technique we show:
1. A layer of higher Tc material on niobium can push the field of first flux entry from a field consistent with Hc1 to a field consistent with Hsh.
2. For multilayer systems without insulator there is a wide range proximity effect to be considered
3. There is strong evidence for magnetic impurities on the surface of Nb/Cu samples
Questions?