## Slide 1
This work is funded by US Department of Energy and CNAM
Extreme Electrodynamic and Local Harmonic Measurement of Nb Thin Films
Bakhrom Oripov , Steven M. Anlage
Notes: Name
Fund
We built microscope

## Slide 2
Problem: Defects
500 x 200 mm pit
A high resolution near field magnetic field microscope can identify those defects and relate which defects results in the breakdown of the cavities is needed.
welds,
oxidation,
hydrogen poisoning
Cavity Temperature Map
T > Tc
Defect
Notes: Defects due to manufacturing
Have smaller Tc, Jc
Go to normal act as hotspot
Temperature Map – Heat the area
Solution? Built Microscope

## Slide 3
BRF ~ 1 Tesla (in gap)
Reference: IEEE Trans Magn. Vol . 37, No. 2 pp.613-618 2001
Slider with
write coil
Coaxial cable
Read/Write
Head
Thickness
(~1.2 mm)
Suspension
Au bond pads to reader and writer
Air bearing
surface
500 m m
Method: High Resolution Magnetic Probe Scanning

## Slide 4: Surface Current Diagram
Microwave Source
Low Pass Filter
High Pass Filter
Spectrum
Analyzer
Vf +
V3f -
M. V. Milosevic,et al
PHYSICAL REVIEW B 66, 174519 ~2002!
Probe-sample separation: 200 nm
Pole gap: 100 nm
Excitation: 50 mA
Brf
Jsurf

## Slide 5
Nonlinear Setup
RF Coil
on slider
Superconductor
sample
 | SRF | Our Setup
Temperature | 2K | 3.6K-9.3K
RF Magnetic Field | < 200mT | <200mT
Frequency | 1.3 GHz | 1.2GHz– 2.0GHz
Notes: The goal is to diagnose the SRF properties and how they are limited by materials issues.

## Slide 6: Why P3f ?
Defects
D. E. Oates, Y. D. Agassi, B. H. Moeckly,
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 17, NO. 2, JUNE 2007
1)
2)
  Superconducting Sample is the only Source
Notes: Sample is main Source
P3f more detailed
Superfluid Carrier density decreased
Js is not linear with B

## Slide 7
Probe
Sample
Transmission Line
Thermometer
Coaxial Cable
Connection to Probe
4K Plate
T. Bieler, Michigan State University

## Slide 8: BULK NB

## Slide 9
Nb on Copper
Thickness: 1μm

## Slide 10
H0
H1
H2
H3
H4
H5
Thickness: 1μm

## Slide 11
Temperature Dependence of Periodicity

## Slide 12
5th Harmonic

## Slide 14: TF-JLAB-ECR-Nb-aAl2O3-332

## Slide 15: TF-JLAB-ECR-Nb-aAl2O3-353

## Slide 16: TF-JLAB-ECR-Nb-aAl2O3-353

## Slide 17
Thickness: 500μm

## Slide 18
Defects
Nonlinear Meissner Effect
Origins of P3f
-Nonlinear current density scale
Sheng-Chiang Lee, Thesis Defense

## Slide 19
Experiment Data
Curve fitting result (GL model )
Noise floor of spectrum analyzer
JJ, Vortices
Tamin Tai, Behnood G. Ghamsari, and Steven M. Anlage: Nanoscale Electrodynamic Response of Nb Superconductors

## Slide 20
Nonlinearity from JJ between grains
J. Halbritter, Appl. Phys. A 43, 1-28 (1987)
Nb
Nb2O5
NbOx (x<1)
Tc < 2K
Notes: JJ model good agreement at low power

## Slide 21
Rn=200W
S=9x10-14m2
J. Halbritter, “Granular superconductors and their intrinsic and
extrinsic surface impedance,”
Tc=9.25 K

## Slide 22
Superconductor
Vf +
Microwave Source
Low Pass Filter
Tuning Fork Controller
Interaction
High Pass Filter
v3f
Spectrum
Analyzer
Driving Signal
Quartz
Tuning Fork
Response from Sensor
Resonance Frequency Shift
Future Plans
Directional coupler
Cryogenic
Environment
XYZ Pieze Positoin Controller
Resonance Frequency Shift
Notes: No Distance Controll and Scanning Capability with good resolution

## Slide 23
Sample
Transmission Line
4K Plate
Piezo Scanner
Scanning Stage
Coaxial Cable
Probe
Sample
Probe

## Slide 24
Next Step: Scanning
P3f (dBm)
Bi-Sr-Ca-Cu-O
S-C. Lee et al. Phys. Rev. B 71, 014507, (2005).
>77K Scanning

## Slide 25: Conclusion
  Near-field Microwave Microscope that enables mapping of the local electrodynamic response in the multi-GHz frequency regime at cryogenic temperatures was successfully built.
  Advantages of this Method
  1) RF Characterization
  2) Strongly localized so no edge effects
  Disadvantages of this Method
  1) We don’t measure Q or Rs

## Slide 26
  We are looking for Samples and Collaborations.
  Dimensions From 5mm x 5mm Up to 20cm x 20cm
  Flat Surface preferred but not required
  Best Suited : Sample Isolated Defect
  Base Temperature 3.6K , can go down to 100mK if needed
Special Thanks to Dr. Anne-Marie Valente-Feliciano & Dr. tOBIAS Junginger