## Slide 1: Superconducting NbN Thin Films Synthesized by Atomic Layer Deposition
Helmut Baumgart a, Kai Zhang a, Mark J. Sowa b
a Old Dominion University
Dept. Electrical & Computer Engineering –
and
Applied Research Center at Thomas Jefferson Natl. Accelerator Facility
b Ultratech/Cambridge Nanotech

## Slide 2: Introduction
NbN is a Type II superconductor with a Tc of about 16K 1.
NbN thin films were deposited by thermal atomic layer deposition using NbCl5 and NH3.
NbN thin films were also deposited by Plasma-Enhanced Atomic Layer Deposition (PEALD) previously 2.
  Tc = 10.2K, Room T resistivity = 250-cm
Tc of NbN thin films is very sensitive to the growth conditions. Improvements in PEALD NbN process (parameters) may lead to higher Tc and lower resistivity values.
References:
B. T. Matthias, et al., Rev. Mod. Phys. 35, 1 (1963).
M. Ziegler, et al., Supercond. Sci. Technol. 26 (2013) 025008.

## Slide 3: Review of “Multilayer ALD Films for SRF Cavities” (Phase I)
NbN thin films were successfully deposited by thermal atomic layer deposition (ALD) in the temperature range of 450°C – 500°C by reacting the NbCl5 precursor with ammonia (NH3) gas in a first R&D project at the Applied Research Center.
Schematic of Chemical reactions in the ALD process
Savannah 100 ALD reactor system

## Slide 4: Four ALD Reactor Systems in Operation at ODU-ARC Labs

## Slide 5: XRD Results of ALD NbN Films
XRD scan of NbN film deposited on Si substrate at close to 500 C. The following crystalline phases were observed: cubic phase at 2θ = 20.95, at 2θ = 33.42, at 2θ = 41.24, at 2θ = 46.028 and at 2θ = 55.98; one hexagonal phase peak at 2θ = 48.357.
The XRD analysis of the ALD films exhibits the crucial α’ and α” peaks indicative of cubic NbN, which proves experimentally that the superconducting crystalline cubic phase of NbN was achieved.
Crystallization of the resulting NbN films is a sensitive function of ALD deposition temperature. The phase transition to crystalline cubic NbN occurs around 500°C. Furthermore, the feasibility of growing superconductor-insulator-superconductor (SIS) multilayer structures was demonstrated by depositing NbN on ALD Al2O3 films.

## Slide 6: Cross-sectional Micrographs of ALD NbN Thin Films
Figure 1. High resolution cross-sectional TEM image showing a partially crystallized 10 nm ALD NbN thin film on Si substrate deposited by ALD at the relatively low temperature of 450 °C. Large NbN crystallites are visible, which are embedded in amorphous NbN.
Figure 2. Cross-sectional TEM image showing 10 NbN thin film deposited on top of 30 nm ALD Al2O3 on Si substrate in order to realize a superconductor – insulator multilayer structure. The NbN film has similar structure as shown in the TEM of Figure 1.
Figure 3. Field emission Scanning Electron Microscopy (FE-SEM) image of thick ALD NbN film on Si substrate. At a film thickness above 100nm the ALD NbN film exhibits a columnar polycrystalline structure.

## Slide 7: Disadvantage of the old chemical ALD Precursor of NbCl5 available for the initial Feasibility Study
While the research goal of superconducting cubic ALD NbN films was achieved with NbCl5, it was felt, that the corrosive nature of the previous old chemical ALD NbCl5 precursor and of its reaction by-products could be detrimental for large scale technical applications in SRF technology.
NbCl5
Development of a new chemical precursor for ALD growth of NbN is absolutely crucial in order to greatly advance the field of superconducting radiofrequency (SRF) thin films for particle accelerator technology.

## Slide 8: New Developments in Plasma-Enhanced Atomic Layer Deposition (PE-ALD) of Superconducting NbN Films
(t-butylimido) tris(diethylamido) niobium(V) (TBTDEN)
C16H39N4Nb
Form: liquid
Density: 1.015 g/mL at 25 °C

## Slide 9: Experimental
Brand new development of PEALD of NbN films on an Ultratech/CNT ALD
With novel chemical ALD precursor (t-butylimido) tris(diethylamido) niobium(V) (TBTDEN) (100°C)
Spectroscopic ellipsometry for film thickness, n, and k
Four point probe technique to assess thin film resistivity
Tc measured with Quantum Design PPMS through a Stanford Research Systems SR830 lock-in amplifier
Composition data from PHI Versaprobe XPS
The substrate surface is exposed to TBTDEN, which generates a saturated mono-layer on the substrate.
The residual TBTDEN is purged with argon to avoid additional chemical vapor deposition.
The mono-layer is reduced by a hydrogen plasma to form a mono-layer of NbN.
A second argon purge.
Each cycle produced one mono-layer of NbN.

## Slide 10: NbN Film Composition using the new ALD Precursor with PEALD Technology
Binding energy of the Nb 3d5/2 peak is ~203.5 eV for all samples consistent with NbN (203.5 - 204 eV) or NbO (202.8 - 204.8 eV) but not Nb metal (201.8 - 202.5 eV)5
C1s peak at ~282.5 eV suggests presence of NbC5
Depositions resulted in Nb-rich films
H-rich plasmas deplete film of N resulting in higher Nb:N
Temperature increase increases Nb and decreases N resulting in higher Nb:N

## Slide 11: Resistivity and Superconductivity with new ALD Precursor
Resistivity decrease and Tc increase depend primarily on temperature and H2 flow rate increases
Plasma power increase is a secondary influence on decreasing resistivity and increasing Tc
Nb-rich films have lower resistivity and higher Tc
Negative linear relationship between Tc and resistivity predicts 100C (3035-cm) and 150C (772-cm) films not superconducting

## Slide 12: NbN Film Growth Per ALD Cycle with New Precursor
GPC primarily depends on temperature
Small GPC increase with H2 flow at 300°C/300W
Small GPC decrease over power range at 80sccm H2/300°C

## Slide 13: Optical Properties of NbN Films synthesized with new ALD Precursor
Refractive index decreases and extinction coefficient increases depend primarily on temperature and H2 flow rate increases
Plasma power increase is a secondary influence on decreasing n and increasing k
Higher k and lower n in Nb-rich films

## Slide 14: Conclusion
Superconductive NbN thin films could be achieved by PEALD using the newly developed (t-butylimido) tris(diethylamido) niobium(V) (C16H39N4Nb) chemical ALD precursor.
The new PEALD NbN Films exhibit Tc values as high as 13.5K showing tremendous potential for further optimization. This is a game changer!
Room-temperature resistivity values as low as 173-cm.
Resistivity and n decrease, Tc and k increase as NbN films become more Nb-rich at high deposition temperature, high H2 flow rate, and high plasma power.
NbCl5