## Slide 1
Status Report on Reactive Ion Etching of SRF Cavities in an RF Ar/Cl2 Discharge
Jeremy Peshl,a J. Upadhyay,a A. Palczewski,b D. Im,a S. Popovic,a
A.-M. Valente-Feliciano,b L. Philips,b and L. Vuskovica
aDepartment of Physics, Center for Accelerator Sciences
Old Dominion University, Norfolk, VA
bThomas Jefferson National Accelerator Facility, Newport News, VA

## Slide 2: Superconducting Radio Frequency Cavity
Elliptical SRF cavity made of Niobium,
Superconducting material at 9.2K
BCP and EP of the cavity with
The help of HF and other acids
Complex shaped crabbing cavity
9 cell Elliptical SRF cavities are 1m long and 1.5 GHz has approx. 15 cm diameter
Q0 Versus Eacc Graphs for SRF Cavity
Experimental Set-up for Plasma Etching of Single Cell SRF Cavity

## Slide 3: Motivation and Challenges
Motivation
Low cost in both setup and operation
No wet chemistry (specially no HF)
Environment and people friendly
(compare to wet etching process)
Full control on the final surface (A variety of surfaces can be intentionally created through plasma processing, such as pure niobium pent oxide, doping of any material or thin films like superconducting niobium nitride…)
Challenges
Etching of inner surface of a three dimensional object
Removal of 10-150 microns of material from large surface area
Transportation of the removed material outside of the vacuum system
Uniform plasma surface interaction on inner surface of a long cylindrical object with constant or varying diameter
Characterization and modeling of the coaxial plasma, specifically the electronegative coaxial plasma
Establish correlation between process parameters and observables
Increasing the etching rate and reducing the surface roughness

## Slide 4: Etching Mechanism of Niobium in Ar/Cl2 Plasma
J. Upadhyay et al., J. Appl. Phys. 117, 113301 (2015).
Establish correlation between process parameters and observables
Etch Rate as a Function of Gas and Etching Conditions
Etch Rate as a Function of dc Bias
Etch Rate as a Function of Nb Temperature
Sheath Voltage in Coaxial Plasma with dc Bias

## Slide 5: Experimental Setup for Cylindrical Cavity
Etching of inner surface of three dimensional object (dc bias)
Cylindrical Cavity with ring samples, color gradient shows depletion of radicals at first sample
RF Power
Gas Flow
Experimental Set-up for Cylindrical Cavity
Etch Rate of Nb as a function of pressure
Etch Rate of Nb as a function of rf power
Single cell SRF cavity
J. Upadhyay et al., Phys. Rev. ST Accel. Beams. 17, 122001(2014).
Front View of Coaxial Electrode Set-up and Plasma in Cylindrical Cavity

## Slide 6: Etch Rate Uniformity Dependence
Etch Rate Uniformity as a Function of Pressure
J. Upadhyay et al., J. Appl. Phys. 117, 113301 (2015).
Uniform plasma surface interaction on inner surface of a long cylindrical object
with constant or varying diameter
Etch Rate Uniformity as Function of Diameter of Electrode
Etch Rate Uniformity as a Function of Chlorine Concentration

## Slide 7: Self-Bias Dependence on Geometry of Electrode
Self-Bias as a Function of Pressure with Different Surface Area Electrode
Self-Bias as a Function of Pressure with Different Surface Area Electrode
Different Surface Area Electrode
Self-Bias as Function of Power with Different Surface Area Electrode
Etch rate variation as a Function of
Different Surface Area Electrode
Reversal of Asymmetry with Disk Loaded Electrode
J. Upadhyay et al., J. Vac. Sci. Technol. A 33, 061309 (2015).

## Slide 8: Single Cell Pill Box Cavity
Uniform plasma surface interaction on inner surface of a long cylindrical object with constant or varying diameter
Niobium ring samples with plasma inside pill box cavity
Single cell cavity with pill box cavity
Schematic of Single cell cavity plasma processing experimental setup
Complex plasma asymmetry configuration for pill box cavity plasma processing

## Slide 9: Single Cell SRF Cavity
Experimental Set-up for Plasma Etching of Single Cell SRF Cavity
Pill box cavity with electrode and conical gas flow inlet

## Slide 10: First RF Test of Plasma Etched SRF Cavity
Plasma Etched Single Cell Cavity (2/2/15)
BCP Single Cell Cavity (8/27/14)
Image of the residues
Elemental analysis of the residues
J. Upadhyay et al, arXiv:1605.06494 (2016).
8/27/2014: BCP, 6000 C 10-hr bake, degreased, and high water rinsed.
2/2/2015: 24-hr plasma etch, high water rinsed, ultrasonic cleaning.
2/12/2015: 900-1400 C 14 bake.
11/03/2015: Chemical aqua regia solution, phosphoric acid rinse. (No HF!)

## Slide 11: Induced Field Emission for FE Suppression

## Slide 12: Increasing Q0, Efficiency and Etch Rate
Increasing Q0: All Niobium System
Efficiency: Pulsed Operation
Etch Rate: Tailoring the AIEDF
Faster etching, Less surface roughness
No Etching
Etching, High surface roughness
IEDF
E
Eact
IEDF
Eact
Faster etching, Minimal surface roughness
E
IEDF
E
Eact
IEDF
E
Eact
Sinusoidal: No Bias
Sinusoidal: Bias
Pulsed Periodic: Nonsinusoidal
Pulsed Sinusoidal: Bias

## Slide 13: Concluding Remarks
Accomplishments
Etching of inner surface of three dimensional object
Removal of 10-150 microns of material from large surface area
Establish correlation between process parameters and observables
Uniform plasma surface interaction on inner surface of a long cylindrical object with constant or varying diameter
Current and Future Work
Transportation of the removed material outside of the vacuum system
Characterization and modeling of the coaxial plasma, specifically the electronegative coaxial plasma: OES Diagnostics
Converting all working parts to Niobium: Increasing Q0
Pulsed RF power source: Efficiency
AIEDF tailoring: Etch Rate and Surface Roughness

## Slide 14
Work support by DOE, Grant No. DE-SC0007879
Thank You

## Slide 15: Diagnostics: Langmuir Probe vs. OES
Electron temperature and election density trends using Langmuir Probe and Optical Emission Spectroscopy measurements.

## Slide 16: Diagnostics: Optical Emission Spectroscopy
F.O. Viewing Holes
Fiber Optic
Spectrometer Slit
Experimental setup for collection of spectral data in the radial direction.
Intensity profile of each line with respect to radial position at 30 mTorr pressure, 50 W rf power, and no positive DC bias.
Notes: To ensure consistent measurements along radial positions a lens cap was 3-D printed with equally spaced holes.
A fiber optic cable is used to transfer the light from the discharge to the spectrometer.
Three pressures: 15 mTorr, 30 mTorr, 50 mTorr. 8 spectral lines for each position (15) at 50 W, 100 W, and 150 W. Repeated for no positive DC bias, 0 V total bias, and 200 V total bias.

## Slide 17: Diagnostics: Optical Emission Spectroscopy
Work by Boffard et al. opens the door to an interesting diagnostic alternative using the kinetic model.
Ar: Ar/Cl2:
Chart: Ar/Cl2: Electronegative Discharge
Chart: Ar: Electropositive Discharge
Argon Plasma
Argon/Chlorine Plasma
J. B. Boffard et al., J. Phys. D: Appl. Phys. 45, 045201 (2012).