## Slide 1: Building 1.3 Ghz SRF Copper Substrate Cavities for SRF Applications
J. Spradlin, A. Palczewski, L. Phillips, H. Tian, B. Clemens, & C. Reece
Jefferson Lab – SRF Institute – Process & Materials Analysis Group
7th International Workshop on Thin Films and New Ideas for Pushing the Limits of RF Superconductivity

## Slide 2: Copper Cavity Fabrication Scope
Produce Cu cavities as deposition substrates
  1.3 GHz “Low Surface Field” (LSF) cell geometry
Started with initial batch of eight cavities
  Minimalist approach to parts handling and acceptance criteria
  Issues arose with fabrication, both EBW and chemistry
Reworked process for weld prep and weld parameters
  Used reject parts as development tools
Salvaged cavity now serving as a prototype - in CBP
Started the next batch of cavities with vetted procedures

## Slide 3: What went wrong?
Welds had an array of “features” that are not desirable for an RF cavity or substrate
  Voids, pits, uneven HAZ, and lack of part joining
With residues present in the weld region, or insufficient weld spot energy, cracks / voids / features result, which subsequently trap species from chemistry compounding problems
Good Weld
Poor Weld

## Slide 4: Diagnosis & Corrective Actions
Contamination in the weld region was identified as the root cause of “features”
Implemented methods used for Nb cavity fabrication
  Weld trim back & Inspections for burs and surface imperfections
  Aggressive parts etch and strict handling procedures leading into EBW
Optimized weld parameters
  Weld is sensitive to thermal history and part mass
  Pre-heating parts prior to welding provides consistent reproducible seams

## Slide 5: Cu Cavity Fabrication Process (1/2)
Re-etch or Reject
Stock Selection
Q/C on Pedigree
Cut and Shape Beam Tubes and ½ Cells
Q/C on Dimensions
Weld Trim Back
Q/C on Dimensions & Appearance
Braze SS316 Transitions to Beam Tubes
Q/C on Braze
EBW SS316 Flanges to Beam Tube Transitions
Q/C on EBW
Iris Weld Prep Etch
½ Cell Iris to Beam Tube with Flange
Q/C on Appearance
Weld ½ Cell Iris to Beam Tube
Q/C on Appearance
Equator Weld Prep Etch
½ Cell with Beam Tube & Flange
Q/C on Appearance
Weld ½ Cells @ Equator
Q/C on Appearance
Process Step
Quality Control
Corrective Action
Resource Stock
Reject or Repair
Re-etch or Reject
Reject or Repair
Reject or Repair
Reject or Repair
Reject or Repair
Reject or Repair
Reject or Repair

## Slide 6: Cu Cavity Fabrication Process (2/2)
Re-etch or Reject
CBP Step 1
Q/C on Appearance
Etch Cavity
Cu BCP 30 µm
Q/C on Appearance
CBP Step 2
Q/C on Appearance
Etch Cavity
Cu BCP 30 µm
Q/C on Appearance
CBP Step 3
Q/C on Appearance
Etch Cavity
Cu BCP 30 µm
Q/C on Appearance
Tune Cavity
Q/C on Appearance
HPR Cavity
Q/C on Appearance
EP Cavity
Q/C on Appearance
Process Step
Quality Control
Corrective Action
Repeat CBP Step 1, Repeat Cu BCP, or Reject
Reject or Repair
Repeat HPR, Re-etch, or Reject
Re-etch, Re-CBP, or Reject
Repeat CBP Step 3, Repeat Cu BCP, or Reject
Re-etch or Reject
Repeat CBP Step 2, Repeat Cu BCP, or Reject
Re-etch or Reject

## Slide 7: Copper Buffer Chemical Polish
Transene Aluminum Etch A / Cu BCP
H3PO4 : HNO3 : HAc : H2O (18:1:1:2)
  4.5 to 6 µm / min @ 23 °C for conditions comparable to a cavity
  Reported 2.4 µm / min @ 50 °C
Closest to Cavity Conditions
5.5 µm / min
17 g / L
Best Case /
Highest Etch Rate
8.8 µm / min
0.47 g / L
12 cm3 Cu Fresh 350 mL 2 hr
0.6 cm3 in Fresh 1 L for 2 hr
  Bad!
  3.72 µm / min
  0.4 g / L
25kX
5kX
25kX
5kX

## Slide 8: Weld Preparation Chemistry Process
Clean Parts
Q/C on Appearance & Burs
DI Rinse
Q/C on Appearance
Methanol Rinse
Q/C on Appearance
Anti-Static N2 Dry
Q/C on Appearance
Cu BCP Etch
HPO4 + HNO3 + HAc + DI (16:1:1:2)
Q/C on Appearance
Process Step
Quality Control
Corrective Action
Correct Dimensions, Braze, or Weld Issues
then Re-clean, De-bur, & Re-clean
Re-etch for 10 – 15 µm
DI Rinse
1st Drag Retain then to Resistivity
Q/C on Appearance
Sulfamic
Q/C on Appearance
DI Rinse
1st Drag Retain then to Resistivity
Re-etch for 10 – 15 µm
Q/C on Appearance
Methanol Rinse
Q/C on Appearance
Anti-Static N2 Dry
Re-etch for 10 – 15 µm

## Slide 9: Weld Prep
As-Welded Beam Tube
Cleaned Beam Tube
Cu BCP Weld Prep Fixture
(2) Cu Cavity’s Etched Parts Awaiting Assembly for EBW

## Slide 10
We experimented with a variety of current and feed speed combinations with full-mass test cavities.
Finding the Right Weld Parameters

## Slide 11: Welding Cu Cavities
We use 1/8” (~3.175 mm) Cu sheet
  Same forming dies as for bulk Nb cavities
We sought a full-thickness, full-penetration weld parameter
Cu EBW is very different from Nb EBW
  Much lower melting temperature
  Much higher thermal conductivity
Found that the part starting temperature greatly affects attaining full penetration
  Residual EBW heat in the Cu parts significantly affects Cu weld penetration even after 1 hour!
Managed pre-heating is necessary to realize consistent results
  Amount of required pre-heat scales with total part mass

## Slide 12
Inadequate preheat yields inadequate weld penetration.
Weld Quality Examples
Incomplete Penetration
Uneven HAZ
Full Penetration
Incomplete Penetration
Full Penetration
Semi-Full Penetration
Incomplete Penetration
Full Penetration

## Slide 13: Welding Parameters
Further refinement is quite possible, but this is what we are working with now.
Our current weld parameters:
    Gun voltage – V = 50 kV
    Beam current – Iweld = 74 mA
    Weld speed – 20 ipm (50.8 cm/m)
    Oval puddling raster - approx. 0.055" x 0.125“
    Focus point above the surface
  Immediately precede this weld with a pre-heating sealing-pass weld with total energy deposition sufficient to bring whole-part equilibrium temperature to ~118C.
    From development cavity weld studies: ~280 kJ is required to raise whole cavity, 8 kg Cu, from 27 °C to ~118C neglecting radiant heat losses
    Ipreheat = 48 mA, other parameters the same

## Slide 14: Cu Cavity CBP 1st Step + Cu BCP Etch
Slight Water Staining on Cell
Clean Finish on Beam Tube Interior
Slight Water Staining on Cell
Clean Finish on Beam Tube Interior

## Slide 15: Cu Cavity Final EP Surface
CBP + EP – Stain Free after Sulfamic Rinse

## Slide 16: Cu Cavity Fabrication Status
Had some minor delays in fabrication of Cu cavities due to poor quality EBW seams
Weld consistency / reproducibility was poor
  Across a single join and comparing between joins of similar parts
  Visible arcing in the welding process!
Aligned weld pre-process with Nb cavity fabrication
  Emphasis on cleanliness!
Optimized weld parameters for consistent results
  Part thermal character / history is crucial!
Once residues in the seam were removed… it was found that the thermal mass and history of parts influence weld quality
  Cu has higher thermal conductivity and heat capacity compared to Nb  heat removed from HAZ faster and subsequently requires more local energy (i.e. beam power & / or part pre-heat)
Started second batch of cavities this week!

## Slide 17: Acknowledgements
This work is supported by the U.S. Department of Energy, Office of Science, Office of Nuclear Physics under contract: DE-AC05-06OR2317
Jefferson Lab SRF Operations & R&D:
  Parts Machining, Forming, & Brazing: S. Williams
  Welding: K. Worland & A. Auston
  Chemistry & CBP: J. Follkie, T. Harris, A. Anderson, & C. Johnson
  Dimensioning: B. Carpenter & A. G. DeKerlegand
  Tuning: D. Forehand, R. Overton, & C. Dreyfuss
AASC Collaboration

## Slide 18: Cu BCP Etch Rate Surface Morphology Comparison
12 cm2 in Fresh 350 mL Cu BCP for 2 hours
0.6 cm2 in Fresh 1 L Cu BCP for 2 hours
6 cm2 in Used & Stored 1 L Cu BCP for 20 min

## Slide 19: Cu BCP Etch Rate Surface Morphology Comparison
0.6 cm2 in Fresh 1 L Cu BCP for 2 hours

## Slide 20: Cu BCP Etch Rate Surface Morphology Comparison
12 cm2 in Fresh 350 mL Cu BCP for 2 hours