## Slide 1: LTB in N2
Pashupati Dhakal

## Slide 2: 120C/48hrs bake
No Q-change <30 MV/m
FG, RRR ~ 250

## Slide 3: 120C/48hrs bake @ 25 mTorr N2
~ 25% Q improvement at 30 MV/m

## Slide 4: 120C/48hrs bake @ 25 mTorr N2
No Q-improvement @ 30MV
Factor of 2 improvement @ 18MV/m

## Slide 5: Conclusions
LTB in N2 works
Why? What is the mechanism?
Does N2 diffuse? Infuse? Or is it just a surface impurity effect.
Sample study underway.