## Slide 1: Post-mortem investigation of leaky gate valves condition of Viton O-ring in terms of particulate shedding and nature of failure
Greg Marble, Rongli Geng
Six-Month Follow-Up on Action Items of Feb 2016 CEBAF Field Emitter Workshop
September 12, 2016, JLAB

## Slide 2: Beamline Valves Removed from CEBAF during NL12 Cryomodule Swap
NL12
VBV1L11B
VBV1L13A
Both had known leak
Both removed and replaced during SAD 2016

## Slide 3: VAT Mini UHV Gate Valve Sealing Mechanism

## Slide 4
1A Large particle
1B Cav side/large “drop”
1C Gird side/small “drop”
#1
1D Seal surface/track and particles

## Slide 5: 1A Large Particle
This particle is partially embedded into O-ring, it survived air blowing by mouth

## Slide 6: Large Particle Profile
~ 0.5 mm wide, ~0.4 mm height

## Slide 7: 1B Cav side/large “drop”

## Slide 8: Large “drop” profile
~ 0.5 mm wide, Peak height 0.37 mm

## Slide 9: 1C Gird side/small “drop”

## Slide 10: 1D Seal surface/track and particles
Many particles remain on and near sealing surfaces even after blowing with air gun

## Slide 11
#2
2B Seal surface/track
2A Seal surface/ multi particles

## Slide 12: 2A Seal surface/ multi particles
In three areas, multiple particles are embedded into O-ring along sealing surface

## Slide 13: 2B Seal surface/track

## Slide 14: Gate inside valve Body

## Slide 15: Current Understanding
O-rings visually appear to be normal – no cracking or fragmentation observed (contrary to the claim of radiation damage?)
Particulate embedment into the sealing surface seems to be the root cause for leak.