## Slide 1
High Temperature Heat Treatment to Raise the Quality Factor of Large Grain Niobium Cavities
Pashupati Dhakal
Gianluigi Ciovati
Ganapati Rao Myneni
July 16-17, 2012

## Slide 2
July 16-17, 2012
Q0
Eacc (MV/m)
1010
1011
10
20
30
40
50
Increase Q
Increase Eacc
MP, FE, Quench
Q = G/Rs

## Slide 3
July 16-17, 2012
Typical SRF cavity Processes
~100 mm CBP
~Light BCP/EP
HT
(600-800 oC)
~20 mm
BCP/ EP
~LTB (120-140 oC)
HPR
RF Test

## Slide 4
July 16-17, 2012
High Temperature Heat Treatment
1970s  ~1800 oC UHV HT for ~10 hrs.
1980s  ~1300 oC solid state getter, such as Titanium,
was used in-side the furnace to "post-purify”.
2000s  600-800 oC, mainly just to degas hydrogen absorbed
by the Nb during cavity fabrication and surface
treatments.
    BCP/ EP needed to remove “polluted” layer after HT
    Reintroduces hydrogen
    May be the cause of strong RF losses

## Slide 5: High temperature annealing removes gross hydrogen
July 16-17, 2012
Standard (600-800 oC) Furnace Treatment
The standard furnace used for the high-temperature heat treatment of SRF cavities is an ultra-high-vacuum furnace with molybdenum hot-zone; molybdenum (or tungsten) resistive heating elements and cavities are heated by radiation from the heating elements.
Ciovati et al, PRSTAB 13, 022002 (2010)

## Slide 6
July 16-17, 2012
Induction Heating
UHV with all Nb hot zone
Clean (avoid post HT chemical etching)
Pure gas injection for surface passivation
Dhakal et al, Rev. Sci. Instrum. 83, 065105 (2012)

## Slide 7
July 16-17, 2012
Induction Furnace
Dhakal et al, Rev. Sci. Instrum. 83, 065105 (2012)

## Slide 8
July 16-17, 2012
Large Grain Cavity
 | Ta | H | O | N | C | RRR
Ingot |  |  |  |  |  | 
F | 1330 | <1 | <6 | <3 | <30 | 226±10
G | 1375 | 7.1 | <6 | <3 | <30 | 197±8
H | 704 | <1 | <6 | <3 | <30 | 240±9
G1G2
Ingot from CBMM
F1F2  Standard Treatment
G1G2  New Treatment
H1H2  New Treatment (limited by pits)

## Slide 9
July 16-17, 2012
1400 C HT in induction Furnace
Vent with
O2 at RT

## Slide 10
July 16-17, 2012
RF Test
~2 nW
~1nW
Rres
Dhakal et al, IPAC 12, WEPPC091

## Slide 11
July 16-17, 2012
RF Test
4.6x1010 @ 20 MV/m
CEBAF upgrade standard process
average Q0(2K, 70 mT= 1.2±0.7x1010
Q0(1.5K)  2x1011
Dhakal et al, IPAC 12, WEPPC091

## Slide 12
July 16-17, 2012
RF Test
Quench location near equator
Review of impurity depth profiling in Nb by SIMS
By: Prateek Maheshwari : Tomorrow 11:00 am

## Slide 13
July 16-17, 2012
New Proposed Processes
~100 mm CBP
~Light BCP/EP
HT
(600-800 oC)
~20 mm
BCP/ EP
~LTB (120-140 oC)
HPR
RF Test
HT
1400 oC
HPR
RF Test
Surface Passivation

## Slide 14
July 16-17, 2012
The combination of large-grain Nb, high-temperature HT (~1400 °C) is a promising alternative to produce SRF cavities with high Q0 values in the medium field range, which is particularly important for future continuous wave particle accelerators.
Conclusions

## Slide 15
July 16-17, 2012
R. Geng, JLAB
DESY

## Slide 16
Effect of HT on Nb
surface