## Slide 1: Tensile Tests on Single Crystal Specimens with Different Orientations
D. Kang1, D. Baars1, T. Bieler1, C. Compton2
1Michigan State University, East Lansing, MI
2Facility for Rare Isotope Beams, East Lansing, MI
Work funded by DOE-OHEP
7th SRF Materials Workshop

## Slide 2: Identifying active slip systems in Nb
Motivation
  Slip activities  recrystallization  cavity performance
  Simulating deformation and recrystallization
Determining slip systems
  Slip trace: intersection of surface and slip plane
  Slip direction: usually rotates towards tensile direction
  High resolved shear stress
Baars, Investigation of active slip systems in high purity single crystal niobium, PhD dissertation
Single
slip system
Two slip systems
Two with similar trace

## Slide 3
Slip trace analysis – an example
Baars, Investigation of active slip systems in high purity single crystal niobium, PhD dissertation

## Slide 4
Uniaxial tensile tests for studying active slip systems
12 sets of specimens (O~Z) favoring different slip systems
9 of them deformed to 40% engineering strain
Loading rate: 1mm/min
Baars, Investigation of active slip systems in high purity single crystal niobium, PhD dissertation

## Slide 5
Stress-strain behavior varies greatly with orientations
S and T ended up being the softest two
U hardened more than a typical poly-crystal
P and T had a similar initial hardening slope
Start
End
Baars, Investigation of active slip systems in high purity single crystal niobium, PhD dissertation

## Slide 6
{112} slip almost accounts for all the initial
hardening behavior of the 9 specimens
Specimen | Difference between highest resolved shear stress on primary and secondary {112} slip systems (MPa), and ratio of resolved shear on two highest {112} systems | Initial hardening rate
X3 | 4 1.316 | Barely
Q2 | 4 1.263 | Barely
S3 | 3.5 1.237 | Barely
R2 | 3.5 1.200 | Slight
W3 | 1.4 1.091 | Moderate-Low
T3 | 1.3 1.073 | High
U3 | 0.6 1.027 | Very High
V3 | 0.4 1.022 | Moderate-High
P3 | 0.1 1.042 | High
Baars, Investigation of active slip systems in high purity single crystal niobium, PhD dissertation

## Slide 7
Limitations with previous tests; in-situ tensile tests
Path for orientation evolution from 0% to 40% strain is unknown
Specimens were not heat treated to get rid of preexisting dislocations
In-situ tensile tests
  Better correlation between real time orientations and slip traces
  Multiple locations along tensile axis are examined for orientation gradient effects
  Heat treatment at 800°C for 2h to reduce the number of possible forest dislocations
Start
End

## Slide 8
First attempt with specimen O3, loading rate 4 µm/s

## Slide 9
After deformation to 19% engineering strain*
*Strain is calculated based on positions of the two markers

## Slide 10
Engineering stress-strain curve
Three increments (0%9%12%19%) were used
Tensile stage lost control at the end of first increment and reloaded from 0
The stage reached its limit before 20% strain

## Slide 11
Comparison with previous tests
Nothing striking in terms of yield strength and work hardening

## Slide 12
Before deformation – orientation map
5 mm

## Slide 13
After 9% engineering strain – orientation map
5 mm

## Slide 14
After 12% engineering strain – orientation map
5 mm

## Slide 15
After 19% engineering strain – orientation map
5 mm

## Slide 16
Before deformation – orientation deviation map
5 mm

## Slide 17
9% strain – orientation deviation map
5 mm

## Slide 18
12% strain – orientation deviation map
5 mm

## Slide 19
19% strain – orientation deviation map
5 mm

## Slide 20
Before deformation – pole figures
5 mm

## Slide 21
9% strain – pole figures
5 mm

## Slide 22
12% strain – pole figures
5 mm

## Slide 23
19% strain – pole figures
5 mm

## Slide 24
Before deformation – SEM images
5 mm
200 µm
SEI
BEI
SEI – Secondary electron imaging
BEI – Backscattered electron imaging

## Slide 25
9% strain – SEM images
5 mm
SEI
BEI
200 µm

## Slide 26
12% strain – SEM images
5 mm
SEI
BEI
200 µm

## Slide 27
19% strain – SEM images
5 mm
SEI
BEI
200 µm

## Slide 28: Summary
{112} slip arguably has an advantage over {110} during deformation at room temperature for high purity Nb
In situ tensile tests enable better correlation between slip systems and orientations, although there are challenges
  Could not reach 40% strain due to stage limits
  Occasional hiccups with the tensile stage
  Stress relaxation between strain increments is a potential source for inaccuracy