## Slide 1
Atomic-scale characterization of Nb for SRF cavities using UV
laser-assisted LEAP tomography and Cs-corrected TEM
7th SRF Materials Workshop, JLAB Newport News, VA
July 16-17, 2012
YoonJun Kim1, David Seidman1, Runzhe Tao2, Robert Klie2
1. Department of Materials Science and Engineering
Northwestern University, Evanston, IL
2. Department of Physics, University of Illinois, Chicago, IL

## Slide 2
 LEAP Tomography - Pure Nb coupon
A pure Nb coupon had been analyzed using LEAP.
- Sample ID: R06_17114.RHIT
Sample preparation:
(1) (at FNAL) Pure Nb coupons supplied by Alex Romanenko
- A buffered chemical polished single-grain Nb sheet.
- Test coupons were cut using electrical discharge machining (EDM).
Approximate dimensions of 10 x 10 x 2 mm3
(2) (at NU) Tip preparations
- Baked at 800 oC for 4 hours in UHV furnace
- Pt deposition using South Bay Technology - Ion beam sputtering (≈150nm)
- Lift-out method using a dual-beam FIB
LEAP tomography conditions
(1) Pulse rate: 250 kHz
(2) Pulse energy: 50 pJ (necessary for oxide analysis)
(3) Temp.: 30 K
(4) Evaporation rate: 0.50%

## Slide 3
Results: 3D-reconstruction
Detector Histogram | Tip Profiling | 3-D Reconstruction
 LEAP Tomography – Results (3-D reconstruction)
H
O
Nb
Ga
NbH
NbO
NbO2
Nb2O5
Pt
300 nm

## Slide 4
Results: 3D-reconstruction (Front view)
Sequence (Top down)
: Pt (not displayed)  Oxides (~5 nm, NbO2NbONb2O5)Pure Nb (~5 nm)
 Nb, H, NbH mixture (~40 nm)  Bulk Nb
Nb | H | NbH | NbO | NbO2 | Nb2O5
 LEAP Tomography – Results (3-D reconstruction)

## Slide 5
All (0-10 nm) | All | Nb
NbO | NbO2 | Nb2O5
 LEAP Tomography – 3-D reconstruction- top views

## Slide 6
All (10-20nm) | All | Nb
NbO | NbO2 | Nb2O5
 LEAP Tomography – 3-D reconstruction- top views

## Slide 7
All (20-35 nm) | All | Nb
NbO | H | NbH
 LEAP Tomography – 3-D reconstruction- top views

## Slide 8
 Overall O/Nb and H/Nb Ratios along Z-axis
Oxide
Pure
Nb
Hydride
layer
Bulk
Nb
1.5
O/Nb ratio is highest value of 1.5 at the top surface as deep as 2 nm, then decreases
and is 1.0 at 4 nm depth.
H/Nb fluctuates inside of oxide layer and stabilizes at ~0.7 below a depth of 10 nm
(possibly b or z phases).
Further phase identification has been performed using TEM/EELS in collaboration
with Prof. R. Klie and R. Tao at University of Illinois at Chicago.
0.7
1.0

## Slide 9
Selected Area Diffraction Patterns at R.T. (300K)
 TEM/STEM Analysis – 1. Hydride
110 zone of BCC
110 zone BCC
+ superlattice reflections

## Slide 10
Selected Area Diffraction Patterns at 94 K
b
e
z
 TEM/STEM Analysis – 1. Hydride
H/Nb≈1
H/Nb≈0.75
T. Schober et al., Topics in Applied Physics, 29, 11-71, 1978
H/Nb≈0.70

## Slide 11
1
2
3
4
5
6
7
8
9
10
Nb2O5
NbO2
NbO
Nb
1
2
3
4
5
6
7
8
9
10
NbO2
NbO2
NbO2
NbO2
NbO
Nb
NbO
NbO
NbO
Nb2O5
Nb
 EELS – Plasmon peaks analyses at 94K
Pt Layer
Oxide
Bulk Nb
Bach et al., Microc. Microanal. 15, 505-523, 2009

## Slide 12
 TEM/EELS vs. LEAP Tomography
Oxide
layer
<Core-loss peak of Nb M and O K-edges>
Pt
Layer
NbO2
Nb2O5
Nb
NbO
Nb2O5
NbO2
NbO
Nb
NbH
H
Oxide type identification using Plasmon peak
Three different oxides (NbO2, NbO, and Nb2O5) are coexist with 4-5 nm in thickness.
NbO2 is observed to be a predominant oxide type quantitatively
Sequence of oxides is not perfectly identical between EELS (NbO2 Nb2O5NbO)
and LEAP tomography (NbO2NbO Nb2O5).

## Slide 13
 Summary
3-D LEAP tomographic reconstructions show oxides, hydride, and bulk Nb layers.
Oxide layers consist of NbO, NbO2, and Nb2O5, 5 nm in thickness, followed
by a pure Nb layer about 5nm in thickness.
All types of oxides are found around 110 type pole regions of Nb, but NbO is also
rich in 100 type pole regions.
NbH layer forms at 40 nm between pure Nb layers and is found mostly around
110 type pole regions of Nb.
O/Nb ratio within oxide layer decreases from 1.5 to 1.0 and H/Nb ratio within
hydride layer is 0.70.
There are bumps of H/Nb ratio (rich in H ) at the interfaces between layers.
Oxide analyses compared to EELS analyses
: From line scans of the surface region based on the low-loss EELS spectrum
at 94 K, oxide layer consists mostly of NbO and NbO2. This agrees with
LEAP tomographic analyses.

## Slide 14
This study is funded by USDOE through Fermi National Accelerator Laboratory
(FNAL).
We are grateful to Drs. Lance Cooley and Alex Romanenko in FNAL for supplying
samples and valuable discussions.
The LEAP tomographic measurements were performed at the Northwestern
University Center for Atom-Probe Tomography (NUCAPT).
The LEAP tomograph was purchased and upgraded with funding from
NSF-MRI (DMR-0420532) and ONR-DURIP (N00014-0400798, N00014-0610539,
N00014-0910781) grants.
 Acknowledgements