## Slide 1: Scanning Tunneling Microscopy Studies of Single-Crystal Niobium Oxidation
Natalie A. Kautz, Yichen Yu, Kevin D. Gibson
and Steven J. Sibener
SRF Materials Workshop 2012
The James Franck Institute and The Department of Chemistry
The University of Chicago, Chicago, IL
in partnership with
DOE-HEP Collaboration and FermiLab

## Slide 2
2011-2012… New Cryogenic STM Completed and Fully Operational
Single crystals allow us to identify the physical and chemical properties each individual face contributes to the polycrystalline SRF cavity
Instrument was specially designed and built to function in temperature range between liquid helium and > 1800 oC for this work
System will sputter and heat crystals to temperatures > 1800 oC for sample preparation
Chemical analysis of surface is performed by Auger spectrometry
Capable of studying reaction kinetics and performing TPD experiments
In situ STM and STS can be performed from liquid helium to > 1200 oC temperatures
Nb(110)
Nb(111)
Nb(100)
(111) and (100) used here, (110) available
Crystals heated in UHV to 1800 oC to form niobium oxides
STM performed at room temperature
Notes: Newly designed and built within the last year, fully functional
Imaging hot and at liquid helium temperatures
Kinetic and TPD studies

## Slide 3: Underlying Crystal Face Influences NbO Structure
-1 V, 0.5 nA
1850 oC for >3 hrs.
  NbO on (111) is disordered
Despite extensive heating, no long range NbO structure is
formed
Nb(111) crystal face is very “open”
  Top Nb Layer
  2nd Nb Layer
  3rd Nb Layer
  NbO on (100) orders beautifully
-0.5 V, 0.1 nA
1750 oC for 10 sec.
Repeating “ladder” structure formed after short heating times
Nb(100) is more closely packed
Covers entire surface
Notes: Remember to highlight that this is NbO, not just Nb
More closely-packed surface

## Slide 4
Formation of (nx1) Oxides on Nb(100)
Ladder-like features are composed of NbO
Structural model proposed by An, B.; Fukuyama, S.; Yokogawa, K.; Yoshimura, M. Phys. Rev. B 2003, 68, 68.
(3x1)-O
(4x1)-O
Å
nm
(3x1)-O
(3x1)-O
(4x1)-O
Observe coexistence of two
structures: (3x1)-O and (4x1)-O
Bright features are parallel
rows of Nb atoms
~1.0 nm
Ladder length ranges from
2.5 – 7.5 nm
~1.33 nm
Two NbO structures coexist on the (100) surface
Average
~ 4.8 nm
-0.5 V, 0.1 nA

## Slide 5: Preferential Binding Sites For Molecular Oxygen on Nb(100) Oxide
Surface has been exposed to 9L of O2 at room temperature
Formation of amorphous NbO2 and Nb2O5 structures
Observe large-scale features of the underlying ladder structure
Terraces and step edges remain
Amorphous oxides follow ladder orientation
Oxide clusters do not uniformly cover the NbO surface
O2
-0.5 V, 0.1 nA
Oxygen binds along rows of Nb atoms
Notes: Oxygen does not uniformally cover the surface
Include that this is (100)

## Slide 6: Low-Temperature Anneal Dissolves Higher Oxides Into Nb(100)-O
T = 5 min
Exposure = 9 L
T = 15 min
Exposure = 27 L
T = 0 min
Exposure = 0 L
Nb(100)-O exposed to O2 at room temperature and heated to 430 oC
1 nm
1.33 nm
T = 0 min, E = 0 L
2.5-7.5 nm
T = 15 min, E = 27 L
1 nm
2 nm
Observe smaller domain sizes and increasing surface disorder
Nb(100)-O structure is significantly altered as oxygen moves from the surface into the bulk upon annealing at 430 oC

## Slide 7: Our Results Show Surface Structure Influences Communication With Bulk
Oxygen dissolving into the bulk significantly alters pre-existing surface structure
How robust is the NbO? Sputtering?
What influence do hydrides have on oxygen chemistry?
Is there saturation of the NbO surface?
Spectroscopy and kinetic studies
Specially designed instrumentation allows surface preparation and analysis from liquid helium temperatures to 1800 oC
Crystal face determines surface structure and order
NbO forms multiple structures on Nb(100)
Molecular oxygen preferentially binds on Nb atoms before NbO
Notes: Surface-bulk communication
Influence of underlying Nb structure on surface-bulk
Our Results Show Communication With Bulk Depends on Surface Structure
Crystal face affects surface ordering

## Slide 8
Summary and Plans Going Forward
Early Work: Emphasis on oxide composition and surface defects found in polycrystalline samples provided by FermiLab
XPS results show initial samples contain Nb2O5 and Nb. A robust NbO layer is formed after Ar+ ion sputtering and heating to ~520 oC , with subsequent exposure to air forming NbO2.
A polished sample imaged with SEM and AFM reveal numerous defects, including scratches and weld pits, that can influence overall cavity performance.
Current Work: Emphasis on Nb single-crystal oxidation studies
STM reveals crystal orientation affects NbO surface ordering and structure.
Nb(100)-O forms ladder-like structures that show preferential binding when exposed to molecular oxygen. Low-temperature annealing dissolves higher ordered oxides into the bulk and changes the Nb(100)-O structure.
Currently investigating oxidation kinetics and role of niobium hydrides.
Future Work: Emphasis on niobium thin films and alloys
We are presently prepared to create NbCu thin film substrates to investigate how the chemical and structural changes influence the oxidation chemistry.
We also will explore how alloys such as Nb3Sn affect the physical and chemical properties of niobium reactions.