## Slide 1
LEAP investigation of hydrogen in SRF Niobium
7th SRF Materials Workshop, JLAB Newport News, VA
July 17, 2012
Yoon-Jun Kim and David N. Seidman
Department of Materials Science and Engineering
Northwestern University, Evanston, IL
Northwestern University Center for Atom-Probe Tomography (NUCAPT)
Northwestern University, Evanston, IL

## Slide 2
Cameca (formerly Imago) LEAP 4000XSI
 Local Electrode Atom-Probe (LEAP) Tomography
V: Applied DC voltage
k: Shape dependent factor (~3.3)
R: Tip radius (usually <50 nm)
The electric field at the tip apex (E) is given by:

## Slide 3: 3-D LEAP Tomography Local Electrode Atom Probe (LEAP) Tomography
Analyze data with Cameca’s (formerly Imago) IVAS and our own programs
Can determine spatial positions of individual atoms and their chemical identities with sub-nanometer scale resolution
Analyze volumes >106 nm3
200 x 200 nm2 viewing area maximum
5 x 10-11 torr ultrahigh vacuum
Specimen T: 20 to 300 K
500 kHz electrical pulse repetition rate
1000 kHz repetition rate for a picosecond UV laser (ultraviolet (UV)) light: wavelength 355 nm

## Slide 4
Coordinates of ions (x, y, and z): permits the three-dimensional reconstruction of the lattice in real space
Times-of-flight: Mass-to-charge state ratio yields identification of the elements and their isotopes
Atomic resolution: depth resolution is equal to the interplanar {hkl} spacing (< 0.1 nm); lateral resolution is ca. 0.2 to 0.4 nm in a given {hkl} plane.
Detector efficiency: 50 – 60%. All elements across the periodic table are detected with equal efficiency by a micro-channel plate (MCP).
Atom-Probe Tomography (APT)

## Slide 5
Reconstructed Data
Needle-Shaped Specimen
Raw Data
Atom-Probe Tomography

## Slide 6
FEI Helios Nanolab
Tip sharpening done using an ion energy of 30 kV
Final stage is done using a low energy ion-beam at 2 kV in order to remove the damaged portions of the tip.
 Sample Preparation –FIB/SEM

## Slide 7
(1) Lift-out
(2) Mounting
(3) Tip-Shaping
Pt Deposition
Trench
Lift-out
Transfer
Pt Welding
Cut-off
Initial
Final
Final-High Mag
20 mm
400 nm
20 mm
20 mm
15 mm
5 mm
3 mm
3 mm
2.5 mm
 Sample Preparation –FIB/SEM

## Slide 8
LEAP analyses for two different laser pulse energies: wavelength = 355 nm (UV)
 LEAP tomography of Nb
 | Laser LEAP (High) | Laser LEAP (Low) | Voltage LEAP
Condition | RHIT:15765 (1) Pulse rate: 500 kHz (2) Pulse energy: 50 pJ (3) Temp.: 30 K (4) Evaporation rate: 0.50 -1.00 %  3M ions (Max Volt = 8 kV) | RHIT:15967 (1) Pulse rate: 250 kHz (2) Pulse energy: 10 pJ (3) Temp.: 30 K (4) Evaporation rate: 0.50 -1.00 %  2M ions (Max. Volt = 7.3 kV) | RHIT:15978 (1) Voltage Pulse rate: 100 kHz (2) Pulse amplitude: 20% (3) Temp.: 30 K (4) Evaporation rate: 0.50 -1.00 %  12M ions (Max. Volt = 7.7kV)
3-D image |  |  | 

## Slide 9
Results: 3D-reconstruction (Top-view)
Nb exhibits 100, 010, 111, and 121 type poles.
H is distributed around these poles and 3-fold symmetry is observed for111 type zone.
NbH is most pronounced around 110 type pole for 10 pJ pulses and voltage pulsing
As laser pulse energy is reduced, clear poles are observed.
As laser pulse energy is increased, more H and NbH decorate zones
 | Laser LEAP (50 pJ) | Laser LEAP (10 pJ) | Voltage LEAP
Nb+H |  |  | 
NbH |  |  | 
 LEAP - Nb
10nm
10nm
20nm
Nb
H

## Slide 10
Indexing
Differences with respect to laser pulse energy may come from
field-induced effects, such as surface diffusion of H
and field-induced (or stress induced) hydride formation
 LEAP tomography - - Nb
Nb 50%
H 50%
Voltage pulsing

## Slide 11
Atom-probe tomography can be used for the characterization of SRF-Nb cavities.
Quantitative hydrogen and niobium hydride analyses are dependent on laser
pulse energies – 50 or 10 pJ. H and NbH distributions around different zones
behave differently for different laser pulse energies.
In spite of the dependence on laser pulse energy, hydrogen is clearly observed on
specific crystallographic planes on the niobium surface.
H and NbH distributions around different zones behave differently
as a function of laser pulse energy.
Migration and desorption of H atom can be affected by the electric field or a
thermal effect (in case of UV laser pulsing) from the Nb microtips.
 Summary and conclusions

## Slide 12
This study is funded by USDOE through Fermi National Accelerator Laboratory
(FNAL).
We are grateful to Drs. Lance Cooley and Alex Romanenko in FNAL for supplying
samples and valuable discussions.
The LEAP tomographic measurements were performed at the Northwestern
University Center for Atom-Probe Tomography (NUCAPT).
The LEAP tomograph was purchased and upgraded with funding from
NSF-MRI (DMR-0420532) and ONR-DURIP (N00014-0400798, N00014-0610539,
N00014-0910781) grants.
 Acknowledgements