## Slide 1: Fabrication of Seamless Nb Tube for SRF Cavities
K.T. Hartwig1,2, S. Balachandran1, R. Elwell2, and R.E. Barber2
1Mechanical Engineering Department, Texas A&M University, College Station, Texas 77843.
2Shear Form Incorporated, Bryan, Texas 77801.
* Work supported by DOE SBIR Grant DE-SC0007601

## Slide 2
MANUFACTURING ISSUES FOR Nb SRF CAVITIES :
Tube dimensions- OD, wall thickness, and length
Non uniform deformation characteristics
  Non-uniform microstructure
  Inconsistent microstructure (Reproducibility)
Bulk Defects
Limited microstructures given fabrication constraints.
SRF2011 Hot Topic Discussion, R. L. Geng
$$$
CHALLENGING ISSUES
Notes: Fabrication and manufacturing cavities must focus on possible ways of eliminating the defects, by mechanical design of fabrication equipment and by proper microstructural control of Nb.
Seamless tubes- Eliminates equatorial welds. May reduce some Type I defects.
Singer conclusions on various approaches:
Back extrusion does not work (does not give required mechanical properties)
Spinning: Works for short tubes
Flow forming: In combination with spinning, deepdrawing, extrusion works best for DESY
Concept proven by Black Labs

## Slide 3
DEFORMATION DEPENDS ON ORIENTATION
EXAMPLE- HIGH STRAIN OF BI- CRYSTAL
AFTER A SIMPLE SHEAR OF 1.14;
EQUIVALENT ROLLING REDUCTION (67%)
B
A
B
A
Notes: This is found by equivalent work method…

## Slide 4: SEVERE PLASTIC DEFORMATION TO NORMALIZE MICROSTRUCTURE
Shear Strain per pass is 1.14
Deformation is confined to a thin region.
Rotations between passes changes the strain path leads to rapid refinement of microstructure.
High strains effectively breakdown the microstructure.
Jae- Tek, Im (PhD thesis)
Notes: Idea--Increase dislocation density to the limit. Have very high misorientation regions uniformly distributed to promote nucleation..

## Slide 5
High Angle GB’s >15o created.
HAGB’s are nucleation site for recrystallization.
Possibility of lower temperatures for full recrystallization
Z. Pan, S. N. Mathaudhu, K. T. Hartwig, Q. Wei et.al, Acta Mat, 2012.
4 pass RG Nb. Scale bar 2µm
Cell walls
Hughes, Hansen, Acta Mat, 1995
Notes: Step size is 30nm.

## Slide 6
T2
L2
25mm
25mm
IT IS HARD TO ERASE MICROSTRUCTURAL MEMORY OF Nb
Different starting microstructures, may yield different end results.
CAST RG INGOT

## Slide 7: NORMALIZED MICROSTRUCTURE AFTER SEVERAL SPD AND HT CYCLES
After a strain of 6.9 and Heat Treatment of 1250oC
400μm
After a strain of 2.3 and Heat Treatment of 1100oC

## Slide 8: AFTER A TOTAL STRAIN OF ~11 AND THREE HEAT TREATMENTS
F
L
T
Approximately 3” from front end
L2
T2
200 µm
200 µm
50 μm
50 μm
3.2 mrd
EBSD by: D. Baars, T.R. Bieler (MSU)
Total Length: 1mm
T
L
Rx=700 C

## Slide 9
BULK RRR Nb
ECAE*
GRAIN REFINED BULK Nb
AR* Extrusion
SEAMLESS TUBE
HT**
AXIS SYMMETRIC SEAMLESS TUBE
ECAE
* Area reduction
No change in shape
Grain size 10-30 µm
Weak shear textures
APPROACH WITH PROMISE
Notes: The pole figure is a {110} pf with the important fibers marked.
Extruded tubes will have a strong <110> texture in the extrusion direction .Heat treatment will reduce the intensity of this texture. However, the texture will persist. And this is not axis syymetric
SEC is needed to produce axis symmetric texture. Capability to produce equiaxed fine grain structure with low texture
Spinning of the tube also produces axis symmetric properties. From Crooks presentation, the tubes are fine grain size and low texture too.

## Slide 10: PRELIMINARY RESULTS (RRR Nb tube)
As received (Bulk)
mECAE
AR
500 µm
Rx
Rx
t=0
t= 1500µm
5mm
1 µm
500 µm
As worked seamless tube
P.J. Lee

## Slide 11
500 µm
600o C
700o C
800o C
900o C
THROUGH THICKNESS TUBE MICROSTRUCTURE: AFTER HEAT TREATMENT
Ramp Rate: 2o C/min
Soak Time: 120min
Vacuum Level: 0.2-4 x 10-6 torr
Notes: Banding observed by OM suggets difference in grain growth mechanisms, relations to texture.

## Slide 12
600oC
700oC
800oC*
Temperature (oC) | Grain Size (µm) | HV300
600 | Bi- Modal 10±3; 30±7 | 51±2
700 | Bi-Modal 12±3; 48±3 | 49±3
800 | Bi-Modal 15±6; 72±4 | 50±2
SCALE BAR 100 µm
Ramp Rate: 2o C/min
Soak Time: 120min
Vacuum Level: 0.2-4 x 10-6 torr

## Slide 13
CONTINUING WORK…
ECAE processing of seamless tubes
Bulge testing of recrystallized tubes by C. Compton to evaluate hydroformability.
EBSD charcterization of recrystallized material at MSU. Grain orientation spread data, to quantify residual strain….

## Slide 14: Questions and Discussion
Why is microstructure important?
Why is a uniform microstructure in RRR Nb difficult to achieve? How can this issue be overcome?
Is it possible to make mechanically consistent seamless RRR Nb tubes? What level of inconsistency is tolerable?
What mechanical and microstructural properties (grain size, texture) are needed for good hydroformability and how are they related to processing?
Scale up?
General criteria: High ductility, moderate- high strain hardening.
Specifics with respect to hydroforming needs to be established.
High uniform strain processing and recrystallization
Directly dependent on the homogeneity of the microstructure.
Fabrication expenses. Does microstructure influence cavity performance?

## Slide 15
Thank you for your attention
Comments and Questions…