## Slide 1: Vortex hotspots in SRF cavities
Alex Gurevich
ODU Department of Physics,
Center for Accelerator Science
7-th SRF Materials Workshop, JLab, July 16, 2012

## Slide 2: Outline
Hotspots due to trapped vortices: How do vortices get trapped in a Nb cavity?
Moving vortex hotspots by thermal gradients
Variety of different vortex configurations
Dissipation due to trapped vortices
Hotspots produced by vortex wagging tails: complicated dependence of dissipation on the mean free path, frequency and the length of vortex segments
Reconstruction of hotspot sources revealed by thermal maps

## Slide 3: Why are vortices relevant to cavities ?
Cooldown
in field from
T > Tc to 2K
Vortices can be trapped in a cavity upon cooling below Tc
Vortices trapped at the inner cavity surface oscillate
under the RF field producing hotspots
RF field
Nb
H(t)
λ
London penetration depth of
superconducting currents
≈ 40 nm << d = 3mm
Even a few trapped vortex bundles can produce RF
power comparable to the exponentially small BCS surface resistance:
Δ ≈ 17.5 K for Nb

## Slide 4: Moving vortices by thermal gradients
Thermal force acting on the vortex:
The condition: fT > Jc0 gives the critical
gradient, which depin trapped vortices:
Any change of thermal maps after applying local heaters (laser beams) indicates that hotspots are due to trapped vortices rather than fixed defects
For clean Nb with Bc1 = 0.17 T,
Jc = 1kA/cm2 and T = 2K:
|T|c = 1.6 K/mm
Experment
Ciovati and Gurevich, Phys. Rev. STAB 11, 122001 (2008);
Gigi Ciovati, this conference

## Slide 5: Parallel vortices near the oscillating surface barrier
Gurevich and Ciovati,
Phys. Rev. B 77, 104501 (2008)
Vortex viscous drag:  = 0Bc2 /ρn
Onset of vortex penetration Bv = ϕ0/4πλξ = 0.71Bc
Vortex time constant: τ = μ0λ2Bc2/Bvρn ≅ 1.6×10-12 s
for Nb3Sn, ρn = 0.2 μΩm, Bc2 = 23T, Bc = 0.54T, λ = 65 nm
Supersound initial vortex velocity v = λ/τ ≅ 400 km/s
Penetration times much shorter than the rf period (instant for the SRF cavities)
Bardeen-Stephen viscous vortex drag is inadequate for high velocities;
jump-wise instabilities (Larkin-Ovchinnikov and overheating) of vortex oscillations
x
l
ℓ
d
H0
u(t)
dm

## Slide 6: Wagging vortex tail
Vortex viscous drag coefficient
Nonlocal vortex line tension for isotropic materials
2
λ
l
H(t)
u(z,t)

## Slide 7: Dissipated power
a = ℓ/λ > 1 is the length of the vortex segment and
b = ωηℓ2/ε0 is the dimensionless frequency
Frequency
dependence
Short segments,
b << 1
Long segments, b > 1

## Slide 8: Low frequency limit
Quadratic frequency dependence
Increases as the surface gets dirtier
Increases strongly for longer vortex segments
Low frequency means f << f0 where
For a vortex segment with ℓ = 1μm
in Nb (ρ = 10 -9 Ωm), we get
f0 = 2.5 GHz
For 2GHz Nb cavities, short vortex
segments with ℓ ≲ 1 μm are in
the low-frequency limit

## Slide 9: High frequency limit, b >> 1
Independent of frequency
Independent of the length of the vortex segment
Decreases as the surface gets dirtier
Long vortex segments with ℓ ≳ 1μm
Sparsely distributed (more than ≳ 1μm apart) pinning defects
Single vortex in Nb ( = 40 nm, n = 10-8 Ohm*m, B = 0.1T, Bc2 = 0.4 T):
Q  2 W

## Slide 10: Reconstruction of thermal maps
How much RF power is dissipated in the
hotspots based on the measured
temperature distribution on the outer
cavity surface ?
General reconstruction scheme was
developed based on the solution of the
3D thermal diffusion equation:
Boundary conditions:
Separate the BCS dissipation from the
localized vortex hotspot

## Slide 11: Temperature distribution on the outer surface
Thermal decay length on the outer surface:
The hotspots which produces T – T0 = 0.1 K on the inner cavity surface at
B= 100 mT can result from q  103 – 104 vortices in a bundle
Hotspots can ignite lateral thermal quench

## Slide 12: Conclusions
Hotspots produce RF dissipation comparable to the BCS dissipation
Moving or splitting hotspots by thermal gradients (laser beam) indicates that they
result from trapped vortices rather than fixed structural defects
Vortex hotspots can be dispersed by laser but not easily eliminated
Complicated dependencies of the vortex wagging tail dissipation on the rf frequency,
mean free path and length of vortex segments:
Short segments for denser pinning centers: ℓ ≲ 1μm: Q ∝ B2ω2ℓ3 increases
as ω and ℓ increase. The cleaner the better.
Long segments for sparser pinning centers: ℓ ≳ 1μm: Q is independent of ω and ℓ.
The dirtier the better.
Reconstruction of hotspot sources from thermal maps. Thermal map microscopy.
Trapped vortex bundles can account for the hotspots observed by thermal maps