## Slide 1: Spin-forming of Seamless cavities
Enzo Palmieri
ISTITUTO NAZIONALE DI FISICA NUCLEARE
Legnro National Laboratories
and University of Padua
7th Workshop on SRF Materials, July 16-17, 2012, Jlab, Newport News VA

## Slide 2: Spin-forming of Seamless cavities
Enzo Palmieri
ISTITUTO NAZIONALE DI FISICA NUCLEARE and University of Padua
ITALY
7th SRF materials Workshop. July 16-17, jlab, -Newport News VA

## Slide 22
If we loook for a more engineerable process, seamless tubes are mandatory

## Slide 23
1. The Deepdrawing Process

## Slide 27
2. The Reversal deepdrawing

## Slide 33
3. The Flowturning Process

## Slide 42
2 Nb ninecells fabricated in 2001 for being measured at KEK

## Slide 45
Unfortunately both cavities were broken on last cell during tumbling,
then weld to a standard EB weld monocell in order to have again a 9-cell

## Slide 47
A seamless flange
Cheap alternative to welded Nb-Ti

## Slide 48
New flange design

## Slide 49
Use Kapton Joints for sealing cavities
and …
Life will never be the same!

## Slide 51
Cavities of any shape and any size

## Slide 53
6 GHz cavities
20 mm
36 mm
Seamless flanges
[mm]

## Slide 54
Low research budget  Large amount of cavities
6 GHz

## Slide 55
Mechanical
Starting internal surface conditions:
bad finishing
presence of
contaminants
Streatments:
Mechanical
SiC
ZrO2
Al2O3 + SiO2

## Slide 56
EP
Starting internal surface conditions:
bad finishing
presence of
contaminants
Streatments:
Mechanical
BCP
EP
HF, H2SO4
1:9

## Slide 57
A Mini - Chemical/Electrochemical Lab

## Slide 58
Starting internal surface conditions:
bad finishing
presence of
contaminants
Streatments:
Mechanical
BCP
EP
Thermal
Mini-Furnace: Thermal Treatments
Notes: 58

## Slide 59
Nb Sputtering
Notes: 59

## Slide 60
A dense statistics possibile
  Low cost (material, fabrication, acids, helium… )
  Easy and quick surface treatments
  High number of RF measurements per month
  Possibility to study:
        new surface treatments
          new SC materials
            new cavity shape
              new deposition tecnique (ALD … )

## Slide 62
Nb Clad Cu?
No Problem!

## Slide 70
Nb Clad Cu is a
well-established technology
Nb HIPPED Cu still
needs to be optimized

## Slide 73
The Spinning Proceedure

## Slide 75
The initial staus of the blank surfaace
must be defect and scratch free

## Slide 77
We produced calibrated holes
in a Cu blank and
we used the crack propagation mechanism in order to find out how to spin

## Slide 82
Finding the right parameters by
the Buckingham-PI Theorem
(dimentional analisys):
  D = Blank Diameter
  S= Blank thickness
  v = roller feed velocity
  = Angular velocity
  f = arc of the roller blank contact segment
Reduced parameters are: D/s; w f / v

## Slide 83
What are the advantages of Spinning?

## Slide 84
Spinning
is a
3-D forming process

## Slide 85
For a standard 2-D forming process
A 40% elongation is a limitation

## Slide 86
For Spinning
10,000% elongations are possible wihout annealing

## Slide 87
For standard 2-D forming processes,
material parameters, as:
    young Modulus
    Ductility,
    Hardness
are crucial parameters

## Slide 88
For spinning
we don’t mind!

## Slide 89
For Hydroforming,
the tube thickness uniformity is crucial
Otherwise ….

## Slide 90
For spinning we do not mind!
Tube with not uniform thickness will be re-rolled on the machine just before spinning the cavity

## Slide 91
Drawbacks of the spin-forming process:
Non-uniform wall thickness of the cavity
Need of internal grinding or tumbling
Still a manual process

## Slide 92
Q vs Eacc Results

## Slide 96
Bulk Nb cavities

## Slide 99
The best result on a LNL monocell spun cavity,
measured at KEK by Kenji SAITO

## Slide 101
Spinning is mandatory for Nb/Cu Sputtered cavities
Nb film onto hydroformed cavities does not work!

## Slide 102
Nb sputtered Cu spun cavity

## Slide 103
All last monocells reach 40 MV/m
The 3cell after only a partial grinding reached 25 MV/m

## Slide 104
Current Work:
Tube back-extrusion directly from from billets