## Slide 1: Laser heating and laser scanning microscopy of SRF cavities
G. Ciovati
7th SRF Materials Workshop, July 16th 2012
Jefferson Lab

## Slide 2: Acknowledgements
Design and fabrication of the laser scanning microscope:
  C. Baldwin, G. Cheng, R. Flood, K. Jordan, P. Kneisel, M. Morrone, G. Nemes, L. Turlington, H. Wang, K. Wilson, and S. Zhang (JLab)
  G. Nemes (ASTiGMAT)
Discussions on LSM experiments and data analysis: Steven M. Anlage (Univ. of Maryland)
Discussions on hotspot laser heating: A. Gurevich (Old Dominion Univ.)
Funding: American Recovery and Reinvestment Act (ARRA) through the US Department of Energy, Office of High Energy Physics, Contract No. DE-PS02-09ER09-05

## Slide 3: Hotspots in SRF cavities
Temperature mapping reveals that the surface resistance of SRF cavities is:
  spatially non-uniform
  the field dependence is non-linear
Hotspots

## Slide 4: Low Temperature Laser Scanning Microscopy
Nondestructive spatially resolved characterization (optical, structural and electronic properties) of HTS materials
Point-by-point raster scanning of the surface of a sample-under-test with a focused laser beam
Local heating of the SC  perturbation of its electronic system and changes in intensity and polarization of the reflected beam
Photoresponse PR(x,y)  local LSM contrast voltage dV(x,y)
A. P. Zhuravel et al., Low Temp. Phys. 32, 592 (2006)

## Slide 5: LTLSM setup for SRF cavity
Dimension are in cm
SRF cavity
Thermometry system
Mirrors’ chamber
Optics
G. Ciovati et al., Rev. Sci. Inst. 83, 034704 (2012)
71

## Slide 6: SRF cavity for LSM
18 cm
21 cm
Built from ingot Niobium
TESLA half-cell shape
TM010 mode: 1.3 GHz
TE011 mode: 3.3 GHz
H-field in TE011 mode
G = Q0Rs = 501 W
Bp/√U = 76 mT/√J

## Slide 7: Measurement setup
Assuming Rs(Tf)>>Rs(2K) and Hrf T-independent
dVrms: voltage measured with lock-in amp
V0: voltage from crystal diode with laser off
Pc0: power dissipated in the cavity with laser off
rL: laser beam radius
QL: cavity loaded Q
Qext: external Q of input and pick-up RF antenna
fM: laser modulation frequency

## Slide 8: Results: hotspot vs. coldspot
Pabs = 0.92 W, fM = 10 Hz, rL = 0.435 mm for both scans. Tin ~ 8.5 K
Temperature map of the cavity plate at Bp = 13 mT, Tb = 2.0 K

## Slide 9: Results: hotspots
Pabs = 50 mW, fM = 1 Hz, rL = 0.435 mm for both scans. Tin ~ 4 K, RBCS  3.3 mW
Temperature map of the cavity plate at Bp = 13 mT, Tb = 2.0 K

## Slide 10: Comparison with HTS setup
Thermal diffusion length
k: thermal conductivity
d: wall thickness
hK: Kapitza conductance
Thermal response time
C: specific heat per unit volume
if fMt >> 1
dT ~ 2.2 mm
t ~ 0.4 ms, up to ~ 30 ms for Tout > 2.17 K
Sample size: tens of cm
Size of apparatus: few meters
SRF Cavity: Nb, 2.0 K
HTS, 4.2 K
dT ~ 1-10 mm
t ~ 0.1-10 ms
Sample size: few mm
Size of apparatus: tens of cm
Spatial resolution =

## Slide 11: Eliminating vortex hotspots by thermal gradients
Thermal force acting on the vortex:
The condition fT > JcF0 gives the critical gradient which can depin vortices:
Taking Bc1 = 0.17T, Jc = 1kA/cm2 and T = 2 K for clean Nb yields
|T|c  1.7 K/mm
Vortices in Nb may be moved by moderate thermal gradients
Any change of thermal maps after applying local heaters indicate that some of the hot-spots are due to pinned vortices
A. Gurevich, talk TU104 at SRF’07 Workshop

## Slide 12: Laser hotspot annealing
Dissipation due to vortices // surface can be reduced by pushing them into the bulk
ANSYS thermal analysis of Nb plate with a gaussian laser beam 0.87 mm diameter, Pabs ~ 0.92 W yields T ~ 8 K/mm

## Slide 13: Experimental procedure and results
At 2.0 K:
Baseline cavity RF test: locate RF hotspots by thermometry
RF off, scan laser at hotspot locations (tried different scanning profiles: raster, spiral)
Repeat cavity RF test: locate RF hotspots by thermometry
Top view
T-map after laser heating, 82 mT
T-map before laser heating, 82 mT
Ring 2
Ring 3

## Slide 14: DT before and after laser heating
DT(Bp=82mT, Tb=2.0K) along rings 2 & 3 before and after laser heating
Top view
15°
345°
Ring 2
Ring 3
11°
349°
G. Ciovati et al., to be published
GB
GB

## Slide 15: Conclusions
A setup to perform LTLSM of an SRF cavity has been designed and built at Jefferson Lab to study “hotspots”
  3D maps of surface resistance with ~ 1 mW resolution at 3.3 GHz
  Hotspots can be identified with ~ 2 mm spatial resolution (~ 1 order of magnitude better than thermometry)
The same setup was used to attempt laser “hotspot annealing”
  Pinned vortices are a source of hotspots
  Cannot be easily “eliminated”  improve magnetic shielding of cavities in cryomodule, reduce thermal gradients of cavities in cryomodules during cool-down below Tc