## Slide 1
Using resistivity measurements to track uptake of hydrogen as a function of material working
7th SRF Materials Workshop - July 16, 2012
Alexander Dzyuba and Lance Cooley
Fermi National Accelerator Laboratory
(Superconducting Materials Department)
Superconducting Materials Department

## Slide 2
Motivation
Chart: Eacc [MV/m]
 | 8650263000 | 9256375550 | 8903361250 | 9528619650 | 9743668650 | 9904677900 | 9575599400 | 9088200900 | 8459290250 | 8047348350 | 8143010250 | 7928924000 | 6257366450 | 6393058200 | 6524034750 | 6643272150 | 6849736350 | 6910021550 | 6074833500 | 5973875800 | 5329214350 | 5522615850 | 5274306450 | 4889695900 | 4868667110 | 4443025085 | 4303659740 | 5288395800 | 4807774855 | 4307878085 | 4167605370 | 4095849905 | 4503428820 | 4021455805 | 3954048380
How this works??
  Hydrogen is loaded by EP, BCP and CMP
  Niobium hydrides could be formed during cooling down to 2K
  Hydrides are normal conducting inclusions – lossy
  Hydrides plastically deform Nb lattice – premature flux penetration?
H uptake could kill the cavity:
How much H do we load?
2) Does the cold-work enhance an uptake?
How this works??
Variation within first 100 nm of :
“hydrogen (hydrides) + oxygen+ vacancies + dislocations ”
Leads to a particular Q vs E

## Slide 3
Results. Proof of the principle
F. D. Manchester and J. M. Pitre, in Phase Diagrams of Binary Hydrogen Alloys(2000)
Chart: temperature, K
before EP
after EP
Chart: temperature, K
| 185.95000000000007 | 196.20999999999998 | 204.97 | 212.72 | 219.57 | 225.69 | 231.33 | 236.26 | 240.79 | 244.75
fitting | 0.2659 | 0.3113 | 0.3561 | 0.4011 | 0.4456 | 0.4895 | 0.5337 | 0.5757 | 0.6172 | 0.6558
experim | 0.2829 | 0.3071 | 0.3544 | 0.4024 | 0.4174 | 0.4703 | 0.4991 | 0.5887 | 0.6548 | 0.6856
ΔE~0.07eV
Resistance is meaningful to track
hydrogen upload.

## Slide 4
Results. Hydrides formation at 77K/48h
- SEM data confirms formation of large dendritic objects
(hydrides or ice?).
- These objects don’t survive under SEM

## Slide 5
Results. Samples description
16 Nb bars (2x2x75 mm3) were cutout from the sheet
Elongation in the Instron
(strain: 0%, 12%, 35%,50%)
Electropolishing
(removal: 20um, 80um, 140um,180um)
measure ρ2
measure ρ3
measure ρ1

## Slide 6
Results. H upload during EP
Both residual deformation and amount of material removal increase H concentration in the Nb.

## Slide 7
Chart: Strain, %
| 0 | 12 | 27 | 35 | 56
EP 11K | 0.01885 | 0.02325 | 0.0278 | 0.03075 | 0.0381
800C/2h 11K | 0.0206 | 0.02335 | 0.0244 | 0.02505 | 0.0285
800C/2h (2nd) 11K | 0.02265 | 0.02605 | 0.02665 | 0.0279 | 0.0316
HT bake anneals dislocations
  effect depends on the ε
HT bake dissolves oxide layer
  7nm of Nb2O5 - estimate
Chart: Strain, %
| 0 | 12 | 27 | 35 | 56
stress removal by 800C 11K | 2e-17 | 0.0026 | 0.00565 | 0.008 | 0.0127
stress creation by elongation 11K | 0 | 0.0033 | 0.0081 | 0.0105 | 0.01855
Chart: Strain, %
| 0 | 12 | 27 | 35 | 56
EP 293K | 0.00535 | 0.00585 | 0.00615 | 0.00635 | 0.00725
800C/2h 293K | 0.00535 | 0.0058 | 0.0062 | 0.00635 | 0.00725
800C/2h (2nd) 293K | 0.0054 | 0.0058 | 0.0062 | 0.00635 | 0.00725

## Slide 8
Acknowledgments:
D.Hicks, D.Ford, H.Padamsee, C.Thompson and R.Schuessler
Research is supported by Fermi Research Alliance, LLC
under Contract No. DE-AC02-07CH11359 with the United States Department of Energy

## Slide 11
150um EP
High temperature bake
20um EP
High Pressure Rinse + Alcohol rinse
(Low Temperature Bake)
Water rinse
Half cells formation/ welding
Baseline cavity processing: