## Slide 1: Recent progress with VEP at Cornell Fumio Furuta Cornell University July 17, 2012

## Slide 2: Motivation
Vertical Electro-Polishing for high gradient cavity R&D.
VEP has the Following Benefits:
  No acid circulation.
  No rotary acid seals.
  No sliding electrical contact.
  No cavity vertical/horizontal position control fixtures.
  Simplifies the acid plumbing/containment.
  Lower capital equipment cost.
7th SRFMW

## Slide 3: Parameters
Parameters | 
Cathode | aluminum >99.5%
Stir-tube | PVDF
Paddles | PVDF
Seals | FEP encapsulated O-ring
End group | PTFE, HDPE
Electrolyte | 24 liters/9-cell
Electrolyte composition | 10:1 (H2SO4: HF)
Maximum use | 9g/L dissolved Nb
Current | 150 Amperes
Voltage | 14 Volts
Temperature | 15 to 19 C
Stir-tube transparency | >50%
Stir frequency | 1 Hz
EP removal rate (ave.) | ~0.3um/min.
Stir-tube
Al-cathode
puddle
pivot
1Hz
7th SRFMW

## Slide 4
TESLA single + new EP acid bath
Re-entrant 3-cell
TESLA 9-cell
New bath is available for
All single and multi cell cavities.
Easy EP acid mixing.
EP acid circulation during VEP process.
Images
VEP set up
4
F. Furuta -Recent progress with VEP at Cornell
7th SRFMW

## Slide 5: VEP log
Voltage, Current
Temp. (cell outside)
VEP log, ACCEL9
7th SRFMW

## Slide 6: Analysis on VEP removal
Chart: removal [um]
| 20 | 4 | 30 | 10
single cell | 26.5 | 39 | 27 | 42
single cell* | 30
9-cell | 39 | 25 | 24.5841 | 22.9802 | 27.5
9-cell** | 36
Analysis on the previous VEP results at Cornell, the final VEP removal of less than 10um seems promising for high gradient ~40MV/m.
>Single cells are NR1-2, NR1-3, AES1-002, AES1-006, Re-entrant(60mm).
>9-cells are A9, A10, AES5, Re-entrant(70mm).
>Cavity treatment: Bulk VEP (140~300um) + hydrogen degas + micro VEP + 110CBake.
>Some cavities tumbled to remove defects.
>*HNO3 in electrolyte, 8ml/3.5L.
>**EP after degas was replaced by 100nm oxypolish.
7th SRFMW

## Slide 7: ACCEL9 + minimized VEP(5um)
Chart: Eacc [MV/m]
| 39.46 | 39.14 | 38.67 | 37.4 | 36.410000000000004 | 35.370000000000005 | 32.54 | 31.06 | 29.7 | 26.19 | 26.439999999999991 | 22.5 | 17.420000000000002 | 12.29 | 9.7100000000000009 | 7.3 | 5.46 | 3.79 | 2.66
VEP(5um) | 6712500000 | 6298600000 | 6416100000 | 6596100000 | 7867900000 | 9294400000 | 9099700000 | 11040000000 | 12682000000 | 12856000000 | 14359000000 | 14481000000 | 15182000000 | 14688000000 | 14143000000
re-HPR | 16251000000 | 20221000000 | 15071000000 | 16628000000 | 14125000000 | 13059000000 | 11103000000 | 10723000000 | 18202000000 | 16986000000 | 16957000000 | 15950000000 | 16326000000 | 14039000000 | 13077000000 | 12318000000 | 12408000000 | 11613000000 | 11898000000 | 10399000000 | 9425500000 | 9325500000 | 9553700000 | 9164700000
ILC BCD | 10000000000 | 8000000000
rad VEP(5um) | 34000 | 5000 | 3000 | 1300
rad re-HPR | 0.05 | 0.1 | 1
The first VEP’ed ILC 9-cell cavity achieved ILC’s BCD spec.
TESLA 9-cell, 2K
7th SRFMW

## Slide 8: ACCEL10 + minimized VEP(5um)
Chart: Eacc [MV/m]
| 4.4757176726321406 | 5.0235914762368807 | 5.7444561554718074 | 6.3668267387803965 | 7.2176338417600165 | 7.564871463156865 | 8.4101426643999737 | 9.3270288888793988 | 11.3038010575715 | 12.759228209780465 | 14.066138879502786 | 15.690604208889965 | 17.173773604837177 | 18.647963552365439 | 20.677329014077809 | 22.498136202189635 | 25.286857779630239 | 27.371127416562832 | 27.707093456346215 | 27.816818463029939 | 27.441632126919025
2012May31 | 18883599012.5864 | 19014545592.0931 | 19200154207.0768 | 19244064131.4162 | 18968367414.6943 | 19109010020.2717 | 18830316694.2619 | 18377112995.8536 | 16965850717.552 | 17216162846.0963 | 16641806757.4015 | 16011960599.7449 | 15446375981.7839 | 14961632945.1736 | 14125902171.4259 | 13345898152.9929 | 13217687374.9891 | 12784292630.3982 | 12629107493.1329 | 12697127290.4438 | 12772143710.6058
TESLA 9-cell, 2K
Eacc max =27.8MV/m, Qo =1.27e10, at 2.0K
Limited by quench, No detectable radiation.
7th SRFMW

## Slide 9: Analysis on VEP removal (2)
Chart: final removal [um]
| 4 | 30 | 10
single cell | 26.5 | 39 | 27 | 42
single cell* | 30
9-cell | 27 | 39 | 25 | 24.5841 | 22.9802 | 27.5
9-cell** | 36
>Single cells are NR1-3, AES1-002, AES1-006, Re-entrant(60mm).
>9-cells are A9, A10, AES5, Re-entrant(70mm).
>Cavity treatment: Bulk VEP (140~300um) + hydrogen degas + micro VEP + 110CBake.
>Some cavities tumbled to remove defects.
>*HNO3 in electrolyte, 8ml/3.5L.
>**EP after degas was replaced by 100nm oxypolish.
7th SRFMW

## Slide 10: Comparison w/ horizontal EP
Chart: removal [um]
| 33 | 43 | 43 | 80 | 80 | 80 | 80 | 80 | 83 | 83 | 83 | 83 | 83 | 83
first EP | 41.5 | 45.01 | 49.2 | 45.1 | 44.2 | 48.8 | 42 | 46.1 | 44.73 | 34.25 | 39.3
additional EP | 39.3 | 39.4 | 41.13 | 41 | 40.21 | 42.68 | 52.3 | 52.24 | 50.13 | 52.91 | 52.16 | 34.09 | 48.9 | 43.35 | 40 | 46.5 | 38.41 | 47.07 | 42 | 44.67 | 47.82 | 43.93 | 53.49
*All cavity was processed by KEK’s CBP.
*Quench limitation only.
KEK low loss single cell + horizontal EP.
7th SRFMW

## Slide 11: VEP’ed 9-cell status
Chart: Eacc [MV/m]
| 4.0999999999999996 | 4.83 | 5.95 | 8.27 | 12.16 | 18.47 | 28.87 | 38.020000000000003 | 6.58 | 7.81 | 9.4600000000000026 | 11.370000000000006 | 14.68 | 17.37 | 20.65000000000002 | 25.86 | 23.08 | 27.959999999999987 | 30.93 | 32.410000000000004 | 33.980000000000004 | 37.260000000000012 | 37.58 | 38.090000000000003
ACCEL9 | 16251000000 | 20221000000 | 15071000000 | 16628000000 | 14125000000 | 13059000000 | 11103000000 | 10723000000 | 18202000000 | 16986000000 | 16957000000 | 15950000000 | 16326000000 | 14039000000 | 13077000000 | 12318000000 | 12408000000 | 11613000000 | 11898000000 | 10399000000 | 9425500000 | 9325500000 | 9553700000 | 9164700000
ACCEL10 | 18883599012.5864 | 19014545592.0931 | 19200154207.0768 | 19244064131.4162 | 18968367414.6943 | 19109010020.2717 | 18830316694.2619 | 18377112995.8536 | 16965850717.552 | 17216162846.0963 | 16641806757.4015 | 16011960599.7449 | 15446375981.7839 | 14961632945.1736 | 14125902171.4259 | 13345898152.9929 | 13217687374.9891 | 12784292630.3982 | 12629107493.1329 | 12697127290.4438 | 12772143710.6058
AES5 | 14135093266.5185 | 14420972716.0688 | 14350491508.7818 | 14483302133.9166 | 14204011838.8832 | 14019003920.4169 | 13618841387.8579 | 12881243026.3722 | 11898318956.4256 | 11502889927.1179 | 10865840584.9592 | 10354715322.4355 | 9890802851.5218 | 9495751470.6576 | 9120265272.9961 | 8446178008.1127 | 8000453682.5818 | 8415203849.8148
LR9-1 | 16174150064.7575 | 15857288816.8872 | 15800692393.4655 | 15686470520.7417 | 15310269562.4547 | 15147260959.4147 | 14890866965.8777 | 14742441485.1206 | 14464085518.7155 | 14165751862.3202 | 13853922939.2401 | 13514755964.2809 | 13038420740.7052 | 12788483760.0539 | 12204037203.7259 | 11625686011.1456 | 11011525074.1544 | 9962103394.7527 | 9391576201.7385
7th SRFMW

## Slide 12
Fumio 23Jan12
F. Furuta -Recent progress with VEP at Cornell
12
We have successfully demonstrated capability of VEP for high gradient ~40MV/m with TESLA 9-cell cavity.
Minimizing final VEP removal is key to success.
Next step are
  Reproducibility & yield test.
  Improve Qo curve more flat.
  Cavity shape dependence (Re-entrant, KEK Low Loss).
  Understanding and optimization of VEP process.
  R&D on mirror-like finish CBP + VEP.
  R&D on coin sample cavity.
Summary
7th SRFMW