## Slide 1: Landscape for SRF Thin Films
Larry Phillips
July 18, 2012

## Slide 2: WHY THIN FILMS
Cost is the only driver
Lower cost enables many new applications
Future applications of SRF linacs for which cost is a driver: ILC, or LEP3, ADS, medical, light sources, ….
Of these, an ADS proton linac is most fascinating; it will be the first major industrial accelerator market in the world, giving potential companies two valuable opportunities:
  They will see a large ongoing market
  They can not only own the technology, but own as well their own internal resources for innovation to compete in that market.

## Slide 3: WHY DO THIN FILMS LOWER COST?
- Thin film niobium cavity substrates are of highly formable metals, such as copper or aluminum.
- Enables integration of many system functions in a single low-cost structure, i.e. an aluminum casting.
- Integrated functions:
  Cavity RF surface definition
  High thermal conductivity substrate
  Helium vessel
  Cryogenic manifold with heat exchanger
  Cavity stiffening, and many more……….

## Slide 4: CAST CAVITY IMPLICATIONS
High precision and stability compared to sheet metal
Field flatness and cell alignment built in.
No variation in cavity length from field flatness tuning
Very small tuning range required (small local perturbation or reactive tuner)
Not sensitive to helium pressure variations
Insensitive to Lorentz force detuning

## Slide 5: CAST CAVITY IMPLICATIONS cont.
No microphonics
No financial and environmental cost burden from acids
Lower RF power consumption–no need for microphonic head room.

## Slide 6
Where are we on the road to high quality thin film cavities?
  - What went wrong in the past? Why Q-drop?
- What were the visible differences between bulk niobium and niobium made with conventional magnetron sputtering?
- The only visible differences were loose, voided surface structure and low RRR, which were well known features of magnetron sputtering of high melting point metals. But this was all that was available at the time.

## Slide 7
It was known that a low RRR value could lead to a reduction in Hc1 and explain some if not all of the Q-drop.
Hc1 = 2 Hc (ln  + 0.5)

=  1 = 1 + 1
  0 L
Suppressed Hc1 is compounded further by localized features, such as voids and heavily oxidized surface fissures. This drives Hc1 lower at these spots sometimes causing thermally stabilized regions of normal niobium (after Knobloch) adding additional nonlinearity.
The Q-drop in LEP films do not follow the temperature dependence expected for Hc1, probably for many reasons.

## Slide 8
At JLab a new effort was launched with two main features:
    1. A new niobium deposition process was developed using “energetic condensation” with a niobium ECR plasma in vacuum. (Thesis of Genfa Wu)
    2. The process would be developed using small samples by correlating:
        Deposition parameters
        Film microstructure
        SRF performance
A great value was placed on the development of an understanding before trying to make cavities.

## Slide 9
III. Where things are today.
After much work, how do films made by “energetic condensation” and magnetron sputtering compare today?
A. Conventional Magnetron Sputtering
    10 <RRR<25
    Surface voids are sources of B field enhancement.

## Slide 10
  B. Energetic Condensation
      An extensive map of deposition parameters, film structure, substrate temperature, and RRR has been developed
      Films made today having 200 <RRR <400 can be made repetitively on many substrate materials, including copper
      Smooth, dense films are obtained
      This effort has been highly successful!!!!!!
  If the depression of Hc1 and field enhancement by surface features were dominating Q drop, these problems are solved.
  But what else might be there?

## Slide 11
IV. Unknown Problems
    In addition to the known problems with conventional magnetron sputtering, are there any hidden causes of Q-drop waiting to be discovered? and what might they be?
    RF residual resistance- not understood
      Few measurements exist on energetically condensed films—not yet conclusive—more to come.
    SRF surface and copper substrate are only ~1 micron apart separated by straight grain boundaries along columnar films.

## Slide 12
Unknown Problems – cont.
    Diffusion within grain boundaries can be 104 – 105 higher than surface diffusion. Typical substrate temperatures for copper are Ts/Tm~0.5
    Surface oxidation—unknown effect on niobium films.
    Easy solutions to known “Unknown Problems”
      Diffusion barrier between substrate and film
      Dielectric diffusion barrier on RF surface, or plasma oxidized Nb2 05 –no sub oxides.

## Slide 13
Three Future Tasks
    Understand the physics of residual RF surface impedance and its dependence on deposition parameters for thin Nb films
    Refine small sample Rs measuring process. The development of both niobium films and ML films will depend on this. A higher rate of sample testing is needed. The calorimetric cavity process with high resolution are especially valuable for RF residual resistivity studies.

## Slide 14
    3. Fiber growth films
    - In recent years much attention has been given to hetero epitaxial growth modes. This makes sense since there is much to learn quickly about the effect of deposition parameters on crystal quality, for instance, by growing large crystals on well- characterized substrates.
    Fiber growth is the default mode when depositing on an amorphous surface. Grains having crystal planes with the lowest surface energy exposed to the incident flux will grow faster and “pinch out” competing grains, resulting in grain diameters of fixed column size after the competition is complete.

## Slide 15
To use this growth mode, the average grain diameter at the RF surface much be large enough that Hc1 is not affected by grain boundary scattering.
  - Why bother?
  - From a manufacturing point of view this, would be the simplest and least critical process, given the caveat of grain size.
- the only starting surface requirement is that it be clean and smooth.
  - initial “ion stitching” increases shear strength at the substrate interface and allows a greater film thickness.
  - An extra thick amorphous layer at substrate provides a diffusion barrier for free and more.

## Slide 16: CONCLUSIONS
High quality niobium films can be produced using energetic condensation techniques
Thin film cavity/linac structures have very large cost reduction potential over conventional bulk niobium structures
Such low structure costs will drive the economic optimum to lower real estate gradients and lower volt per dollar values
Thank you on behalf of the JLAB thin film group.