## Slide 1: Nb Coatings for SRF Cavities Produced by High Power Impulse Magnetron Sputtering
Rueben J. Mendelsberg1,2,
Alex Dzyuba3, Joe Wallig1, Lance Cooley3, André Anders1, Thomas Proslier2, and many others

## Slide 2
High Power Impulse Magnetron Sputtering
Ionize the Sputtered Atoms!!!!!!!!
V. Kouznetsov, et al., Surf. Coat. Technol. 122, 290-293 (1999)
500 kW Peak Power
Cu target in 65 mPa Ar
300-550 W/cm2
21-25 W/cm2
J. Vlcek, A. D. Pajdarova, and J. Musil, Contrib. Plasma Phys. 44, 426 (2004)
“HIPIMS is pulsed sputtering where the peak power exceeds the average power by typically two orders of magnitude.”

## Slide 3: Dual HiPIMS of Nb at LBNL
4000 μF
± 750 V
± 200 A
4000 μF
± 750 V
± 200 A
+
-
+
-

## Slide 4: Dual HiPIMS of Nb at LBNL
4000 μF
± 1000 V
± 200 A
4000 μF
± 1000 V
± 200 A
+
-
+
-

## Slide 5: Dual HiPIMS of Nb at LBNL
4000 μF
± 1000 V
± 200 A
4000 μF
± 1000 V
± 200 A
+
-
+
-
4000 μF
± 1000 V
± 200 A
4000 μF
± 1000 V
± 200 A
+
-
+
-

## Slide 11
1050 K !!!

## Slide 12: Power Balance

## Slide 13: Power Balance

## Slide 14: 10 ns Framing Camera Images
3” Planar Magnetron
Cylindrical Magnetrons
Linear Color Scale
Logarithmic Color Scale

## Slide 15: Extended Mechanical Polishing
115 RPM
R&D led by Dr. Charlie Cooper, FNAL

## Slide 16: Extended Mechanical Polishing
Step 1
Step 2
Step 3
Step 5
Step 4
+ Soap & Water
+ Soap & Water
20 μm Alumina and Water
Chemical Buffer Polish
(0.05 µm)
Colloidal Silica
Micro-machining
De-laminating
Grinding
10 μm Alumina and Water

## Slide 17
Courtesy C. Cooper, TTC Milan slides
Ra = 0.014 µm +/- 0.002 µm
Rz = 0.014 µm +/- 0.002 µm
1 mm x 1 mm:

## Slide 18: EMP Cu and Al Substrates
Before Polishing
After Polishing
Before Polishing
After Polishing
Focused on Surface
Focused on Reflection

## Slide 19: Extended Mechanical Polishing
0 μm
0
2.1 μm
100 μm
200 μm
100 μm
200 μm
2.1 μm
0 μm
2.4 μm
100 μm
200 μm
200 μm
2.4 μm
0
Copper
Aluminum

## Slide 20
Electrically Isolated Substrate Heater (9” x 3”) for up to 750 °C

## Slide 21: Optical Microscopy
0 μm
0 μm
500 μm
700 μm
3.4 μm
3.4 μm
Nb on Cu
100 μm

## Slide 22
SEM
5 μm
Copper
Aluminum

## Slide 23
Nb / Cu
Nb / Al
SEM
5 μm

## Slide 24
Nb / Sapphire
SEM

## Slide 25: Superconductivity

## Slide 26: XRD
Cu (111)
Cu (200)
Cu (200)
Nb (110)
Nb (211)
Al (111)
Al (200)
Nb (110)
Al (220)

## Slide 27: Ion Beam Analysis
Al
Si
Nb
Ar
K
Ca
Sc
Ti
Cr
Fe
Cu
Cu
Nb

## Slide 28: The Next Steps
x 10 or more
More Advanced Pulse Patterns

## Slide 29: Acknowledgements
MOLECULAR
FOUNDRY
Kin Man Yu
Delia Milliron
Nick Groll
Alex Nollau
Arno Godeke
Matthijs Mentink
Lots of others