## Slide 1: JLab infusion and LG flux expulsion update
Pashupati Dhakal
09/08/2017
Notes: Title Page

## Slide 2: N-Infusion Update
High purity fine grain Nb Cavity RDL-02: After the fabrication, the cavity was given standard ILC recipe of 150 mm EP, 800 C/2hrs furnace treatment, followed by 20 mm EP.
Cavity was HPR before loading to the furnace and Nb caps were assembled in clean room.
After each heat treatments (with caps), the baseline measurement was done to surface reset with 10 mm EP.
Rs vs T data were taken from 4.3-1.5K at Bp~10mT in order to extract the material parameters.
No post chemistry after the furnace treatment.
Correction to earlier report: N2 gas was injected into the furnace ~280-290 C (unintentional)
Notes: Interior Page Design 1

## Slide 3: RECENT WORK AT JLAB
Standard ILC EP recipe
Notes: Interior Page Design 1

## Slide 4: RECENT WORK AT JLAB
Standard ILC EP recipe with Bake
Notes: Interior Page Design 1

## Slide 5: RECENT WORK AT JLAB
Notes: Interior Page Design 1

## Slide 6: RECENT WORK AT JLAB
Notes: Interior Page Design 1

## Slide 7: RECENT WORK AT JLAB
Notes: Interior Page Design 1

## Slide 8: RECENT WORK AT JLAB
Work in Large grain cavities as well as process control are in progress.
Notes: Interior Page Design 1

## Slide 9: Sample Coupons Study
800°C
800°C+ N2@120°C
800°C+ N2@140°C
800°C+ N2@160°C
The material looks non-uniform. Grain sizes vary between 10-70µm
FSU/ASC
Notes: Interior Page Design 1

## Slide 10: Sample Coupons Study
800°C
800°C+ N2@120°C
800°C+ N2@140°C
800°C+ N2@160°C
Granular surface morphology on low temperature N doped samples
FSU/ASC
Notes: Interior Page Design 1

## Slide 11: Sample Coupons Study
Preliminary XPS Result: Presence of a NbNO peak in low temperature N doped sample
FSU/ASC
Notes: Interior Page Design 1

## Slide 12: Sample Coupons Study
Nb2O5
NbN(1-x)Ox
204.3
800°C+N2@160°C
(F12)
Nb2O5
NbOx/Nb
202.3
800°C /3h (F9)
NbN(1-x)Ox
Nb2O5
NbOx
Nb
Bulk
Nb
Nb2O5
Bulk
FSU/ASC
Nb2O5, and NbN(1-y)Oy exists within first 10nm in low temperature N infused sample
Notes: Interior Page Design 1

## Slide 13: Magnetization/AC Sussceptility
Surface effect with N-infusion

## Slide 14: SIMS
One sample shower higher C content, may have segregated C
Oxygen profile consistence with earlier studies of LTB
Higher N concentration for 140 and 160C/48hrs treatments.

## Slide 15: Sample Coupons Study
Q-slope
High Eacc
High Rres
High Q
WHY?
The lower residual resistance can be achieved by reducing the thickness of normal layer thickness and also the normal-superconducting interface resistance. Kubo & Gurevich, SRF2017

## Slide 16: Conclusions
Nitrogen Infusion at low temperature works and can be ideal processing recipe to achieve high Q, high gradient cavities.
Low temperature N-doping of Nb affects the surface properties significantly
  Increase in Hc3 value, an indication of reduced electron mean free path on surface.
  Different baking temperature in N2 atmosphere leads to different surface condition.
  Preliminary XPS on low temperature nitrogen infused sample shows a presence of NbN(1-y)Oy and a protective Nb2O5 within the first 10nm. The presence of other sub-oxides cannot be ruled out. XPS analysis is in progress.
But the bulk properties remains unaffected
  Tc is unchanged
  Number of pinning sites (evident from magnetization loop) are almost same. The effect is different from high temperature N-doping.
  Sample study shows higher flux trapping efficiency, similar to conventional nitrogen doping.
Notes: Interior Page Design 1

## Slide 17: Flux Expulsion on LG cavities
Where does the flux trap? Surface or bulk?
RF only sees the surface flux trapping where as flux expulsion is bulk effect.
We measure the flux expulsion and flux trapping studies on LG cavities with different impurities in order to see the correlation of purity (bulk RRR) and surface preparations (EP, LTB and N-doping)

## Slide 18: Flux Expulsion on LG cavities

## Slide 19: Flux Expulsion on LG cavities Surface (EP)
RRR = 60
RRR = 107
RRR = 486
Cavity | DT>4K(Bsc/Bn ~ 1.5) dRres/dBa nW/mG | DT<0.1K(Bsc/Bn ~ 1) dRres/dBa nW/mG
TC1N1 (RRR=60) | 0.13 ±0.01 | 0.51 ±0.02
KEK-R5 (RRR=107) | 0.10 ±0.02 | 0.28 ±0.04
G2 (RRR=486) | 0.11 ±0.01 | 0.57 ±0.02

## Slide 20: Cavity G2 (EP vs N-doped)
Cavity | DT>4K (Bsc/Bn ~ 1.5) dRres/dBa nW/mG | DT<0.1K(Bsc/Bn ~ 1) dRress/dBa nW/mG
G2 (EP) | 0.11 ±0.01 | 0.57 ±0.02
G2 (EP+N2-7umEP) | 0.13 ±0.01 | 1.06 ±0.03

## Slide 21: KEK-R5 (EP vs LTB 120/24hrs)
Cavity | DT>4K (Bsc/Bn ~ 1.5) dRres/dBa nW/mG | DT<0.1K(Bsc/Bn ~ 1) dRress/dBa nW/mG
KEK-R5 (EP) | 0.10 ±0.02 | 0.28 ±0.04
KEK-R5 (EP+LTB) | 0.10 ±0.01 | 0.41 ±0.03
Increase due to LTB

## Slide 22
DT <0.1K
DT >4 K

## Slide 23
Eacc = 36 MV/m, Q0 = 2x1010

## Slide 24: Summary
Good flux expulsion (DT>4K) regardless of RRR
dRres/dBa ~ 0.1-0.13 nW/mG, regardless of RRR and surface preparations as long as DT > 4K.
The trapping sensitivity increase from 0.57 to 1.06 nW/mG (about a factor of 2) in N-doped cavity made from high purity LG niobium
The trapping sensitivity increase from 0.28 to 0.41 nW/mG due to LTB in cavity made from medium purity Nb.
May help to understand the bulk/surface pinning effect on Rres.
More details analysis to follow…..