## Slide 1: Update on Cornell Low Temperature Doping Studies
P. N. Koufalis
Cornell University

## Slide 2
Low temperature baking (120 – 160 oC) in a low pressure nitrogen atmosphere results in ‘Q-rise’ and higher low-field Q0 values
  A . Grassellino et al., Unprecedented Quality Factors at Accelerating Gradients up to 45 MV/m in Niobium Superconducting Resonators via Low Temperature Nitrogen Infusion. arXiv:1701.06077.
  P. N. Koufalis, D. L. Hall, M. Liepe, J. T. Maniscalco. Effects of Interstitial Oxygen and Carbon on Niobium Superconducting Cavities. arXiv:161208291.
Nitrogen diffuses only 2 – 5 nm into niobium at these temperatures
Observed that carbon and oxygen diffuse significantly into niobium at 160 oC
Introduction

## Slide 3
anti-Q-slope
higher Q0
160 oC
low T dope
800 oC
high T dope
low T bake profile
Continuously flowing N2 atmosphere
Max Quality Factor:
Q0 = 3.6 × 1010 @ 16 MV/m
Thermal Quench:
25 MV/m (Bpk ~ 107 mT)
RF Performance

## Slide 4
Field Dependence of
RBCS decreases with increasing Eacc; same effect seen in high-T nitrogen-doped cavities (caused by reduction of mean free path!)
Which impurity is reducing the mean free path?
Low T Dope
High T Dope

## Slide 5
RF layer (~)
Oxide layer (~5 nm)
160 oC
low T dope
Carbon and oxygen concentrations two orders of magnitude higher than nitrogen in RF layer
SIMS Analysis

## Slide 6
RF layer (~)
Oxide layer (~5 nm)
160 oC
low T dope
Carbon and oxygen concentrations two orders of magnitude higher than nitrogen in RF layer
SIMS Analysis
Typical concentration between – cm-3 or (0.09 – 0.36 at. % N) for 800 oC N-doped cavities
Typical 800 oC N dope

## Slide 7
Other Impurities:
C and O

## Slide 8
Ultra High Purity Argon (99.999 %)
Research Plus Argon (99.9999 %)
The purity of gas used has a high impact on the impurity concentration! The argon with higher trace impurities leads to a higher concentration in the RF layer.
Gas Purity

## Slide 9
The research plus argon mixed with 10 ppm CO2 significantly increases the concentration of carbon in the niobium! Trace impurities in the gas play important role.
Research Plus Argon (99.9999 %)
Research Plus Argon + 10 ppm CO2
(99.9999 %)

## Slide 10
Depth dependence of mean free path is given by the relation to the impurity concentration
Mean free path changes rapidly with increasing depth then levels off throughout the penetration depth
and are constants that depend on impurity species and is the impurity concentration

## Slide 11
Argon-Carbon Dioxide Bakes
Initial performance is very poor with both a strong Q-slope, low Q, and small quench field
After HF rinsing, anti-Q-slope becomes apparent and Q rises significantly!
  lossy oxide layer?
Oxypolishing after the bake results in a strong Q-slope but overall higher Q than the cavity with no post-bake etching
LTE1-1
LTE1-2
LTE1-2

## Slide 12
BCS Resistance
HF Rinse
Oxypolish
shown at 2.0 K!
anti-Q-slope
anti-Q-slope
Anti-Q-slope in after HF rinse due to decrease in
Decrease in w/ oxypolishing but curve has different shape
Linear dependence of on looks similar to Nb3Sn

## Slide 13
Material Properties
Low T dope
High T N doped

## Slide 14
Baking in CO2-rich Ar atmosphere at low results in high impurity concentrations of C and O
Mean free path dramatically reduced in the RF penetration layer but quickly reduces to the clean limit as you go deeper into the material
Lossy oxide layer seems to be cause of low Q
  HF rinsing restores Q and reveals anti-Q-slope!
Oxypolishing dramatically changes behavior of the surface resistance
  Why?
  Residual resistance increases linearly with RF field; also seen in Nb3Sn cavities
  Need more data with various amounts of etching to see how the surface resistance evolves
Concluding Remarks