## Slide 1: High current polarized electron sources
Luca Cultrera

## Slide 2: Outline
Spin polarized photocathode requirements
  eRHIC and Linac Ring option;
Non-Exaustive state-of-the-art of GaAs-based photocathodes;
Photocathode R&D at Cornell University
Cs2Te activated GaAs;
New venues for improving polarized sources;

## Slide 3: eRHIC and the linac ring option
The linac-ring option needed polarized electron beam with average currents up to 50 mA.
Electron sources was based on III-V semiconductors photocathodes materials that cannot sustain that average current for longer than few minutes.
Limited effort to address the actual challenge of improving the polarized photocathodes using new classes of materials and/or activation strategies
GaAs @ 532 nm (~5 Watts)
200 Coulomb
B. Dunham et al, Appl. Phys. Lett. 102, 034105 (2013)
QE ~ 2%
QE ~ 10%

## Slide 4: Existing photocathodes
All these photocathodes requires Cs-O activation to achieve Negative Electron Affinity (NEA) and vacuum levels better than 10-11 Torr to survive a few days (without even running the beam)
At 1.6% QE the required laser power “on the cathode” @800 nm to generate 50 mA is about 5 Watts

## Slide 5: State-of-the-art of polarized electron sources
Superlattices are the best choice
Parameter | Value | Value
Laser Rep Rate | 499 MHz | 1500 MHz
Laser Pulse Length | 30 ps | 50 ps
Laser Wavelength | 780 nm | 780 nm
Laser Spot Size | 0.45 mm | 0.35 mm
Photocathode | GaAs/GaAsP | GaAs/GaAsP
Gun Voltage | 100 kV | 200 kV
Beam Current | 1 mA | 4 mA
Run Duration | 8.25 hr | 1.4 hr
Extracted Charge | 30.3 C | 20 C
Charge Lifetime | 210 C | 80 C
Fluence Lifetime | 132 kC/cm2 | 83 kC/cm2
Bunch Charge | 2.0 pC | 2.7 pC
Peak Current | 67 mA | 53 mA
Peak Current Density | 42 A/cm2 | 55 A/cm2
J. Grames et al., PAC07, THPMS064
QE(q) = QE0 e–(q / 80)
R. Suleiman et al., PAC11, WEODS3
Up to 4 mA of polarized e-beam
Lifetime limited to few hours

## Slide 6: Distributed Bragg Reflector
Total laser absorption in the SL layer is usually <5%
A DBR can be used to reflect the unused laser beam back to the SL
QE is now a factor 6 larger
Potential for higher currents
Less laser power, less heat to dissipate
Quite complex structure

## Slide 7: But QE alone is not sufficient
NEA is achieved and can be maintained only in extreme vacuum
  XHV require massive pumping to reach 10-12 Torr;
Ions backstreaming is still limiting operating lifetime
  Clearing electrodes and or biased anode;
  Higher gun voltages;
At 350kV, only <50% of ions are created compared to 130kV
I=2.0 mA, P=8.0 × 10-12 Torr
A single HV breakdown event inside the gun
Can get the vacuum high enough to instantly
“kill” the cathode
Courtesy of J. Grames

## Slide 8: ERL R&D aimed at high average currents
L. Cultrera et al., Physical Review ST- Accelerators and Beams 14 (2011) 120101
B. Dunham, et al., Appl. Phys. Lett. 102 (2013) 034105
L. Cultrera et al, Appl. Phys. Lett. 103 (2013) 103504
20
40
60
80
100
Up 75 mA (held for a few minutes)
CsK2Sb
CsK2Sb
Cs3Sb
Na2KSb
The Cornell ERL injector prototype has demonstrated the highest levels of average current
But also GaAs, GaAsP, GaN…

## Slide 9
Na2KSb: 24 hours long run…
These results were possible because we choose
investing in experimenting with cathode materials….
Time (hours)
> 2600 Coulombs

## Slide 10: Alternatives to Cs-O for NEA
There are alternative ways for generating the NEA on GaAs that are less sensitive to vacuum conditions?
Df=(24.8-21.7)= 3.1eV
H. Sugiyama et al , J. Phys. Conf. Series 298 012014 (2011)
M. Kuriki, P3 workshop, LBNL, 2014

## Slide 11: Cs2Te over GaAs can yield NEA!!
Cs2Te is used in many RF gun (FLASH, DESY, LBNL…)
Promises:
  Operating gun at higher voltages;
  Operation in RF (and SRF) guns;
  Long term cathodes storage;
  Cathodes transport in suitcases;
Will the Cs2Te layer preserve the spin polarization during the electron transport?

## Slide 12: Mott polarimeter @SLAC
Electrostatic bend
Mott target and detectors
Cesiation Chamber
Electrostatic lens
distributer
Channeltrons HV
and counters
Electrostatic lens
Power supply
Detector threshold HV
SLAC => Jlab => Cornell University
In 1993!!

## Slide 13: Photocathode Lab

## Slide 14: Mott polarimeter @ CU
The retarding field Mott polarimeter has been refurbished upgraded and fully integrated into the photocathode lab UHV installation.
Vacuum level is below 10-10 Torr
Bulk GaAs cathode
Electrostatic bend
Mott target and detectors
Thanks to M. Poelker and M. Stuzman for helping in debugging and setting up the polarimeter

## Slide 15: Cs2Te on GaAs
GaAs substrate samples p-type Zn doped 1e18 cm-3
Wet etch to remove oxide and passivate surface
-H2SO4:H2O2:H2O (20:1:1) 2 min @ RT
-HCl:iPA (20:80) 3 min @ RT
Heat cleaning at 400 C overnight
Room Temperature Cs activation yields ~3% QE @ 532nm
Surface is clean enough to perform NEA activation!!
We also used H3PO4 and HF to remove the oxides with HF giving the best results in terms of QE
Rough surface
Many pits

## Slide 16: Growth Cs2Te on GaAs
Cs
Te
Cs
Cs+Te
Cs
~1 nm of Te => ~2 nm Cs2Te

## Slide 17: Cs2Te on GaAs
Auger spectroscopy confirms the presence of Cs and Te over the GaAs surface
Ga ans As peaks are still visible meaning that the CsTe layer is thinner than few nm
C and O peaks likely coming from the e-gun
We do NOT see an emission threshold shift
Partial coverage of the surface?

## Slide 18: Cs2Te on GaAs
Beam energy in our setup is about 40 eV
Beam energy in PES gun
About 3 order of magnitude larger probability to ionize hydrogen than in a real gun
Due to low energy electron the ion back bombardment damage is likely to affect the very surface of our samples.
Why the re-cesiated samples have a lower lifetime than the as-grown samples?
Could it be because the Cs stays only at the surface?
@532 nm
5X LIFETIME!

## Slide 19: Electron beam polarization
The same GaAs wafer was activated first with Cs-O and later with Cs2Te
Spin polarization is not affected by the Cs2Te surface layer

## Slide 20: 3 weeks ago…
QEs are not that exciting
(we believed the wet etch with H3PO4 was not effective)
but anyway this new coating shows 30x lifetime w.r.t. Cs-O
We attempted achieving NEA with a new material
(considering patenting the method)

## Slide 21: Last week results
LIFETIME UNDER SIMILAR CONDITION IS MEASURED TO BE ABOUT 80x LONGER
Polarization will be measured soon
(but, as for Cs2Te, we do not anticipate issues)
We used HF based wet etching
and 600 C heat clean cycle to fully remove oxides from GaAs surface
5% @ 532nm
2% @ 780nm
0.15 C
0.0093 C
0.0019 C
~20 nm thin coating

## Slide 22: Polarization in few days
The polarimeter is currently being baked
Upgraded with a cryogenic sample holder
Improve the beam spin polarization by mitigating the relaxation rates as function of temperature
W. Liu et al., APPLIED PHYSICS LETTERS 109, 252104 (2016)

## Slide 23: In the near future
We plan to perform test in our 400 kV gun in 2019
Aiming at demonstrating high average current levels and measuring lifetime

## Slide 24: Conclusions
Robust PES capable of high currents:
  most relevant for LR-eRHIC;
  Longer operational lifetime;
  Other application (…polarized positrons);
PES still based on III-Vs semiconductor:
  Robust NEA activation can yield almost two orders of magnitude longer lifetime;
  Polarization measurement in few days;
  Lifetime measurement in the gun in few months;

## Slide 25
Thank you for the attention!!
Acknowledgements to:
NP-DOE (DE-SC0016203 and DE-SC0019122)
NSF (PHY-1461111)
and collaborators:
Ivan Bazarov (PI),
Jai Kwan Bae (graduate student),
And the photocathode development group at CLASSE

## Slide 26
~10 mA
2 hours
No RF trips
~20 mA
2 hours
many RF trips
Central damaged area
Alkali antimonides ion back bombardment
Fresh cathode
Stay away from the electrostatic center!

## Slide 27: Nitrides
453 nm
785 nm
Electron beam polarization is only 0.13%
Expected result because the GaN had hcp rather than cubic structure
Air stable NEA without Cs !!
simulation
results
Band bending

## Slide 28: Alternative approaches
Are III-Vs our only option to generate intense spin polarized photo-currents?
Half-metal can be resourceful!
Electronic band structure depends on spin polarization
Polarization up to 100% are possible
Within the conduction band
Let see a few examples….

## Slide 29: CrO2
Stable material
Lowest workfunction is 3.4eV
Require UV light
Up to 4.4 eV photon energy only one spin can be photoexcited => 100% polarization
f
Ef
Kamper et al, PRL 59, 2788 (1987)
Mustonen et al, PRB 93, 014405(2016)
Attema et al, PRB 77, 165109 (2008)

## Slide 30: Spin filters
Cu
Cu
EuO
Jutong et al, PRB 86, 205310 (2012)
Spin dependent barrier below Tc

## Slide 31: Can we make real electron beams?
Field emission experiment W/EuS date back in 1972
Required operation at cryo-temperatures to get EuS<Tc
Polarization of 89±7 % was measured at 21K
Muller et al, PRL 29, 1651 (1972)