## Slide 1: Nonlinear RF losses of a trapped vortex in different pinning landscapes under strong RF field in a superconducting film
Old Dominion University
Department of Physics and Center for Accelerator Science
Norfolk VA 23529, USA
W.P. Manula Pathirana
Alex Gurevich
Supported by NSF under Grants No. PHY 1632749 and PHY 1734075,
and by DOE under Grant No. DE-SC0010081.
15th March 2021

## Slide 2: Outline
We report extensive numerical simulations of the nonlinear dynamics and losses of a trapped elastic vortex under strong RF field.
We took into account:
  Vortex line tension,
  Vortex mass,
  Bardeen-Stephen, and Larkin-Ovchinnikov (LO) viscous drag coefficients,
  Different distribution of pinning centers.
At low field, the surface resistance can increase linearly with H
We show that the LO decrease of viscous drag coefficient with vortex velocity results in a vortex residual resistance Ri(H) which decreases with H at higher fields and frequencies.
The Joule overheating can mask the LO decrease of Ri(H).
Opportunities to investigate extreme nonlinear dynamics of vortices. Heating is much weaker than in pulse flux flow measurements.

## Slide 3: Goals
y(x,t)
z(x,t)
Lω
Decay length of oscillating bending disturbance along the vortex line
We want to understand the behavior of field-dependent residual resistance Ri(H) as functions of:
RF field amplitude
Frequency
Volume density of pinning centers
Strength and statistical distributions of pinning centers
The effect of LO velocity dependence of viscous drag coefficient
Effect of Joule overheating at high vortex velocities
L⍵ can be much greater than λ.
Nb3Sn
H(t)

## Slide 4: Pinning Configurations
Bulk pinning
Surface pinning
Cluster pinning
Un- Gain in the condensation energy in the vortex core at the pin.
pinning potential
pinning force

## Slide 5: Balance of different forces
M-vortex mass, η(v)-nonlinear viscosity, ε-vortex line energy
The effective vortex mass mostly results from the kinetic energy of quasiparticles in the normal core, For Nb, MSuhl~7 x 10-22 kg/m
H. Suhl, Phy. Rev. Lett., vol. 14, no. 7, p. 226, 1965.
Line tension arises from change in vortex line energy
κ=λ/ξ is the Ginzburg-Landau parameter

## Slide 6: Dimensionless equations for numerical simulations
γ α frequency
ζn α pinning strength
β α RF field amplitude
α0 α 1/(LO critical velocity)^2

## Slide 7: Bardeen-Stephen viscous drag force
J
FL
This model assumes superconductor is local and has a finite normal core with size ξ.
Finite electric field E proportional to v generate energy dissipation.
E
Viscous drag
Bardeen-Stephen viscous drag coefficient
At strong currents
Quasiparticles in the core are accelerated by E and diffuse away from the core.
Size of the core decreases as the velocity v increases.

## Slide 8: Larkin – Ovchinnikov (LO) instability
Velocity depend vortex drag:
Jumps of straight vortices at FL>Fmax =η0v0/2
v>v0
A. I. Larkin and Yu. N. Ovchinnikov, Sov. Phys.–JETP 41, 960 (1975)
The LO instability has been observed in many materials.
(G. Grimaldi et al., PRB,92, 024513 (2015). M.Kunchur, PRL,87, 177001 (2001), A. I. Bezuglyj et al. PRB, 99, 174518 (2019).
What happens to the vortex if its fast tip is LO-unstable while the rest of the vortex is LO-stable?
LO unstable
LO stable
For Nb v0 ~ 0.1 km/s – 1km/s near Tc and decreases as T decreases
LO vortex drag force

## Slide 9: Effect of pinning density on Ri(H)
~0.2-3 GHz
Bardeen-Stephen limit
Using the solution for R(x,y,z,t) power p was calculated
Nv- Number of vortices
Surface resistance Ri(H)
B0-Field due to trapped flux
ri(β) at ni=0.16λ-3 < ri(β) at ni=0.83λ-3
Bulk pinning

## Slide 10: Effect of pinning fluctuations on Ri(H)
f ~0.2-3 GHz
Depinning of the vortex between clusters
different statistical distributions of pins with same pin density
Strong fluctuations in Ri(H) at the small field under different statistical realizations of the pinning potentials are observed.
Bulk pinning

## Slide 11: Global surface resistance
hysteretic losses
viscous-dominated
f ~0.2-3 GHz
The low-field Ri(H) averaged over statistical realizations of random pinning potentials exhibits a nearly linear increase with H.
Qualitative behavior of Ri(H) is the same for surface and cluster pinning
Bulk pinning

## Slide 12: Effect of pinning Strength on Ri(H)
ri(β) calculated at γ=0.04, κ=10, l=10λ
The temporal escape of the vortex tip
Cluster pinning
The temporal escape of the vortex tip occurs at
  βc ~ 0.35 at ζn=10
  βc ~ 0.03 at ζn=1
βc is the depinning field
Larkin-Overchinnikov theory of collective pinning :

## Slide 13: Effect of frequency on the field dependence of Ri(H)
ri(β) calculated at κ=10, ζn=1 (Bulk pinning)
As frequency decreases a linear field dependence of Ri(H) develops at small field.
Qualitative behavior is similar for surface and cluster pinning

## Slide 14: Frequency dependence of Ri(f)
Finite length effect
ζn=1
ζn=20
γ=0.04, l/λ=20, κ=10 ni=0.0625λ-3
Pinning-dominated
viscous-dominated
(Bulk pinning)

## Slide 15
ζn=0.08,
ζn=0.04
γ=0.01, κ=2, l=10λ (f~ 0.2-3 GHz)
Strong pinning
Weak pinning
ζn=0.8
α0=104
α0=104
α0=105
Ri(H) for the LO drag at strong RF fields
Strong pinning
Weak pinning
LO instability at v~v0
Vortex moves as a stick
Vortex line tension and pinning suppress the LO instability at v~v0

## Slide 16: Ri(H) at strong RF fields at high frequencies
γ=1, κ=2, l=10λ (f ~ 10-50 GHz)
α0=1
α0=10
Strong pinning
ζn=0.8
βp
β=3,α0=10,ζn=0.8
Pins in the vicinity of the vortex are shown to clarify the vortex behavior.
α0=1
Weak pinning
ζn=0.08
Transition from a nearly harmonic oscillations to highly anharmonic oscillations at β=βp. Elastic skin depth Lω increases with β
α0 α 1/v0^2

## Slide 17: RF overheating
At high vortex velocities, the Joule overheating can mask the LO decrease of Rs(H).
*A. Gurevich, Rev. Accel. Sci. Technol. 5,119 (2012).
α Trapped flux density
Thermal feedback for trapped vortices and linear BCS*:
αk-Kapitza
k-thermal conductivity
d-thickness
(At Weak overheating)
h ~ 0.1-10, s ~ 43 and a ~ 11 (For moderately dirty Nb with κ=2 at T0=1.6 K and f ~ 1.5 GHz.

## Slide 18: RF overheating
γ=0.04
γ=0.4
Dirty Nb/High frequency
(f ~3-10 GHz)
Clean Nb/Low frequency
(f ~0.5-3 GHz)
γ=0.04
(f ~0.5-3 GHz)
LO limit
Bardeen-Stephen limit
LO limit

## Slide 19: Summary
Field dependent Ri(H) strongly depends on pinning density, strength and their statistical distributions at small fields.
The low-field global surface resistance averaged over statistical realizations of a random pinning potential can exhibits a nearly linear increase with H and level off at higher fields.
Ri(H) at strong RF field becomes a nonmonotonic function of H which decreases with H at higher frequencies due to the LO decrease of η(v). This can contribute to the negative Q(H) slope in SRF cavities.
Overheating can mask the descending field dependence of Ri(H) as frequency increases.
Measurements of Ri (H) due to trapped vortices offer opportunities to investigate an extreme nonlinear dynamics of vortices driven by strong Meissner current densities at T<<Tc