## Slide 1: Plasma Electrolytic Polishing as a promising treatment replacement of electropolishing in the Cu and Nb substrate preparation for SRF
The 9th International Workshop on "Thin films applied to Superconducting RF: Pushing the limits of RF Superconductivity"
Eduard Chyhyrynets
15-18 March 2021
Work supported by the INFN CSNV experiment TEFEN

## Slide 2: Motivation
Current and Future Developments in Accelerator Facilities, 2010 IOP Meeting Immediate source: http://www.hep.ucl.ac.uk/iop2010/talks/14.pdf
S. Tazzari and M. Ferrario, ‘Trends in high energy particle accelerators’, Rep. Prog. Phys., vol. 66, no. 6, pp. 1045–1094, Jun. 2003, doi: 10.1088/0034-4885/66/6/204.

## Slide 3: Motivation
Daniele Sertore Cavities fabrication¶ EASISchool 3 2020
Gianluigi Ciovati SURFACE PREPARATION 2015
Daniele Sertore Cavities fabrication¶ EASISchool 3 2020
C A Cooper and L.D. Cooley 2013 Supercond. Sci. Technol. 26 015011
Claire Antoine Materials and surface aspects in the development of SRF Niobium cavities 2012

## Slide 4: Motivation
D.M. Turley, L.E. Samuels Metallography +, 275 (1981) and Turley and Samuels; J Iron and Steel Inst, 186 (1957) 211.
Collier, David, and Rod Schuster. “Superpolishing Deep-UV Optics.” Photonics Spectra, February 2005.
Deformed layer 100-200 μm
Defect layer 1-100 μm
Defect-free Bulk
Upper layer 0,1-1 μm

## Slide 5: Content
PEP state of art.
Comparison with EP.
Potential benefits and prospects for SRF.
Trials and optimization.
Proof of concept: Polishing of Cu and Nb.

## Slide 6: Historical overview
The possibility of electrolysis using an electrical discharge was shown by Gubkin 1 in 1887, J. Gubkin, Ann. Physik 32 [III]
This technology was developed for surface treatments in previous Soviet Union. Many literatures were published in Russian language by Russian and Ukrainian scientists (from 1930s - 1992).
This technology was systematically reviewed and started to draw attention by the Western world researchers until the end of the 20st century (Yerokhin et al. 1999).
Recently technology is being adapting in the various industries and studied in the research institution of Belarus, Bulgaria, Germany, China, Netherland, Russia, Slovakia, USA, Japan, Ukraine and others.
2021
2000
1930
1887
Plasma Electrolytic Process

## Slide 7: State of art
Conventional electrolysis 0-60 V
v
Current, A
Voltage, V
60 V
0

## Slide 8: State of art
v
Current, A
Voltage, V
60 V
Continuous plasma ignition
Arcing regime
Spark ignition
Active gas production
60 V
500 V
0
Plasma electrolytic processing 200-500 V
200 V

## Slide 9: State of art
Parameters | Values
Voltage range , U | 200-360 V
Current density, i | 0,15-0,5 A/cm2
Bath temp. , Tb | 40-95 °C
Time, τ | 1-10 min
Conductivity, δ | 40-300 mS/cm
PEP parameters
I. Danilov, M. et. al, ‘Process Understanding of Plasma Electrolytic Polishing through Multiphysics Simulation and Inline Metrology’, Micromachines, vol. 10, no. 3, p. 214, Mar. 2019, doi: 10.3390/mi10030214.
Vana, D et. al, V. Surface Properties of the Stainless Steel X10 CrNi 18/10 after Application of Plasma Polishing in Electrolyte. Int. J. Mod. Eng. Res. 2013, 3, 788–792.

## Slide 10: State of art: equipment
M. Cornelsen, C. Deutsch, and H. Seitz, ‘Electrolytic Plasma Polishing of Pipe Inner Surfaces’, Metals, vol. 8, no. 1, p. 12, Dec. 2017, doi: 10.3390/met8010012.
Inner surface polishing design
Magnetic stirrer & heater
Beaker with solution
Cathode (s.s.)
Anode/sample
Chemical stand with connections to the power supply
High voltage,
High current PSU
LNL system

## Slide 11: Applications
Semiconductor processing Alloy and multi-metal polishing
Dental implants polishing
Final polishing
Metal surface cleaning
quick surface decontamination (from 30 seconds)
removal of various contaminations (paints, oils, scales, rust/oxides, abrasive impurities) Blunting and deburring
quick removal of burrs with length up to 3 mm
Preparation for coating
cleaning and defatting
etching
surface activation
effective removal of defective coatings for repeated coating
significant improvement of surface wettability

## Slide 12: Applications
Commonly polished, available recipes
Various stainless steel alloys
Brass, Bronze Cr, Ni, Co, Mo, W, Zn alloys.
Not well studied, challenging applications
Nb, V, and alloys
Cu and its alloys
Ti and its alloys
E.V. Parfenov, V.R. Mukaeva, R.G. Farrakhov, Plasma electrolytic treatments for advanced surface finishing technologies, Mater. Technol. Des. 1 (1) (2019) 34–41 http://journal.ugatu.ac.ru/index.php/mtd/article/view/1843/1911 .

## Slide 13: Applications
Commonly polished, available recipes
Stainless steel alloys
Brass, Bronze Cr, Ni, Co, Mo, W, Zn alloys.
Not well studied, challenging applications
Nb, V, and alloys
Cu and its alloys
Ti and its alloys

## Slide 14: Comparison EP vs PEP
Parameters |  | Conventional EP | Plasma Electrolytic Polishing
Pre-treatment |  | Requires (in some cases mechanical) cleaning | Not required
Roughness |  | 0,2 μm | Achievable up to 0,01 μm
Cathode |  | Should follow the shape of the piece | Shape isn’t important
Electrolytes | Metals | Harsh electrolytes, concentrated acids | Greener, diluted water based salts (1-10%)
 | Copper | H3PO4(85%):Butanol = 3:2 | 
 | Niobium | H2SO4(95-98%):HF(49%)=9:1 | Salts
Time to remove 100 μm |  | 3 h – 7 h | 15-30 min
Voltage |  | 2-60 V | 260-360 V
Temperature |  | Ambient | > 65 ֯C
Current density |  | 0,01-0,04 A/cm2 | 0,2-0,6 A/cm2

## Slide 15: Advantages and disadvantages
Economical (time & materials)
Ecological (non harsh electrolytes)
Quality (better roughness limits)
Pre-treatment is not required step
Possible substitution of some mechanical treatments
Security requirements
Higher price of PSU.
Holes, pits, caves are hard to treat (like EP).
Higher temperature requirements.

## Slide 16: Potential benefits and prospects for SRF
Avoid of mechanical pre-treatment of cavities.
Chemical polishing decrease from 1 day to 1 hr time.
Less harmful, concentrated, expensive wastes. Greener way to treat the substrates.
Less (to prove) of Hydrogen in the Niobium. No H2SO4 – no sulfur residuals.
H S

## Slide 17: Risk assessment comparison
BCP 1:1:2
EP Nb 1:9
PEP Nb

## Slide 18: Risk assessment comparison
BCP 1:1:2
EP Nb 1:9
PEP Nb
93 %
79 %
~5%
Quantity of chemicals (w. %)

## Slide 19: Risk assessment comparison
BCP 1:1:2
EP Nb 1:9
PEP Nb
93 %
79 %
~5%
Quantity of chemicals (w. %)
Acids, harsh chemicals
3 Acids: HF:HNO3:H3PO4
2 Acids: HF:H2SO4
No acids! Only salt(s)

## Slide 20: Risk assessment comparison
BCP 1:1:2
EP Nb 1:9
PEP Nb
93 %
79 %
~5%
Quantity of chemicals (w. %)
Acids, harsh chemicals
3 Acids: HF:HNO3:H3PO4
2 Acids: HF:H2SO4
No acids! Only salt(s)
RISK * TIME = More RISK, Time to remove 200 μm
~8-11 h
~4 h
~1 h

## Slide 21: Trials and optimization
Around 10 different compounds were tried and their mixtures.
Study of the bath temperature.
Cathode shape study.
Salts production.
Conductivity study.

## Slide 22: Trials and optimization
Around 15 different compounds were tried.
Study on the bath temperature.
Voltage range.
Conductivity study.

## Slide 23: Proof of concept: Nb
Comparison BCP, EP and PEP
Process / parameters | BCP (1:1:2) | EP (1:9) | PEP
Solution composition | HF:HNO3:H3PO4 | HF:H2SO4 | 1-5 % of Salt
Voltage | - | 18 V | 300 V
Current density | - | 0,025 A/cm2 | 0,4-0,6 A/cm2
Power draw | - | 0,45 W/cm2 | ~150 W/cm2

## Slide 24: Proof of concept: Nb
Comparison BCP, EP and PEP
Process / parameters | BCP (1:1:2) | EP (1:9) | PEP
Solution composition | HF:HNO3:H3PO4 | HF:H2SO4 | 1-5 % of Salt
Voltage | - | 18 V | 300 V
Current density | - | 0,025 A/cm2 | 0,4-0,6 A/cm2
Power draw | - | 0,45 W/cm2 | ~150 W/cm2
Removing rate | 1 µm/min (15 ̊C) * | 0.3 µm/min (30 ̊C) * | 3.5 µm/min (78 ̊C)
Faster then BCP by 3,5 x Faster then EP by 11,6 x

## Slide 25: Proof of concept: Nb
Comparison BCP, EP and PEP
Process / parameters | BCP (1:1:2) | EP (1:9) | PEP
Solution composition | HF:HNO3:H3PO4 | HF:H2SO4 | 1-5 % of Salt
Voltage | - | 18 V | 300 V
Current density | - | 0,025 A/cm2 | 0,4-0,6 A/cm2
Power draw | - | 0,45 W/cm2 | ~150 W/cm2
Removing rate | 1 µm/min (15 ̊C) * | 0.3 µm/min (30 ̊C) * | 3.5 µm/min (78 ̊C)
Time of treatment | 5 min | 20min | 2 min
To remove similar values = 6-7 µm

## Slide 26: Proof of concept: Nb
Comparison BCP, EP and PEP
Process / parameters | BCP (1:1:2) | EP (1:9) | PEP
Solution composition | HF:HNO3:H3PO4 | HF:H2SO4 | 1-5 % of Salt
Voltage | - | 18 V | 300 V
Current density | - | 0,025 A/cm2 | 0,4-0,6 A/cm2
Power draw | - | 0,45 W/cm2 | ~150 W/cm2
Removing rate | 1 µm/min (15 ̊C) * | 0.3 µm/min (30 ̊C) * | 3.5 µm/min (78 ̊C)
Time of treatment | 5 min | 20min | 2 min
Removed | 6 µm | 6,5 µm | 7 µm
Roughness evaluated with a Veeco Dektat 8 Profilometer

## Slide 27: Proof of concept: Nb
Comparison BCP, EP and PEP
EP 20min 6,5 µm
PEP 2 min 7 µm
PEP 2 min 7 µm
BCP 5 min 6 µm
Ra 548±62 nm Ra 440±17 nm Ra 390±23 nm Ra 251±31 nm
Rq 557±142 nm Rq 481±92 nm Rq 327±71 nm Rq 267±29 nm
Initial

## Slide 28: Proof of concept: Nb
Comparison BCP, EP and PEP
Initial
BCP
EP
PEP

## Slide 29: Proof of concept: Nb
Comparison BCP, EP and PEP
PEP 2 min; 7µm
EP 20 min; 6,5 µm
BCP 5 min; 6 µm
Initial
Initial
BCP
EP
PEP

## Slide 30: Proof of concept: Nb
Initial 100x
Initial 500x
Initial 1000x
PEP 100x; 2 min
PEP 500x; 2 min
PEP 1000x; 2 min

## Slide 31: Proof of concept: Cu
Comparison SUBU5, EP and PEP
Process / parameters | SUBU5 | EP (3:2) | PEP
Solution | Sulfamic acid 5 g/l; NH4-citrate 1 g/l Butanol 50 ml/l; H2O2 50 ml/l; | 85 % H3PO4 : n-Butanol | Diluted salts
Voltage | - | 2-6 V | 300 V
Current density | - | 0,01 – 0,03 A/cm2 | 0,35-0,45 A/cm2
Power draw | - | 0,12 W/cm2 | 135 W/cm2

## Slide 32: Proof of concept: Cu
Comparison SUBU5, EP and PEP
Faster then SUBU5 by ~ 3 x Faster then EP by ~10 x
Process / parameters | SUBU5 | EP (3:2) | PEP
Solution | Sulfamic acid 5 g/l; NH4-citrate 1 g/l Butanol 50 ml/l; H2O2 50 ml/l; | 85 % H3PO4 : n-Butanol | Diluted salts
Voltage | - | 2-6 V | 300 V
Current density | - | 0,01 – 0,03 A/cm2 | 0,35-0,45 A/cm2
Power draw | - | 0,12 W/cm2 | 135 W/cm2
Removing rate | 1,5 (70±2 ̊C) μm/min * | 0,15-0,5 (25 ̊C) μm/min | 3-6 (72-80 ̊C) μm/min

## Slide 33: Proof of concept: Cu
Comparison SUBU5, EP and PEP
To remove similar values = 7,5-8 µm
Process / parameters | SUBU5 | EP (3:2) | PEP
Solution | Sulfamic acid 5 g/l; NH4-citrate 1 g/l Butanol 50 ml/l; H2O2 50 ml/l; | 85 % H3PO4 : n-Butanol | Diluted salts
Voltage | - | 2-6 V | 300 V
Current density | - | 0,01 – 0,03 A/cm2 | 0,35-0,45 A/cm2
Power draw | - | 0,12 W/cm2 | 135 W/cm2
Removing rate | 1,5 (70±2 ̊C) μm/min | 0,15-0,5 (25 ̊C) μm/min | 3-6 (72-80 ̊C) μm/min
Time of treatment | 5 min | 30 min | 2 min

## Slide 34: Proof of concept: Cu
Comparison SUBU5, EP and PEP
Process / parameters | SUBU5 | EP (3:2) | PEP
Solution | Sulfamic acid 5 g/l; NH4-citrate 1 g/l Butanol 50 ml/l; H2O2 50 ml/l; | 85 % H3PO4 : n-Butanol | Diluted salts
Voltage | - | 2-6 V | 300 V
Current density | - | 0,01 – 0,03 A/cm2 | 0,35-0,45 A/cm2
Power draw | - | 0,12 W/cm2 | 135 W/cm2
Removing rate | 1,5 (70±2 ̊C) μm/min | 0,15-0,5 (25 ̊C) μm/min | 3-6 (72-80 ̊C) μm/min
Time of treatment | 5 min | 30 min | 2 min
Removed | 7,5 μm | 8 μm | 8 μm
Roughness evaluated with a Veeco Dektat 8 Profilometer

## Slide 35: Proof of concept: Cu
Comparison SUBU5, EP and PEP
EP 30min 8 μm
Initial ! Rough surface !
SUBU 5 min 7,5 μm
PEP 2 min 8 μm
Ra 490±19 nm Ra 113±21 nm Ra 98±9 nm Ra 72±12 nm
Rq 562±84 nm Rq 331±126 nm Rq 152±41 nm Rq 93±19 nm

## Slide 36: Proof of concept: Cu
Comparison of SUBU, EP and PEP
Initial
EP 30 min
8 μm
SUBU 5 min 7,5 μm
PEP 2 min 8 μm

## Slide 37: Proof of concept: Cu
Comparison of SUBU, EP and PEP
Initial
EP 30 min; 8 μm
SUBU 5 min; 7,5 μm
PEP 2 min; 8 μm
Initial
SUBU
EP
PEP

## Slide 38: Proof of concept: Cu
75x PEP 5 min
600x PEP 5 min
2400x PEP 5 min
600x Initial
2400x Initial
150x Initial

## Slide 39: Conclusions
Two recipes of PEP were developed and studied to polish Nb and Cu.
Similar or better surface can be achieved with PEP comparing to EP.
Proved higher performance, and ecological benefits.
Hydrogen disease – to evaluate.

## Slide 40: Future work
Further optimization and look out of recipes for PEP of Nb and Cu.
Design and implementation of PEP polishing of inner surfaces of 6 & 1.3 GHz cavities.
Website https://surfacetreatments.it
https://chyhyrynets.com Thanks to Cristian Pira, Fabrizio Stivanello, Vanessa Garcia, Roberta Caforio, Matteo Zanierato
Material Science and Technology Service for Nuclear Physics crew

## Slide 41: State of art
A. L. Yerokhin, X. Nie, A. Leyland, A. Matthews, and S. J. Dowey, ‘Plasma electrolysis for surface engineering’, Surface and Coatings Technology, vol. 122, no. 2–3, pp. 73–93, Dec. 1999, doi: 10.1016/S0257-8972(99)00441-7.

## Slide 42: Nb chemistry
A: 2Nb + 5H2O = Nb2O5 + 10H+ + 10e
6 Nb + 10 HNO3 = 3 Nb2O5 + 10 NO↑ + 5 H2O
Nb2O5 + 10 HF = 2 NbF5 + 5 H2O
Electrochemistry
2Nb + 5NO3- = Nb2O5 + 5NO2 + 5e
Nb2O5 + 6HF ⇒ H2NbOF5 (soluble)
NbO2F ∙ ½H2O (insoluble) + 1.5H2O
NbO2F ∙ ½ H2O + 4HF ⇒ H2NbOF5 + 1.5H2O
BCP
C: 2 H+= H2 + 2e-
Nb2O5 + HF = H2NbOF5(aq) + HNbF6(aq)+ NbF5(aq)+ H6NbO2F7(aq)+ H2NbF7(aq) +H2O