## Slide 1: Investigation of Local Nonlinear Microwave Response of Nb3Sn and Nb-on-Cu in the Superconducting State
Chung-Yang Wang, Bakhrom Oripov, Steven Anlage
Quantum Materials Center, Department of Physics, University of Maryland
Thin Film SRF workshop 2021

## Slide 2: Outline
Motivation: SRF (Superconducting Radio Frequency) physics and local measurement
Measurement method and nonlinear response
Result for Nb3Sn (sample from Cornell)
Result for Nb-on-Cu (sample from CERN)
Summary and future work

## Slide 3: Superconducting Radio Frequency Cavity
https://www.classe.cornell.edu/rsrc/Home/Research/SRF/SrfCavitiesAPrimerOne/SRFBas1.GIF
https://www-bd.fnal.gov/srf/about_NML.html
SRF2019 (Anna Grassellino)
1.3 GHz

## Slide 4: Near-field microwave microscope
Brf
Jsurf
Brf
sample
Use a near-field microwave microscope to study defects and their relation to cavity performance.
Input: (f, Pinput)
Response: (f, Pf), (2f, P2f), (3f, P3f), etc.
near SRF cavity operating frequency

## Slide 5: Nb3Sn film information (Sn-plating converted Nb3Sn )
Size: 1 cm *1cm
Substrate thickness: 3 mm
Surface SEM
Grain size: 100 nm – 2 um
Cross-section

## Slide 6: Fixed-point measurement for Nb3Sn (Tc around 18.3 K)
T
B
SC
normal state
superconducting transition-induced nonlinearity
↓
around phase boundary

## Slide 7: Fixed-point measurement for Nb3Sn (Tc around 18.3 K)

## Slide 8: Temperature scan

## Slide 9: Temperature scan for various input powers
strong power
↓
weak power

## Slide 10: Sources of 3rd harmonic response
arXiv:1912.07576
Likely harmonic generation from vortex semi-loop
Evidence of several Sn-deficient/Sn-rich Nb3Sn phases
magnetic writer head
sample

## Slide 11: Nb-on-Cu film information
HiPIMS – No bias
1.5±0.1 µm
HiPIMS -25V bias
1.20±0.05 µm
HiPIMS -50V bias
1.24±0.04 µm
HiPIMS -75V bias
1.15±0.04 µm
HiPIMS -100V bias
1.17±0.04 µm
HiPIMS -125V bias
1.25±0.03 µm
DCMS – No bias
3.50±0.08 µm
sample 2
sample 1
sample 3

## Slide 12: First Nb-on-Cu sample (100 V bias sample)

## Slide 13: Temperature scan

## Slide 14: Temperature scan for various input powers
strong power
↓
weak power

## Slide 15: Second Nb-on-Cu sample (no bias sample)

## Slide 16: Temperature scan
low temperature nonlinearity up to 9 K
↓
likely to be intrinsic response of Nb

## Slide 17: Comparison among Nb-on-Cu samples
HiPIMS – No bias
1.5±0.1 µm
HiPIMS -100V bias
1.17±0.04 µm
DCMS – No bias
3.50±0.08 µm
sample 2
sample 1
sample 3
find no nontrivial signal
intrinsic signal from Nb
superconducting transition around 6.1 K (oxide of Nb?)

## Slide 18: Conclusion
Demonstration of magnetic microwave microscope as a RF characterization
Reveal possible existences of lower-Tc superconducting transition
Future work:
AFM-based microwave microscope
shielded microwave
probe

## Slide 19: Acknowledgement
Nb3Sn sample (Cornell): Matthias Liepe, Zeming Sun, Thomas Oseroff
Nb-on-Cu sample (CERN): Guillaume Rosaz
This work is funded by US DOE / HEP through grant # DE-SC0017931 and the Maryland QMC.
Special thanks to Seagate Corp. and Western Digital Corp. for providing magnetic probes for us.

## Slide 20: Sample fabrication for Nb3Sn
Sn-plating converted Nb3Sn (not vapor diffusion approach)

## Slide 21: Coating parameters for Nb-on-Cu
Parameter | HiPIMS | DCMS
Average Power (kW) | 1.3kW | 1.3kW
Discharge Voltage (V) | -660 | -377
Current (A) (peak for HiPIMS) | 160 | 3.4
Gas | Kr | Kr
Pressure (mbar) | 2.3.10-3 | 2.3.10-3
Temperature (˚C) | 150 | 150
Coating duration (min) | 60 | 60