## Slide 1: Status of the ALPI Upgrade for the SPES facility
A.Tsymbaliuk; E. Munaron; D. Bortolato; E. Chyhyrynets; F. Stivanello; C. Pira; G. Keppel
Instituto Nazionale di Fisica Nucleare Laboratori Nazionali di Legnaro (INFN – LNL)
University of Ferrara

## Slide 2
SPES facility in LNL-INFN
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it
ISOL1
ISOL2
1+ area
HRMS
cyclotron
CB - MRMS
RFQ
ALPI SC_linac
Selective Production of Exotic Species (the SPES Facility):
Second generation ISOL facility for nuclear physics:
production and re-acceleration with ALPI linac of exotic beams
Research and production radioisotopes for nuclear medicine:
LARAMED and ISOLPHARM Projects;
Accelerator-based neutron source (proton and neutron facility for applied physics).
Cyclotron
ISOL RIBs+ Post-Acc.
Nuclear Applications
Nuclear Medicine

## Slide 3
Project of ALPI upgrade for SPES facility
Additional 8 cavities
Re-positioned low β cavities
Upgrade advantages: higher energy (+2 cryostats, 8 cavities), higher transmission, increased reliability.
3
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 4: Beam Energies with full SPES Upgrade for Piave-Tandem-ALPI
Chart: 
| 2 | 3 | 2 | 4 | 2.6666666666666665 | 4 | 4.3636363636363633 | 4.4615384615384617 | 3.7647058823529411 | 4.0625 | 4.3529411764705879 | 4.8235294117647056 | 5.6 | 6.4285714285714288 | 4.3809523809523814 | 5.8125 | 8.3333333333333339 | 5.7142857142857144 | 5.0769230769230766 | 5.8461538461538458 | 6.5666666666666664
At present | 22.7 | 16.8 | 22.4 | 11.6 | 17.4 | 11.6 | 11.9 | 10.9 | 12.3 | 13.2 | 12.4 | 11.3 | 8.7 | 8.8 | 9.9 | 8.4 | 6.8 | 8.5 | 9.5 | 8.3 | 7.5
With ALPI in SPES configuration | 28.6 | 19.7 | 28.6 | 14.4 | 23.3 | 14.6 | 13.8 | 13.5 | 16.2 | 18.5 | 16.2 | 14.2 | 10.7 | 10.5 | 13.6 | 10.3 | 8.2 | 10.5 | 11.7 | 10.3 | 9.3
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 5: History of the ALPI Upgrade
5
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 6
Cryostat measurement of previously sputtered medium-β QWR
Chart: Eacc [MV/m]
| 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8
1W | 65325115.2495 | 146981509.3113 | 261300460.9979 | 408281970.3092 | 587926037.2452 | 800232661.8059 | 1045201843.9914 | 1322833583.8017 | 1633127881.2366 | 1976084736.2963 | 2351704148.9807 | 2759986119.2899 | 3200930647.2238 | 3674537732.7824 | 4180807375.9657
3W | 21775038.4165 | 48993836.4371 | 87100153.666 | 136093990.1031 | 195975345.7484 | 266744220.602 | 348400614.6638 | 440944527.9339 | 544375960.4122 | 658694912.0988 | 783901382.9936 | 919995373.0966 | 1066976882.4079 | 1224845910.9275 | 1393602458.6552
7W | 9332159.3214 | 20997358.473 | 37328637.2854 | 58325995.7585 | 83989433.8922 | 114318951.6866 | 149314549.1416 | 188976226.2574 | 233303983.0338 | 282297819.4709 | 335957735.5687 | 394283731.3271 | 457275806.7463 | 524933961.8261 | 597258196.5665
15W | 4355007.6833 | 9798767.2874 | 17420030.7332 | 27218798.0206 | 39195069.1497 | 53348844.1204 | 69680122.9328 | 88188905.5868 | 108875192.0824 | 131738982.4198 | 156780276.5987 | 183999074.6193 | 213395376.4816 | 244969182.1855 | 278720491.731
30W | 2177503.8416 | 4899383.6437 | 8710015.3666 | 13609399.0103 | 19597534.5748 | 26674422.0602 | 34840061.4664 | 44094452.7934 | 54437596.0412 | 65869491.2099 | 78390138.2994 | 91999537.3097 | 106697688.2408 | 122484591.0927 | 139360245.8655
FC 44 (1999) | 213183400 | 201335900 | 196308700 | 195838100 | 192590500 | 185434100 | 187928700 | 189331800 | 179223600 | 180599800 | 173631700 | 174806200 | 167501900 | 166883400 | 163138300 | 155511300 | 142209300 | 133840300 | 114081100 | 96182140 | 87431980 | 80998300 | 70970290 | 74900100 | 70718130 | 50501000
6
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 7: Sputtering parameters definition
7
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 8
Process of research activity
Refurbishing and modification of the QWR sputtering system.
More then 15 tests were done in order to find best sputtering parameters for QWR deposition process.
Refurbishing and modification of the cryostat for low temperature measurements.
Definition of the best sputtering parameters with cleaned quartz for the QWR plates was done.
More then 5 high-β QWRs were deposited from 2019.
More then 12 low temperature measurements of medium-β and high-β QWRs were done.
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 9
Parameters | # 6 | # 7 | # 8 | # 9 | # 10 | # 11 | # 12 | # 13 | # 14 | # 15
Pre sputtering baking |  |  |  |  |  |  |  |  |  | 
Chamber temp. [°C] | - | 120 – 150 | 120 – 200 |  |  |  |  |  |  | 
Cavity temp. [°C] | - | 300 – 400 | 350 |  |  |  |  |  |  | 
Time [hours] | - | 51 | 63 | 48 | 72 | 48 | 88 | 72 | 48 | 72
 | - |  |  |  |  |  | 3 | 1,3 | 1,6 | 4,6
Sputtering parameters |  |  |  |  |  |  |  |  |  | 
Full time [min] | 60 | 165 |  |  | 150 | 160 | 165 |  | 260 | 240
Series | 4 x 15 | 11 x 15 |  |  | 10 x 15 | 11 x 15 |  |  | 17 x 15 | 16 x 15
Pressure [mbar] | 0,1 - 0,21 |  |  |  |  |  |  |  |  | 
Bias voltage [V] | -130 |  |  |  |  |  |  |  |  | 
Cavity temp. [°C] | 25 | 300 |  |  |  |  |  |  |  | 
Cathode current [A] | 3 | 3 | 3 | 3,5 | 4 | 3,25 | 3,25 | 3,25 | 2 | 3,25
Parameters of the test measurements for QWR deposition
Parameters of different sputtering tests
9
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 10
Scheme of the system for high-β QWR deposition
10
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it
Vacuum chamber
grounded
QWR resonator
(130 V)
Grounded grids
Nb cathode
(-700V)
Biased cathode
(130 V)

## Slide 11
Results of the tests sputtering
– Deposition rate vs sputtering current
Chart: Current, A
| 2 | 3 | 3.25 | 3.5 | 4
internal | 12 | 13 | 11 | 8.2 | 8
external | 3.2 | 11 | 11.3 | 14 | 15.2
top position | 4.25 | 6 | 9 | 5 | 8
11
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 12
Sputtering process | 
Parameter | 
Sputtering pressure [mbar] | 0,1
Cycle time [min] | 15
Number of cycles | 20
Total time [min] | 300
Cathode current [A] | 3.25
Bias voltage [V] | -130
Temperature of the cavity before sputtering [°C] | 300
Experimentally defined optimal parameters
Baking process | 
Parameter | 
Temperature (zone 1) [°C] | 200
Temperature (zone 2) [°C] | 120
Temperature (zone 3) [°C] | 200
Cavity temperature [°C] | 350 – 400
Baking time [hours] | 48
12
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 13: Nb/Cu high-β QWR cavity production
13
13
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 14
Nb/Cu QWR preparation
№ | Process | Parameters
1 | Tumbling | Abrasive form: Green finishing pyramids; time 12 hours
2 | Ultrasound cleaning | 
3 | Electro polishing | Solution: H3PO4 : Butanol 3:2 v.r.; Volume: 90 l; Time: 2,5 hours.
4 | High Pressure Rinsing | Solution: water
5 | SUBU 5 | Solution: Sulfamic acid 5 g/l , Ammonium citrate - 1 g/l, Butanol - 50 ml/l , H2O2 - 50 ml/l; Time: 4 min.
6 | Rinsing | 
7 | Passivation | Solution: Sulfamic acid 10 g/l; Time: 5 min.
8 | Rinsing | 5 times
9 | Ultrasound cleaning | 10 min.
10 | Rinsing | 5 min.
11 | High Pressure Rinsing, ethanol rinsing, nitrogen drying, packaging | 
14
14
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 15
Nb/Cu QWR sputtering
Sputtering process | 
Parameter | 
Sputtering pressure [mbar] | 0,1
Cycle time [min] | 15
Number of cycles | 20
Total time [min] | 300
Pause between depositions [min] | 150
Cathode current [A] | 3.25
Bias voltage [V] | -130
Temperature of the cavity before sputtering [°C] | 300
Baking process | 
Parameter | 
Temperature (zone 1) [°C] | 220
Temperature (zone 2) [°C] | 120
Temperature (zone 3) [°C] | 220
Cavity temperature [°C] | 400
Baking time [hours] | 48 - 96
15
15
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 16: Results of Nb/Cu high-β QWR cryostat measurements
16
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 17
Preparation methodology of Nb/Cu QWR for cryostat measurement
№ | Process | Parameters
1 | Pumping of the system. | 
2 | Liquid Nitrogen transfer in the external shield. | 
3 | Cavity baking. | 350 K; 48 – 120 h.
4 | “Hot conditioning”. | 1 – 70 W; 24 – 48 h.
5 | Liquid Nitrogen cooling down of the cavity. | From 350 K to 100 K.
6 | Liquid Helium cooling down of the cavity. | From 100 K to 4,2 K.
7 | “Cold conditioning”. | P(He) = 5,0E-5 mbar.
8 | Cryostat measurements | 
17
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it
Notes: 1)
2)
3)

## Slide 18
Chart: Eacc [MV/m]
| 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8
1W | 65325115.2495 | 146981509.3113 | 261300460.9979 | 408281970.3092 | 587926037.2452 | 800232661.8059 | 1045201843.9914 | 1322833583.8017 | 1633127881.2366 | 1976084736.2963 | 2351704148.9807 | 2759986119.2899 | 3200930647.2238 | 3674537732.7824 | 4180807375.9657
3W | 21775038.4165 | 48993836.4371 | 87100153.666 | 136093990.1031 | 195975345.7484 | 266744220.602 | 348400614.6638 | 440944527.9339 | 544375960.4122 | 658694912.0988 | 783901382.9936 | 919995373.0966 | 1066976882.4079 | 1224845910.9275 | 1393602458.6552
7W | 9332159.3214 | 20997358.473 | 37328637.2854 | 58325995.7585 | 83989433.8922 | 114318951.6866 | 149314549.1416 | 188976226.2574 | 233303983.0338 | 282297819.4709 | 335957735.5687 | 394283731.3271 | 457275806.7463 | 524933961.8261 | 597258196.5665
15W | 4355007.6833 | 9798767.2874 | 17420030.7332 | 27218798.0206 | 39195069.1497 | 53348844.1204 | 69680122.9328 | 88188905.5868 | 108875192.0824 | 131738982.4198 | 156780276.5987 | 183999074.6193 | 213395376.4816 | 244969182.1855 | 278720491.731
30W | 2177503.8416 | 4899383.6437 | 8710015.3666 | 13609399.0103 | 19597534.5748 | 26674422.0602 | 34840061.4664 | 44094452.7934 | 54437596.0412 | 65869491.2099 | 78390138.2994 | 91999537.3097 | 106697688.2408 | 122484591.0927 | 139360245.8655
DD (01.08.2019) | 920143641.3187 | 1321883430.9866 | 1328581500.7396 | 1221594211.8268 | 943233615.9496 | 959333223.1926 | 987518533.8956 | 1024551731.2016 | 1051048758.7327 | 1089752493.046 | 1134993384.567 | 927528749.6165 | 787868969.3558 | 689457685.2581 | 638923368.0071 | 609328223.0012 | 583662036.3707 | 533132214.3847 | 520860703.283 | 488699688.6763 | 455407207.6382 | 436473578.8558 | 432598680.9881 | 401457974.5819 | 390406952.1194 | 360486601.4759 | 341196806.6063 | 329666515.9188 | 295948847.3408 | 291106484.3804 | 713092925.9566 | 727951796.6762 | 768050454.9979 | 794773984.9816 | 825373876.3166 | 846575363.3369 | 902155396.194 | 949734865.5824 | 984040396.3098 | 1007174350.8467 | 1017780370.0132 | 1073925038.2856 | 1102122879.4678 | 1145713397.7794 | 1260694060.5827 | 1299277685.0916 | 1656684922.4696 | 1480752955.6113
HB 7 (29.11.2019) | 357560617.491 | 361549512.8481 | 370638238.2564 | 375423252.3075 | 385003592.6593 | 390695193.5565 | 406401190.2166 | 417216065.6399 | 427300750.9364 | 441834790.0839 | 450206396.6328 | 469453936.4761 | 506430519.6283 | 524000558.0644 | 245877112.026 | 201081464.1132 | 231838177.7899 | 192971598.5268 | 91389558.186 | 101943451.5681 | 119636443.4497 | 126927885.9528 | 135094384.2276 | 152318105.8592 | 162974030.0789 | 164899784.152 | 179689814.0839 | 190059948.0299 | 197975210.3421 | 208516455.7715 | 218688161.202 | 229173992.5426 | 234093494.5806 | 245416494.3295 | 253455960.9048 | 266294034.184 | 273186585.4493 | 284991936.9908 | 318104400.9394 | 95466647.7246 | 60551981.3843 | 46749813.4839
HB 8 (27.02.2020) | 398000000 | 444000000 | 504000000 | 333000000 | 298000000 | 262000000 | 242000000 | 227000000 | 210000000 | 205000000 | 196000000 | 185000000 | 174000000 | 165000000 | 157000000 | 148000000 | 139000000 | 127000000 | 114000000 | 318000000 | 311000000 | 140000000 | 105000000 | 93400000 | 88300000 | 81400000 | 74400000 | 65400000 | 70300000 | 54400000
Nb/Cu QWR cryostat measurement results
Power | Eacc | Q
7 W | >4,5 MV/m | >1,0E8
Measurement goal
Target
18
18
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 19
Nb/Cu QWR cryostat measurement results
Cavity number | Q[0] | Eacc, [MV/m] | Q (at 7W) | ΔT (plate – cavity)
DD cavity | 2,07E+9 | 6,6 | 4,2E+8 | 0,96
HB 5 | 7,6E+8 | 5,5 | 2,8E+8 | 1,66
HB 8 | 1,5E+8 | 3,8 | 1,4E+8 | 2
HB 7 | 3,2E+8 | 3,7 | 1,8E+8 | 2,8
HB 6 | 7,6E+7 | 2,6 | 6,7E+7 | 3,2
19
19
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 20
Current status of the ALPI Upgrade
Conclusions
Sputtering and measurement vacuum systems for QWR production were refurbished and modified;
QWR sputtering technology was updated for production of Nb/Cu high-β QWR cavities;
Several Nb/Cu QWR cavities were produced;
2 Nb/Cu QWR cavities are ready for use;
The best performance of the produced QWR:
Q[0] = 2,07E+9; Q[7W] = 4,2E+8 E[acc] = 6,6 MV/m)
20
20
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it

## Slide 21
Thank you for attention!
21
21
TFSRF-2021 15-18 March Andrii.Tsymbaliuk@lnl.infn.it
Special thanks to my research team: Giorgio Keppel, Enrico Munaron, Damiano Bortolato, Fabrizio Stivanello, Eduard Chyhyrynets and Cristian Pira.