## Slide 1
Deposition and Characterisation of Alternative Superconducting thin films to Niobium for SRF applications
Reza Valizadeh
on behalf of the team
9th International Workshop on Thin Film JLAB

## Slide 2
Image © STFC John Dawson
MOTIVATION
Bulk niobium (Nb) for the past three decades has been the material of choice for SRF applications:
  It has the highest Tc (9.25K) for pure metal
  It has highest lower magnetic field Hc1
  Can be Easily fabricated
But it has achieved the magnetic field limitation so further improvement of cavity RF performance dictate to turn to other superconducting materials.
Nb3Sn and NbTiN alloy are type II superconductor with ideal Tc of 18 K and superheating field about 400 mT. Hence can offer improvement in
  Cryogenic efficiency
  Performing at higher accelerating field.
  Recently there has been positive progress in producing Nb cavities with Nb3Sn coating.
The materials can be deposited as thin film either in:
  Single layer (Nb3Sn / NbTiN on Cu or Nb)
  Double layer (Nb /Nb3Sn or Nb / NbTiN on Cu)
  Multilayer (SIS): Nb /Insulator/ Nb3Sn, or Nb / insulator / NbTiN on Cu
9th International Workshop on Thin Film JLAB

## Slide 3: Nb3Sn unit cell Structure
In Nb3Sn unit cell the Sn atoms forms a bcc lattice and each cube face is bisected by orthogonal Nb chains.
In bcc Nb the shortest distance between the atoms is 2.860 A starting from a lattice parameters of a= 3.300 A
In Nb3Sn the lattice parameters is about a = 5.290 A for stoichiometric composition and the distance between the Nb atoms is 2.650 A
The reduction of distance between the Nb chains is responsible for the high Tc in comparison to bcc Nb.
Sn deficiency may cause the Nb to occupy the site and effect the long range order
Material | Tc (K) | ρn(μΩcm) | Hc(0) [T] | Hc1(0) [T] | Hc2(0) [T] | (0) [nm] | Δ [meV] | ξ [nm]
Nb3Sn | 18 | 20 | 0.54 | 0.05 | 30 | 80-100 | 3.1 | 4

## Slide 4: Nb3Sn binary phase diagram
Intermetallic niobium–tin is based on the superconductor Nb, which exists in a bcc Nb structure or a metastable Nb3Nb A15 structure
When alloyed with Sn and in thermodynamic equilibrium, it can form either Nb1−βSnβ (about 0.18≤β≤0.25) or the line compounds Nb6Sn5 and NbSn2.
Both the line compounds at β = 0.45 and 0.67 are superconducting, with
  Tc<2.8 K for Nb6Sn5
  Tc<2.68 K for NbSn2

## Slide 5: Nb3Sn deposition system and parameters
Magnetron sputtering from a RRR 300 Nb target
Substrate Temperature, Deposition Rate, Deposition Thickness, Substrate Bias, Concurrent Ion Bombardment can be varied independently.
Substrates are loaded into the load lock and system fully Baked.
Nb deposition:
400 W, 470v, 0.85A
4 hours deposition
Dc sputtering
Nb3Sn deposition:
200 W, 489 V, 0.41 A
2 Hours deposition
DC sputtering

## Slide 6: Cu/Nb3Sn deposition (single layer) at various Temperature
Nb3Sn were deposited on copper with no prior chemical cleaning such (EP or SUBU5) at various Temperature of RT, 450°C and 600°C. The RT deposition showed no sign of superconductivity.
Best performance in terms of superconducting properties is achieved by the film deposited at 600°C (A15-6) with a Tc of 15.7 K, a lattice parameters of 0.529 nm and grain size in order of 8 to10 nm.
The film deposited at moderate temperature of 450°C has its performance much reduced with Tc of 14.6 K
The film deposited at room temperature and then post annealed at 650°C (A15-9) has the worst performance since M/Mi drop sharply at very low field of about 10 mT.

## Slide 7: Cu (EP)LNL / Nb3Sn (single layer) deposited at 650C
There is some diffusion of copper at the interface
There is a clear oxide layer at the interface despite high temperature treatment prior deposition
There are area that seems to be Sn deficient where there are dark contrast spots.
The Tc was determined to be between 17.75K (on sapphire) and 17.5 on copper
First Ben for 50mT and 140mT deposited on Cu and Sapphire, and HC2 above 16 T.
An interesting results which gives the opportunity of direct deposition of copper cavity rather than Niobium cavity.
Layer t (1e15at/cm2) t (nm) r(1e22at/cm3) Nb Sn Al O
1 7606.631 1489.817 5.106 75.0000 25.0000 0.0000 0.0000
2 821647.625 69631.156 11.800 0.0000 0.0000 40.0000 60.0000
Chart: Bdc [Oe]
Film thickness of 2.5 Microns

## Slide 8: Cu /Nb/Nb3Sn (double layer)
Layer t (1e15at/cm2) t (nm) r(1e22at/cm3) Nb Sn O Al
1 7644.333 1497.201 5.106 75.0000 25.0000 0.0000 0.0000
2 15920.986 2855.270 5.576 100.0000 0.0000 0.0000 0.0000
3 898207.563 76119.281 11.800 0.0000 0.0000 60.0000 40.0000
The interfaces both at Cu/Nb and Nb/Nb3Sn is well define
Nb layer is grown in large grain and in a perpendicular direction to the substrate surface
No intermixing of elements is observed
Some area of Sn deficiency and rich Sn in Nb3Sn layer can be observed
First Ben is estimated at 95mT.
Tc(Nb3Sn)~17K
Tc (Nb)~8.8K
Chart: Bdc [Oe]

## Slide 9: Cu/Nb/Nb3Sn (double layer)
Two distinct area can be observed:
  Perfect area with sharp interface with correct stoichiometry for Nb3Sn layer
  Copper diffusion from the interface to top surface.
Nb and Nb3Sn layers are completely intermixed and there is a substantial volume of copper substrate is present throughout the depth of the layer and at the surface
Inside the cavity there are trace silicon and aluminium oxide.

## Slide 10: SIS Structure of thick Nb3Sn/AlN/Nb multilayer on copper
Chart: Bdc [Oe]
Tc (Nb3Sn)~ 17 K
Tc (Nb)~ 8K
Although the layers are well identified however there is again some degree of mixing can be observed.
Sn segregation at Cu/Nb interface
Nb3Sn into Nb layer
Copper diffusion on to the surface
Some level of Nitrogen diffusion into all the layers.
The Ben in parallel external field is estimated to be 61mT and 4mt for Cu and Sapphire Substrate

## Slide 11: SIS Structure of thin layer (Nb3Sn/AlN)2/Nb multilayer on Cu
Layer t (1e15at/cm2) t (nm) r(1e22at/cm3) Nb Sn Al N O
1 245.384 48.060 5.106 75.0000 25.0000 0.0000 0.0000 0.0000
2 252.853 26.394 9.580 0.0000 0.0000 50.0000 50.0000 0.0000
3 321.916 63.050 5.106 75.0000 25.0000 0.0000 0.0000 0.0000
4 132.522 13.833 9.580 0.0000 0.0000 50.0000 50.0000 0.0000
5 11761.658 2109.336 5.576 100.0000 0.0000 0.0000 0.0000 0.0000
6 1143361.875 96895.070 11.800 0.0000 0.0000 40.0000 0.0000 60.0000
The observed distortion of the Nb3Sn / AlN bilayer is most probably due to mechanical polishing prior to ion beam milling, since such distortion is not present in the RBS spectra
The RBS analysis predicts stoichiometric layers with the second AlN layer almost being double the thickness of the first AlN layer. Similarly the first Nb3Sn layer is 25% thicker than the second Nb3Sn layer.

## Slide 12: SIS Structure of thin layer (Nb3Sn/AlN)2/Nb multilayer on Cu
Chart: Bdc [Oe]
Tc (Nb3Sn) ~ ??
Due to Small DC field, lots of copper
Tc (Nb) ~ 9.2 K
The Ben in parallel external field is estimated to be 108 mT and 130 mT for Cu and Sapphire Substrate
There is nearly no hysteresis in the thin double SIS structure
This can be due to the protective effect of multilayers which reduces the sensitivity to pinning effect.

## Slide 13
Surface Resistance as function of Temperature
Multilayer Nb3Sn in SIS structure measured in SIC Cavity at JLAB courtesy Dr Sayeed.
The Tc of Nb3Sn is cannot be measured due to its thin layer or low field
The comparison between the ML layer structure and Self supporting Nb3Sn synthesised with different method at JLAB shows an increase of surface resistance by up to a factor of 10 which at 6 K is about 3.5 mΩ.

## Slide 14: B1 compounds -NbTiN
Material | Tc (K) | ρn(μΩcm) | Hc(0) [T] | Hc1(0) [T] | Hc2(0) [T] | (0) [nm] | Δ [meV] | ξ [nm]
NbTiN | 17.3 | 35 | - | 0.03 | 15 | 150-200 | 2.8 | 5
NaCl structure
Ti and Nb form fcc lattice and N occupy all the octahedral interstices
High Hardness,
Not as brittle as Nb3SN
Good adhesion,
Very good corrosion and erosion resistance
Reasonably good conductor
Moderately easy to synthesis
High sublimation temperature
Tc depends both on stoichiometry and deposition temperature

## Slide 15: NbTi and NbTiN Single layer
(111)
(200)
(220)
(311)
(222)
For both system the superconducting phase only materialises at high Temperature.
The higher the temperature the higher Tc ranging from 14 K to 17 K.
The best Tc and hysteresis was found to be on Cu substrate.
Can be synthesised quite easily with both alloy target and concurrent single elemental target.
Both RBS and EDS showed good compositional uniformity for all the film.
The XRD matched well with the published data with lattice parameter of 4.326 A and grain size of 28.5 nm.

## Slide 16: Multilayer SIS deposition of B1 SC
Substrate heated 20 h prior deposition deposition temperature 650C
Deposition SIS:
Nb/AlN/NbTiN/AlN/NbTiN/AlN/ NbTiN
5 h or 2h (400 W DC) for Nb, 7 min (200 W Pulsed DC) for AlN (10 - 15 nm) and 10 min (300W DC) for NbTiN (30 nm)
Nb/AlN/NbN/AlN/NbN
2h (400 W DC) for Nb, 7 min (200 W Pulsed DC) for AlN (10 - 15 nm) and 10 min (300W DC) for NbN (35 nm)

## Slide 17: Multilayer SIS deposition
Layer | Layer thickness (1e15at/cm2) | Layer thickness (nm) | Nb | Ti | N | Al | O
1 | 227.7 | 52.6 | 20.1876 | 19.33 | 60.47 | 0 | 0
2 | 109.3 | 11.4 | 0 | 0 | 50 | 50 | 0
3 | 263.95 | 58.7 | 20.8 | 26.05 | 53.1 | 0 | 0
4 | 105.68 | 11.03 | 0 | 0 | 50 | 50 | 0
5 | 285.32 | 67.11 | 15.2 | 20.51 | 64.27 | 0 | 0
6 | 141.06 | 14.7 | 0 | 0 | 50 | 50 | 0
7 | 13510.8 | 2423.05 | 100 | 0 | 0 | 0 | 0

## Slide 18
21/08/19 – Nb/[AlN/NbTiN]3
( Nb 2h, AlN 7min, NbTiN 10min )
Cu, Ta, Sapphire subst., Self-Supported film (SS)
Chart: Bdc [Oe]
4.22 K
Cu
Sapp
SS

## Slide 19
16/08/19 – Nb/[AlN/NbTiN]3
( Nb 2h, AlN 7min, NbTiN 5min )
Cu, Ta, subst.
Chart: Bdc [Oe]
4.22 K
Cu
SS

## Slide 20
19/08/19 – Nb/[AlN/NbTiN]3
( Nb 5h, AlN 7min, NbTiN 5min )
Cu, Ta, Sapphire subst., Self-Supported film (SS)
Chart: Bdc [Oe]
Cu
Sapp
SS
4.22 K

## Slide 21: Summary
Nb3Sn can be successfully deposited from an alloy target with satisfactory SC properties when it is deposited at high temperature (around 600-650 °C)
Final Smooth surfaces and sharp interface between layers can be achieved by suitable surface preparation method/process of substrate
Impurities such as silicon oxide may cause complex defects to be formed when Nb3Sn is deposited in multilayer structure.
Substrate preparation can influence the growth of the film and hence its SC properties
Protective effect of multilayers to some extend is been shown :
Reducing sensitivity to pinning defects
Multilayer structure even without insulating layer reduced the hysteresis loop
Defects are still present in individual layers but not detected anymore when SIS structure fully SC.
Complementary non-destructive technique such as RBS proved to be a powerful technique to distinguish post sample preparation damage.
NbTiN can be considered as a practical alternative material due to its ease of synthesis and reproducibility.
It has good adhesion, wide range of SC composition window, has high hardness and good resistivity to corrosion and erosion with moderate normal surface resistance. Can be deposited at lower temperature with good SC performance.

## Slide 22: Special Thanks to all the team member STFC and international Partners
STFC
Adrian Hannah
Gavin Stenning
Francis Lockwood Estrin
Felix Walk
Daniel Turner
Yukari Dan (Hitachi)
Karl Dawson
Sepideh Aliasghari
Stuart Wilde
James Conlon
Oleg Malyshev
Tobias Junginger
James Bradley
Graeme Burt
Vinod Dannak
IEE
Eugen Seiler
Rastislav Ries
University of Siegen
Michael Vogel
Stewart Leith
INFN
Cristian Pira
Eduard Chyhyrynets
CAE
C.Z.Antoine
JLAB
Anne Marie Valente
M N Sayeed
HZB
O. Kugeler
D. Tikhonov
RTU
A Medvids

## Slide 23
@STFC_matters
Science and Technology Facilities Council
Science and Technology Facilities Council
Notes: The abstract pattern can be removed or repositioned if required. Be careful to ‘Send to Back’ so that it does not obscure any important information.