## Slide 1: INVESTIGATION OF SIS MULTILAYER FILMS AT HZB
D. Tikhonov, O. Kugeler, S. Keckert, J. Knobloch, E. Chyhyrynets, S. Leith, M. Vogel, C. Pira
EASITrain – European Advanced Superconductivity Innovation and Training. This Marie Sklodowska-Curie Action (MSCA) Innovative Training Networks (ITN) has received funding from the European Union’s H2020 Framework Programme under Grant Agreement no. 764879
9th International Workshop on Thin Films and New Ideas for Pushing the Limits of RF Superconductivity
Presenter
Dmitry Tikhonov
Early stage researcher
Helmholtz-Zentrum Berlin
dmitry.tikhonov@helmholtz-berlin.de
+49-30-8062-12922

## Slide 2: Temperature behaviour of the samples
 | SIS films tested | Structure | Base test? | Produced by
J-Lab SIS [1] | NbTiN – AlN – Nb(bulk) | 75nm – 15 nm – bulk Nb | Yes | J-lab
ARIES 1st SIS | NbN – AlN – Nb(film)/Cu | 197nm – 35 nm – 3 µm Nb | Yes | Siegen
ARIES 2nd SIS | NbN – AlN – Nb(film)/Cu | 180nm – 8 nm – 4 µm Nb | No | Siegen
ARIES 3ed SIS | NbN – AlN – Nb(film)/Cu | 180nm – 24 nm – 4 µm Nb | No | Siegen
The manufacture of the QPR samples received funding from the European Union’s Horizon 2020 Research and Innovation programme under Grant Agreement No 730871
[1] S. Keckert, Rf characterization of an s-i-s’ multilayer sample, Proceedings of SRF2019, Dresden, Germany, THFUA1
Substrate and the coated sample
4 Multilayer samples tested at HZB
Samples 2 & 3 coated with HiPIMS, substrate is polished by INFN

## Slide 3: Coating parameters
Lab | Process
INFN-LNL | EP 40 min
Siegen | 650 deg C annealing
Siegen | 1st layer: Sample coated for 40 mins with DCMS Nb layer and HiPIMS interlayer
HZB | QPR test, Rinsed with UP water (18 MOhm), inserted into the QPR, cooldown, tested
HZB | Dismounted from the QPR and disassembled in the local clean area. Stored with room air in the container.
Siegen | Bake out overnight with temperature set at 650 deg C.
Siegen | 2nd and 3ed layers: AlN: DCMS process 600mPa dep pressure, 100% N2 process gas 1rpm rotation speed 5 mins coating @ 7 nm/min dep rate = 35 180°C substr. Temp NbN: DCMS process 1400mPa deposition pressure, Ar + 8% N2 (48sccm) 1rpm rotation speed 29 min coating @ 6.81 nm/min dep rate = 200 nm 290°C substr. Temp
 | SIS films tested | Structure | Base test? | Produced by
ARIES 1st SIS | NbN – AlN – Nb(film)/Cu | 200nm – 35 nm – 3 µm Nb | Yes | Siegen

## Slide 4: Coating parameters
INFN | EP
USi | ARIES 2nd SIS, Coated in one run: 1. HiPIMS Nb (4mu) 2. AlN (8nm) 3. HiPIMS NbN (180nm)
HZB | QPR test, Cleanroom inspection, rinsing with u.p. water (>18 MOhm), drying 48h in ISO 5 Clean room.
INFN | Stripping
INFN | Fast EP, No black dots, pitting (obviously not removed)
INFN | Passivation, HPR, packaging.
USi | ARIES 3ed SIS, Coated in one run: 1. HiPIMS Nb (4mu) 2. AlN (23/24nm) 3. HiPIMS NbN (180nm)
 | SIS films tested | Structure | Base test? | Produced by
ARIES 2nd SIS | NbN – AlN – Nb(film)/Cu | 180nm – 8 nm – 4 µm Nb | No | Siegen
ARIES 3ed SIS | NbN – AlN – Nb(film)/Cu | 180nm – 24 nm – 4 µm Nb | No | Siegen

## Slide 5: Temperature behaviour of the samples
 | SIS films tested | Structure | Base test? | Produced by
J-Lab SIS | NbTiN – AlN – Nb(bulk) | 75nm – 15 nm – bulk Nb | Yes | J-lab
ARIES 1st SIS | NbN – AlN – Nb(film)/Cu | 197nm – 35 nm – 3 µm Nb | Yes | Siegen
ARIES 2nd SIS | NbN – AlN – Nb(film)/Cu | 180nm – 8 nm – 4 µm Nb | No | Siegen
ARIES 3ed SIS | NbN – AlN – Nb(film)/Cu | 180nm – 24 nm – 4 µm Nb | No | Siegen
Non-monotonic temperature dependence is observed at different temperatures
On 1st ARIES sample the effect is lower, but still resolvable
Measurement results for Q1 ~ 415 MHz

## Slide 6: Temperature behaviour of the samples
 | SIS films tested | Structure | Base test? | Produced by
J-Lab SIS | NbTiN – AlN – Nb(bulk) | 75nm – 15 nm – bulk Nb | Yes | J-lab
ARIES 1st SIS | NbN – AlN – Nb(film)/Cu | 197nm – 35 nm – 3 µm Nb | Yes | Siegen
ARIES 2nd SIS | NbN – AlN – Nb(film)/Cu | 180nm – 8 nm – 4 µm Nb | No | Siegen
ARIES 3ed SIS | NbN – AlN – Nb(film)/Cu | 180nm – 24 nm – 4 µm Nb | No | Siegen
Non-monotonic temperature dependence is observed at different temperatures
On 2nd sample the effect is lower, but still resolvable
Sample with 8 nm insulator was produced to try to shift the peak, nothing observed
Measurement results for Q1 ~ 415 MHz

## Slide 7: Temperature behaviour of the samples
 | SIS films tested | Structure | Base test? | Produced by
J-Lab SIS | NbTiN – AlN – Nb(bulk) | 75nm – 15 nm – bulk Nb | Yes | J-lab
ARIES 1st SIS | NbN – AlN – Nb(film)/Cu | 197nm – 35 nm – 3 µm Nb | Yes | Siegen
ARIES 2nd SIS | NbN – AlN – Nb(film)/Cu | 180nm – 8 nm – 4 µm Nb | No | Siegen
ARIES 3ed SIS | NbN – AlN – Nb(film)/Cu | 180nm – 24 nm – 4 µm Nb | No | Siegen
Non-monotonic temperature dependence is observed at different temperatures
On 2nd sample the effect is lower, but still resolvable
Sample with 8 nm insulator was produced to try to shift the peak, nothing observed
Another coating also shows no result
Measurement results for Q1 ~ 415 MHz

## Slide 8: Temperature behaviour of: ARIES 1st sis
High residual resistance
Non-monotonic dependence is observed at low field
At higher field it changes to a monotonic “plateau”
 | SIS films tested | Structure | Base test? | Produced by
ARIES 1st SIS | NbN – AlN – Nb(film)/Cu | 197nm – 35 nm – 3 µm Nb | Yes | Siegen

## Slide 9: Temperature behaviour of: ARIES 1st sis
3d reconstruction of Rs at Q1 ~415 MHz
 | SIS films tested | Structure | Base test? | Produced by
ARIES 1st SIS | NbN – AlN – Nb(film)/Cu | 200nm – 35 nm – 3 µm Nb | Yes | Siegen

## Slide 10: Temperature behaviour of: ARIES 1st sis
At 415 MHz Rres is increased also ‘BCS’ is bigger for SIS structure then baseline
Nothing is observed for 2nd mode Q2 ~850 MHz
Measurement results for: Q1 ~ 415 MHz and Q2 ~850 MHz, B 10 mT
 | SIS films tested | Structure | Base test? | Produced by
J-Lab SIS | NbTiN – AlN – Nb(bulk) | 75nm – 15 nm – bulk Nb | Yes | J-lab
ARIES 1st SIS | NbN – AlN – Nb(film)/Cu | 197nm – 35 nm – 3 µm Nb | Yes | Siegen

## Slide 11: Temperature behaviour of: ARIES 1st sis
At 415 MHz Rres is increased also ‘BCS’ is bigger for SIS structure then baseline
Nothing is observed for 2nd mode Q2 ~850 MHz
For J-lab SIS the peak shifted for second mode
Measurement results for: Q1 ~ 415 MHz and Q2 ~850 MHz, B 10 mT
 | SIS films tested | Structure | Base test? | Produced by
J-Lab SIS | NbTiN – AlN – Nb(bulk) | 75nm – 15 nm – bulk Nb | Yes | J-lab
ARIES 1st SIS | NbN – AlN – Nb(film)/Cu | 197nm – 35 nm – 3 µm Nb | Yes | Siegen
[1] S. Keckert, Rf characterization of an s-i-s’ multilayer sample, Proceedings of SRF2019, Dresden, Germany, THFUA1

## Slide 12: Temperature behaviour of: ARIES 1st sis
 | SIS films tested | Structure | Base test? | Produced by
ARIES 1st SIS | NbN – AlN – Nb(film)/Cu | 197nm – 35 nm – 3 µm Nb | Yes | Siegen
Peak has shifted
After a shift observed, a VTS thermocycle (>25K) was done to check is peaks are due to trapped flux
Disclaimer: lines added for visual effect, and not a fit; errorbars coming from the thermal behavior of He system/cavity/heater, and come from statistical average
Interesting results are obtained after 2nd Cooldown of same sample:
Pre-conditions
Warmup after 1st test Sample was stored in the cavity under nitrogen/air Test break: 4 month
Measurement results for Q1 ~ 415 MHz

## Slide 13: Temperature behaviour of the best samples
 | SIS films tested | Structure | Base test? | Produced by
ARIES 2nd SIS | NbN – AlN – Nb(film)/Cu | 180nm – 8 nm – 4 µm Nb | No | Siegen
ARIES 3ed SIS | NbN – AlN – Nb(film)/Cu | 180nm – 24 nm – 4 µm Nb | No | Siegen
Temperature dependent part (BCS) is growing slower then bulk Nb
Measurement results for Q1 ~ 415 MHz
Sample | Rres
ARIES 2nd SIS | ~45 nOhm
ARIES 3ed SIS | ~127 nOhm
Bulk Nb | ~23 nOhm

## Slide 14: Temperature behaviour of the best samples
 | SIS films tested | Structure | Base test? | Produced by
ARIES 2nd SIS | NbN – AlN – Nb(film)/Cu | 180nm – 8 nm – 4 µm Nb | No | Siegen
ARIES 3ed SIS | NbN – AlN – Nb(film)/Cu | 180nm – 24 nm – 4 µm Nb | No | Siegen
Measurement results for Q1 ~ 415 MHz
Sample | Rres
ARIES 2nd SIS | ~45 nOhm
ARIES 3ed SIS | ~127 nOhm
Bulk Nb | ~23 nOhm
Temperature dependent part (BCS) is growing slower then bulk Nb, here the data for subtracted ~residual resistance

## Slide 15: Temperature behaviour of the best samples
 | SIS films tested | Structure | Base test? | Produced by
ARIES 2nd SIS | NbN – AlN – Nb(film)/Cu | 180nm – 8 nm – 4 µm Nb | No | Siegen
ARIES 3ed SIS | NbN – AlN – Nb(film)/Cu | 180nm – 24 nm – 4 µm Nb | No | Siegen
On the ARIES 2nd SIS we observed quieted low Field dependant Rs growth, comparable to bulk Nb!
On the other hand max field (quench of the film) is stiel low, and there is a room for improvement
Measurement results for Q1 ~ 415 MHz
Sample | Bmax (2.5K)
ARIES 2nd SIS | 32 mT
ARIES 3ed SIS | 26 mT

## Slide 16: Field limit of SIS
Chart: Temperature, K
| 1.8 | 2.5 | 4.5 | 5.5 | 6.5 | 7.5 | 8 | 8.5
 | 27 | 29.8 | 29.2 | 28.5 | 27.4 | 25.4 | 24.7 | 22.3
Max field converging to >9K
 | SIS films tested | Structure | Base test? | Produced by
ARIES 3ed SIS | NbN – AlN – Nb(film)/Cu | 180nm – 24 nm – 4 µm Nb | No | Siegen

## Slide 17: Concl.?
Unusual temperature behavior due to thermal properties of insulator? (exclude?)
Unusual temperature behavior due to Flux trapping
Due to the Film defects (no baseline tests)?
Unusual temperature behavior: No persistence, reproducible dependence
Results: good temp and field dependence, comparable for bulk Nb, except Max field and Residual resistance

## Slide 18: THANK YOU!
D. Tikhonov, Authors
EASITrain – European Advanced Superconductivity Innovation and Training. This Marie Sklodowska-Curie Action (MSCA) Innovative Training Networks (ITN) has received funding from the European Union’s H2020 Framework Programme under Grant Agreement no. 764879
Presenter
Dmitry Tikhonov
Early stage researcher
Helmholtz-Zentrum Berlin
dmitry.tikhonov@helmholtz-berlin.de
+49-30-8062-12922
Conf logo

## Slide 19: Notes

## Slide 20: The Quadrupole resonator (QPR)
Coaxial gap
Sample
Pumping and
Coupler ports
4 hollow
rods (Nb)
He
Cavity (Nb)
Pole shoes
Heater
T-Sensor
Gap ≈ 0.5 mm
Calorimetry chamber
Brief overview:
Calorimetric measurement: Surface resistance is calculated from dissipated power
Operating frequencies 414, 847, 1285 MHz
Bmax on sample up to 120 mT
T on sample from 2 to 20 K
Resolution (limits) < 1 nΩ
Measurements of Magnetic field penetration depth and critical field
Vacuum exp. up to
~1E-6 mBar
Vacuum
~1E-9 mBar