## Slide 1: Tailored material for SRF
Protection, low secondary emission yield
High Tc SC
S-I-S multilayers
Structure, high thermal conductivity (Copper ?)
External layer, optimized for thermal transfer
High purity Niobium Optimized only for thermal conduction
Native oxide
Unstable upon annealing
RF side
Helium side
Today
Future ?
Niobium or…
Native oxide
Not optimized for thermal transfer
At stakes :
Cooling power (any application ); can we go to cryocooling ?
High accelerating fields ?

## Slide 2: Challenges
Bulk Nb
= pure metal
Metallurgy = ~ 6000 years
Higher Tc material
= compounds
Chemistry = ~ 250 years old
Thin films
CVD/PVD = ~ 100 years
Physics vs Real life
Technologies
Not all defects are harmful (see doping in Nb). Which one do we need to get rid of ?

## Slide 3: The importance of mean free path, MgB2 example
  if then:
      x
      l
      k
mean free path
Most developments of HTc are done in view of magnet applications : small x high l ,by playing with
Small x makes the superconductors very sensitive to (usual) crystalline defects (wanted for magnets, not for SRF)
Typical values found in literature for MgB2 : l ~100-150 nm x ~ 5-10 nm
l~50 nm
x ~
some 10 nm ?