## Slide 1: Nb3Sn coating of a 2.6 GHz Nb SRF cavity using a Cylindrical Magnetron Sputtering System
Sharifuzzaman Shakel, Nizam Sayeed, Hani E. Elsayed-Ali (Old Dominion University)
Grigory V. Eremeev (Fermilab)
Anne-Marie Valente-Feliciano, Uttar Pudasaini (JLab)
Frank Batten College of
Engineering & Technology
Old Dominion University

## Slide 2
Frank Batten College of
Engineering & Technology
Old Dominion University
Design, Commissioning and Initial operation of Cylindrical Magnetron Sputtering System
Optimizing conditions for Nb3Sn fabrication using Multilayer Sequential Sputtering Method
Properties Nb3Sn films developed on flat Nb and Sapphire substrates
Nb3Sn coating inside of a 2.6 GHz Nb SRF cavity : Analyzing coated cavity performance
Optimizing cavity coating conditions
Outline

## Slide 3
Cross section sketch of Cylindrical Magnetron Sputtering System
Magnetron movement controller shaft
Gate valve
Vacuum chamber
Cylindrical magnets
Water flow controller
Top magnetron
8’’ ConFlat (CF) port
Tube target
Chamber door
2.6 GHz Nb SRF cavity
Bottom magnetron
Design of Cylindrical Magnetron Sputtering System
09/20/2022 | Shakel

## Slide 4
Turbo pump
Motor controller
Communication controller
Gas flow controller
Gate valve
Pressure gauge
Cooling water flow rate: 0.9 L/min
Maximum travel distance by each magnetron: ~280 mm
Maximum magnetron travel speed: 1.3 mm/s
Baseline pressure: 4 x 10-8 Torr
Typical deposition pressure: 3-10 mTorr
Ar gas flow: 50 SCCM
Available DC power in: 1 kW
Features of Cylindrical Magnetron Sputtering System
4
09/20/2022 | Shakel

## Slide 5
Spacer
Magnet
Neodymium magnets
(N55 grade)
Magnetic field distribution vs Distance
Cylindrical magnetron
Top magnetron
Bottom magnetron
5
09/20/2022 | Shakel
Magnetic Field Distribution

## Slide 6
Top beam tube
Bottom beam tube
Equator
Nb tube
target
Sn tube
target
2.6 GHz Nb SRF cavity placed on
the chamber
Mocking the beam tubes and equator positions of the cavity with Nb substrates
6
09/20/2022 | Shakel

## Slide 7
8 W
12 W
2 W
18 W
15 W
12 W
(a)
(b)
(c)
(d)
(e)
(f)
Power Calibration for Nb deposition
Different DC power used for discharging
50 SCCM Ar gas flow and 10 mTorr pressure used
Minimum 18 W DC power (or higher) needs to be applied for ~8/10 minutes to get symmetric plasma formation
Once symmetric plasma formation appears, it sustains even power is reduced.
7
09/20/2022 | Shakel

## Slide 8
Power Calibration for Sn deposition
Stable and Symmetric plasma formation at 8 W DC power (21 mA)
Calibrated the power to prevent Sn target from melting
09/20/2022 | Shakel

## Slide 9
DC power used : 30 W
Current: 101— 106 mA
Nb tube target discharged
0.9’’ OD x 0.8’’ ID x 4.5’’, 99.99% pure
~50 nm thick coating on equator position
Nb layer deposition
Nb target completes
2 passes across the cavity length, moving speed 1 mm/s
Nb deposition using top magnetron
10 mTorr Ar pressure, 50 sccm flow
09/20/2022 | Shakel

## Slide 10
DC power used : 8 W
Current: 22 — 23 mA
Sn tube target is discharged
0.9’’ OD x 0.8’’ ID x 4.5’’, 99.99% pure
~25 nm thick Sn deposited on equator position
Sn layer deposition
Sn target travels one time across cavity length. Moving speed 0.75 mm/s
Sn deposition using bottom magnetron
10 mTorr Ar pressure, 50 sccm flow
09/20/2022 | Shakel

## Slide 11
 | Top beam tube | Equator | Bottom beam tube
Nb | 36 nm | 50 nm | 33 nm
Sn | 19 nm | 25 nm | 18.5 nm
Ratio | 1.89 | 2 | 1.78
Total Film Thickness
Top Beam tube | Equator | Bottom beam tube
880 nm | 1200 nm | 824 nm
Nb and Sn each layer thickness
(16 layers of each)
50 nm Nb
25 nm Sn
200 nm Nb
Nb substrate
Nb3Sn fabrication by Multilayer Sequential Sputtering method
50 nm Nb
25 nm Sn
50 nm Nb
25 nm Sn
09/20/2022 | Shakel

## Slide 12
12
09/20/2022 | Shakel
Temperature was ramped at 60 C/min to reach the annealing temperature from the room temperature.
Films are annealed at 9500 C for 3 hours in separate furnace
Annealing of the Nb3Sn samples

## Slide 13
Formation of single phase Nb3Sn after annealing is confirmed comparing the X-ray diffraction patterns of the (a) as-deposited and (b) annealed films
(a) as-deposited films
(b) annealed films
Structural Characterization
09/20/2022 | Shakel

## Slide 14
Composition of Sn in the (a) as-deposited films (b) annealed films
Position | Sn (atm %) As-deposited films | Sn (atm %) Annealed films
Top beam tube | 33 | 22
Equator | 32 | 19
Bottom beam tube | 25 | 19
Position | RMS roughness as-deposited (nm) | RMS roughness annealed (nm)
Top beam | 68 | 50
Equator | 26 | 28
Bottom beam | 43 | 50
09/20/2022 | Shakel

## Slide 15
Sample position | Tc (K) | ΔTc (K) | RRR
Top beam tube | 17.61 | 0.24 | 2.26
Equator | 17.76 | 0.06 | 3.00*
Bottom beam tube | 17.73 | 0.1 | 5.01
Superconducting critical temperature (Tc) for Nb3Sn
on sapphire
09/20/2022 | Shakel
Superconducting Properties

## Slide 16
SRF cavity
Ar gas line
Cavity coating with multilayers of Nb and Sn
Uniform deposition
No color gradient
No pilling-off film
No patchy regions
09/20/2022 | Shakel
Cavity Coating

## Slide 17
Temperature profile of furnace used for annealing of the coated cavity
(9500C for 3 hours)
Coated cavity annealed and performance test done in FermiLab
Post annealing cavity pictures
09/20/2022 | Shakel
Annealing of coated cavity

## Slide 18
Results
(Q0) of 3.2 x 108 at Eacc = 5 MV/m at Tbath = 4.4 K
(Q0) of 1.1 x 109 at Eacc = 5 MV/m at Tbath = 2.0 K
Nb Q0 ~ 7 x 109
@ Tbath = 2.0 K
Nb Q0 ~ 1 x 108
@ Tbath = 4.0 K
Cold test set up for cryogenic RF testing of the cavity in
Vertical test stand
09/20/2022 | Shakel
Nb3Sn coated cavity performance

## Slide 19
The transition temperature of Nb3Sn layer is observed at ~ 17.9 K
Loaded Quality Factor (QL) vs Temperature (T)
Frequency shift vs Temperature
09/20/2022 | Shakel
Nb3Sn coated cavity performance

## Slide 20
Replicating the similar plasma geometry/density, magnetron current value to that of actual 2.6 GHz SRF cavity.
More accurate film thickness and film surface analysis will be possible compared to deposition in flat samples.
Experiment in progress for uniform thick Nb3Sn deposition across the entire length of the cavity using multilayer sequential sputtering method
09/20/2022 | Shakel
Optimizing the cavity coating conditions
Installing a mock-up cavity

## Slide 21
Current profile of magnetrons discharging without cavity installed
Discharging without cavity, magnetron current for Nb and Sn deposition are steady across the deposition range
Discharging inside cavity, magnetron current fluctuates due to the changes in pressure while the magnetron’s moving inside the cavity
Position of gas inlet into the cavity needs to be reconsidered
Pressure
gradient
Sn discharge
Inside cavity
~6% fluctuation in current
Nb discharge
Inside cavity
~15% fluctuation in current
Pressure/Current changes due to cavity
09/20/2022 | Shakel
Challenges

## Slide 22
Designed and commissioned a cylindrical magnetron sputtering system
Used multilayer sequential sputtering to coat Nb3Sn into 2.6 GHz Nb SRF cavity
Film Tc 17.61 – 17.76 K obtained
In cryogenic RF testing the quality factor (Q0) of 3.2x108 at Eacc = 5 MV/m at Tbath = 4.4 K and Q0 of 1.1x109 at Eacc = 5 MV/m at Tbath = 4.4 K.
The transition temperature of Nb3Sn layer is measured at about 17.9 K.
Optimization of multilayer sequential sputtering method.
09/20/2022 | Shakel
Summary

## Slide 23
09/20/2022 | Shakel
Optimizing multilayer coating conditions using mock-up cavity – resolving pressure/current gradient, uniform coating covering entire length of the cavity
Cavity performance improvement using multilayer sequential sputtering of Nb3Sn
Optimizing plasma formation and deposition conditions for Co-sputtering of Nb and Sn Cavity coating by Co-sputtering technique
Acknowledgement
This work support was provided by the U.S. Department of Energy, Office of High Energy Physics, Contact No. DE-SC0022284.
Future Plans

## Slide 24: Thank You!