## Slide 1
Development of an
SNSPD UV imager
Adam McCaughan
NIST, Boulder, CO
Notes: Introduction + September Cover of APL

## Slide 2: Superconducting nanowire single photon detectors (SNSPDs)
Cryogenic – 1K to 4K
Operate in photon-counting mode
  No read noise
  UV to mid-IR
Low dark count rates (~0.01 counts/hr/pixel)
High quantum efficiency
  ~100% QE generally
  Measured 70-80% system detection efficiency @ 250nm (higher possible)
  More sensitive as photon energy increases
MHz count rates

## Slide 3: Principles of operation

## Slide 4: Principles of operation

## Slide 5: Principles of operation

## Slide 6: Principles of operation

## Slide 7: Principles of operation

## Slide 8: Principles of operation
Reddy, D. V., et. al, Superconducting nanowire single-photon detectors with 98% system detection efficiency at 1550 nm. Optica 7, 1649 (2020).

## Slide 9: SNSPD photon transduction/amplification
~1-10 eV input photon
~100-1,000 eV electrical output
Broadband (~1 GHz)
Low amplitude (~1 mV)
Focus of this work: building a scalable array architecture

## Slide 10: SNSPD arrays over the years
Year
Array size
1024 pixels

## Slide 11: The problem – symmetric coupling
Notes: How do you multiplex SNSPDs?
Maybe electrically connect to a single bus?

## Slide 12: The problem – symmetric coupling
Notes: Photon hits->Electric pulse->Couple to the bus

## Slide 13: The problem – symmetric coupling
Notes: But this coupling is symmetric
Ergo if there are more than one SNSPDs, the pulse is diverted all of them and effectively diffuses.
Can’t truly SCALE

## Slide 14: Asymmetric coupling: Thermal switch
McCaughan, A. N., et. al. Nature Electronics 2, 451–456 (2019).
heater
superconducting
nanowire
Notes: What if we had an Asymmetric component
Made with a narrow heater on top of a wider Superconducting wire.

## Slide 15: Asymmetric coupling: Thermal switch
heater
resistive
nanowire
Asymmetric process!
McCaughan, A. N., et. al. Nature Electronics 2, 451–456 (2019).
Notes: Current applied to the heater, heats the nanowire which forms a hotspots.
Please see my poster right after this for more discussion about operation, energy requirements.

## Slide 16: Thermal readout bus
superconducting nanowire
readout bus
Notes: We take a MW readout line, and current bias it

## Slide 17: Thermal readout bus
superconducting nanowire
readout bus
Notes: Next let’s put an SNSPD nearby and use it to detect a photon

## Slide 18: Thermal readout bus
superconducting nanowire
readout bus
Notes: When the photon is detected, we get an output pulse from the SNSPD that will heat the attached resistor

## Slide 19: Thermal readout bus
Notes: A hotspot is formed which creates 2 outgoing pulses.

## Slide 20: Thermal readout bus
Notes: Measure the difference in arrival times, time-delay, pinpoint which pixel clicked

## Slide 21: Thermal readout bus
Notes: Neighboring SNSPDs have no effect.

## Slide 22: Inidividual pixels
Time-of-flight readout
Small separation ambiguity between adjacent pixels
Large separation reduced count rate
Differential delay (ns)
Counts/min
Inter-pixel delay length: 400µm
Inter-pixel delay time: 352ps
heater
ground plane
readout bus
Notes: WSi MW bus covered with Nb Ground Plane.
GND plane creates a slow delay line
Heater connected to SNSPD out of picture

## Slide 23: Row/column format
Layer 1: SNSPDs = columns
Notes: Detector Array

## Slide 24: Row/column format
Layer 1: SNSPDs = columns
Layer 2: SNSPDs = rows
Imaging area entirely detectors
Notes: Detector Matrix -> Camera

## Slide 25: Row/column format
Layer 1: SNSPDs = columns
Layer 2: SNSPDs = rows
Row-col thermal coupling
Allmaras, J. P., et. al. Nano Lett. 20, 2163–2168 (2020).
hν
Notes: How Single photon can click 2 SNSPDs?
Demonstrated and illustration by Jason Allmaras, the hotspot generated in the column SNSPD can heat a nearby row SNSPD

## Slide 26: First result: 1,024-pixel array
Flood illumination
Excellent resolution of all 1024 pixels
Column differential delay (ns)
Row differential delay (ns)
500 um
A. N. McCaughan et al., Appl. Phys. Lett., vol. 121, no. 10, p. 102602, Sep. 2022
Notes: Well, the measurement went extremely well.
What you see on the right is the result of flood illuminating the device and reading out the row/col positions from the readout busses
Each of those blue dots is actually several hundred detection events, as you can see here

## Slide 27: First result: 1,024-pixel array
Flood illuminate
Excellent resolution of all 1024 pixels
Column differential delay (ns)
Row differential delay (ns)
A. N. McCaughan et al., Appl. Phys. Lett., vol. 121, no. 10, p. 102602, Sep. 2022
Notes: If you look closely at the zoomed figure on the left, you’ll see there’s a couple events that are ambiguous (kind of between rows), but for the most part this time-of-flight readout method gives extremely good row and column resolution

## Slide 28: First result: 1,024-pixel array
Column differential delay (ns)
Row differential delay (ns)
Flood illuminate
Excellent resolution of all 1024 pixels
Notes: As a sanity check, we can make histograms of just the row-readout or just the column-readout
These end up looking very well spaced, giving us some reassurance that the row and column readouts aren’t influencing each other

## Slide 29: First result: 1,024-pixel array
99.83% distinguishability
Column differential delay (ns)
Row differential delay (ns)
Counts
Offset from nearest row/column (ps)
FWHM
28.0 ps
Notes: We can also compare every count recorded in that entire 2D diagram to its nearest row and column and get an idea of how many counts aren’t nicely centered on those dots.
We’ll consider counts that are too far from the nearest centroid non-distinguishable and try to get an idea of how often that happens.
It’s hard to see here because there are so few, but this gave us a lower bound of 99.8% distinguishability. This was reassuring, because we really don’t want to have to throw away counts because we’re not sure which row or which column they actually landed on.
This diagram was also helpful to let us examine the readout jitter for the whole array. In this experiment the FWHM ended up being less than 30 picoseconds which was very good.

## Slide 30: First result: 1,024-pixel array
Imaging a 373 nm spot
Approaching unity Q.E., but not quite
X-pixel
Y-pixel
Counts
A. N. McCaughan et al., Appl. Phys. Lett., vol. 121, no. 10, p. 102602, Sep. 2022

## Slide 31: SNSPD arrays over the years
Year
Array size
This work

## Slide 32: First result: 1,024-pixel array
Many issues with this array
  Poor detector yield (~90%)
  Upper layer superconductor degraded vs lower layer
  Non-uniform heater properties
X-pixel
Y-pixel
Counts
A. N. McCaughan et al., Appl. Phys. Lett., vol. 121, no. 10, p. 102602, Sep. 2022

## Slide 33: Fabrication process
33
1mm
6) Top Wire (Nb: 250nm, PdAu: 10nm)
5) Resistors (PdAu: 30nm)
4) Top Detector (WSi: 4nm, aSi: 2nm)
3) Insulator (BCB: 40nm, SiO2: 25nm, aSi: 4nm)
BCB: Benzocyclobutene
2) Bottom Wire (Nb: 90nm, PdAu: 10nm)
1) Bottom Detector (WSi: 4nm, aSi: 2nm)
6mm
Notes: This architecture seemed really promising but did require a good amount of fabrication development.
Keep in mind there is a single readout, hence a sporadic count from a single nanowire is problem.
Topography of NW1 is a problem for NW2

## Slide 34
Row differential delay (ns)
Column differential delay (ns)
Gaussian spot illumination
60,000 pixel array measurement
Notes: As a sanity check, we can make histograms of just the row-readout or just the column-readout
These end up looking very well spaced, giving us some reassurance that the row and column readouts aren’t influencing each other

## Slide 35
Gaussian spot illumination
Excellent resolution of all 60,000 pixels (90 kpixel design)
Row differential delay (ns)
Column differential delay (ns)
2x dysfunctional sections
1 or 2 bad detectors each
1mm
60,000 pixel array measurement
297/300 nanowire yield
Notes: As a sanity check, we can make histograms of just the row-readout or just the column-readout
These end up looking very well spaced, giving us some reassurance that the row and column readouts aren’t influencing each other

## Slide 36
Gaussian spot illumination
Excellent resolution of all 60,000 pixels (90 kpixel design)
1mm
60,000 pixel array measurement
Measure-then-prune bad detectors
Notes: As a sanity check, we can make histograms of just the row-readout or just the column-readout
These end up looking very well spaced, giving us some reassurance that the row and column readouts aren’t influencing each other

## Slide 37: 60,000 pixel array measurement
Row differential delay (ns)
Column differential delay (ns)
Column differential delay (ns)
Row differential delay (ns)
Counts/min
Counts/min
Counts/min
Counts/min
Excellent distinguishability
Count rate = 2×105 cps
Notes: As a sanity check, we can make histograms of just the row-readout or just the column-readout
These end up looking very well spaced, giving us some reassurance that the row and column readouts aren’t influencing each other

## Slide 38: 60,000 pixel array measurement
Excellent distinguishability
Count rate = 2×105 cps
Row differential delay (ns)
Column differential delay (ns)
Row differential delay (ns)
Column differential delay (ns)
Counts/min
Counts/min
Notes: As a sanity check, we can make histograms of just the row-readout or just the column-readout
These end up looking very well spaced, giving us some reassurance that the row and column readouts aren’t influencing each other

## Slide 39: 60,000 pixel array measurement
1.5mm
5.5mm
Notes: As a sanity check, we can make histograms of just the row-readout or just the column-readout
These end up looking very well spaced, giving us some reassurance that the row and column readouts aren’t influencing each other

## Slide 40: 60,000 pixel array measurement
Row differential delay (ns)
Column differential delay (ns)
1.5mm
5.5mm
60x improvement
Notes: As a sanity check, we can make histograms of just the row-readout or just the column-readout
These end up looking very well spaced, giving us some reassurance that the row and column readouts aren’t influencing each other

## Slide 41: SNSPD arrays over the years
This work
Year
Array size

## Slide 42: Scaling – array size
Notes: Now, a natural question follows – how can we scale this to very large sizes? Ultimately, we’d like to have a megapixel or larger array, so how would that be possible?

## Slide 43: Scaling – array size
Only requires longer readout bus!
Notes: Fortunately, we get a very easy way of scaling – all we do is add more rows and columns, and make our readout bus longer like shown on the right.
That’s something not possible in any other architecture right now, and to my point at the beginning of the talk, this is only possible because neighboring SNSPDs are so well-isolated from each other. There’s very little interaction between neighboring SNSPDs, so adding additional rows and columns is very straightforward.
The one issue potential issue with scaling this way is that the longer the readout bus is, the more dead time there is between photon detections. Think of it this way – since the readout bus is a time-of-flight measurement, if it’s 10 nanoseconds long you can only count at 100 MHz. If you add twice as many rows and columns, you’ll end up with the readout busses being 20 ns long, meaning you can only count at 50 MHz which is half the rate.
Fortunately, there’s an easy solution for this

## Slide 44: Scaling – count rate
Notes: Up until now we’ve only considered having one pair of readout busses.
This is convenient because you could have an enormous array read out with only 4 microwave lines, but clearly this will limit your ultimate count rate.
For higher count-rate applications, we can examine what happens when we add more readout busses.

## Slide 45: Scaling – count rate
N2 scaling for count-rate
Notes: It turns out that there’s a really favorable N^2 scaling factor: if you double the number of readout microwave lines, you can obviously read out twice as many pulses. But on top of that, if the number of rows and columns stays the same, that means each readout line has half as much dead time. This means if you’re willing to double the number of microwave readout lines, you get a factor of 4 increase in the count rate.
If you’re willing to use, say, 10 times as many microwave lines, you’ll get a factor of 100 increase in the count rate your array can achieve.

## Slide 46: Thermal modeling
Extensive thermal modeling to understand phonon behavior
Particularly interested in thermal crosstalk
Higher fill factors will require dense wires
McCaughan, A. N., et. al. Nature Electronics 2, 451–456 (2019).

## Slide 47: Thermal modeling
Extensive thermal modeling to understand phonon behavior
Particularly interested in thermal crosstalk
Higher fill factors will require dense wires
McCaughan, A. N., et. al. Nature Electronics 2, 451–456 (2019).

## Slide 48: Thermal crosstalk experiments
PEACOCQ array (NbTiN)
  2×10-4 crosstalk @ 400nm pitch
NASA DSOC array (WSi)
  < 1×10-4 crosstalk @ 1200nm pitch
  ~1×10-2 crosstalk @ 800nm pitch
TCI arrays (WSi)
  ~5×10-3 crosstalk @ 1 um pitch
  < 1×10-4 crosstalk @ 2 um pitch
Exponential falloff of crosstalk
  1/e ≈ 0.1-0.5 μm (material)
~ 100 - 101 ns delay in crosstalk receiving channel
[1] I. Craiciu et al., “High-speed detection of 1550 nm single photons with superconducting nanowire detectors,” (2022) ArXiv: 2210.11644
[2] M. D. Shaw, et. al. "Arrays of WSi Superconducting Nanowire Single Photon Detectors for Deep-Space Optical Communications," in CLEO 2015
[3] Allmaras, J, “Modeling and Development of SNSPDs”, Thesis, Caltech, 2022

## Slide 49: Future infrastructure for UV-EUV
NIST SURF facility
  Synchotron source
  Tunable 4-400nm radiation
  Single-photon to 10^6 photons per pulse
Finished design of custom cryostat for beamline
NIST-standardized power calibrations
NIST SURF facility
Cryostat for SURF

## Slide 50: Muon veto
cosmic ray muons: one likely source of background counts
“sandwich” detector between scintillating substrates with local detectors
veto signal counts that coincide with scintillating counts
Light-blocking screens
~1.3 eV (930 nm)
“Signal” SNSPD chip
Scintillating GaAs substrate with SNSPD
Scintillating GaAs substrate with SNSPD
S. Derenzo et al., 1802.09171
J. Chiles et al., unpublished (2022)
Notes: What else can we do? Remember that we saw some dark counts, which means there’s still room for improvement if we can find the cause of them. Right now, we’re pursuing a muon veto, since we expect them to be a potential source of interference and false counts. The idea is to put our main signal SNSPD between two scintillating substrates with their own local detectors. When a muon transits through all three, it will produce scintillating 930 nm photons in the gallium arsenide chips, which will give counts on each chip at the same time – a coincidence. When this happens, we can ignore any click on our signal detector that was also there at the same time.

## Slide 51: Muon veto: preliminary data
Muons should scintillate GaAs @ 980 nm
Data shows “dark counts” have same characteristics as muon scintillation!
muon flux: ~ 10 cm-2 min-1 (NIST Boulder elevation)
coincidence rate: ~ 2.1 cm-2 min-1
Small improvements could yield close to 100% muon veto efficiency
Notes: Here’s some preliminary data on this. We measured two SNSPDs fabbed on the same gallium arsenide chip. For each one, we recorded the saturation curve for 980 nm photons as a proxy for what a scintillating photon would be like. So we know that for example when we bias the SNSPD at 14 uA, it will efficiently detect such photons. Then we turned off the laser and looked at clicks “in the dark” – no sources of light except some blackbody, and importantly, cosmic ray muons. When both detectors click at the same time, it could be a muon. When we swept the bias current in the dark, we found a telltale signature of coincidence detection events which exactly follows the SNSPD’s saturation curve for 980 nm photons. We found about 2 events per minute per centimeter squared, which is 20% of what we expected at our elevation. So with just two relatively small detectors covering a tiny fraction of the chip surface, we’re already seeing a good fraction of the events, and with small improvements, we could easily reach close to 100% reliability at finding and vetoing muons.

## Slide 52: Conclusion / outlook
Advantages
  Simple to scale
  Highly independent detectors
Lots to do still!
  Megapixel sizes
  Higher fill-factor (10% now)
  UV measurements 4-400nm
  Higher count-rate
Notes: Overall we’re very excited about the results and where we can go with this architecture.
One of the things I want to emphasize here is that this architecture scales really easily – all you have to do is add more rows and columns, and make the readout busses a little longer.
If you want to increase the count rate, you just add extra readout busses and run a few more microwave lines.
Now, all that said there’s still a lot to do! We’re looking at building higher pixel-count arrays, characterizing with free-space images, doing faster counting by adding readout busses, and other quality-of-life improvements like increasing the fill-factor

## Slide 53: People & Acknowledgements
Bakhrom Oripov (NIST)
Dana Rampini (NIST)
Boris Korzh (JPL)
Jason Allmaras (JPL)
Tannaz Farrahi (NIST)
Sae Woo Nam
Rich Mirin
Notes: I want to thank everyone who’s contributed to this so far, and I want to thank NASA especially for funding this work.
I also want to briefly mention that all of these layouts were designed in Python using our PHIDL layout package.
We have a poster about that in the online poster session, or you can look it up on google by searching for the word “phidl”

## Slide 54: Extra slides

## Slide 55: Scaling
Dynamic range of megapixel array
Optimistic
50 ps separation
2 ns bus reset
10 Mcps per SNSPD
1 dark count/hour/SNSPD
Current
400 ps separation
200 ns bus reset
1 Mcps per SNSPD
1 dark count/min/SNSPD

## Slide 56
Before BCB

## Slide 57
After BCB

## Slide 58: System detection efficiency measurements
Crucial for accurate measurement
  Count every photon
  Don’t estimate!
  Don’t artificially discount non-idealities
Basic procedure
  Accurately measure # of photons/sec in fiber
  Any photons not detected by detector are losses
D. V. Reddy, et. al., “Superconducting nanowire single-photon detectors with 98% system detection efficiency at 1550 nm,” Optica, vol. 7, no. 12, p. 1649, Dec. 2020

## Slide 59: 98% system detection efficiency

## Slide 60: UV SNSPD progress
NbTiN-based SNSPD process
  Tc = 11K
Measured @ 370nm
Plateau (unity QE) at 3.4K, nearing at 5K
Operated at 6K