## Slide 1: A superconducting nanowire pulse counter integrated with an SNSPD
11/29/2022
Superconducting Electronics and Detectors Workshop– Jefferson Lab
Matteo Castellani*1, Owen Medeiros1, Reed Foster1, Alessandro Buzzi1, Marco Colangelo1, Joshua C. Bienfang2, Alessandro Restelli2, Karl Berggren1
1Electrical Engineering and Computer Science, Massachusetts Institute of Technology, Cambridge, Massachusetts, United States; 2Joint Quantum Institute, National Institute of Standards and Technology and University of Maryland
Gaithersburg, Maryland, United States
Notes: Add all the other logos

## Slide 2: Superconducting Nanowire Single-Photon Detectors (SNSPDs)
Wide wavelength sensitivity.
High efficiency.
Low dark count and jitter.
Applications: quantum information, life science, imaging.
2 μm
J. P. Allmaras, PhD Thesis CalTech (2020)
Notes: App: quantum infor, life science, low power optical comm, imaging,
Signal digitalized at room temp with scope or time-tagger

## Slide 3: Superconducting Nanowire Single-Photon Detectors (SNSPDs)
D. Wang et al. Sensors 22(3)
Wide wavelength sensitivity.
High efficiency.
Low dark count and jitter.
Applications: quantum information, life science, imaging.
Standard readout setup
2 μm
J. P. Allmaras, PhD Thesis CalTech (2020)
Notes: App: quantum infor, life science, low power optical comm, imaging,
Signal digitalized at room temp with scope or time-tagger

## Slide 4: Superconducting Nanowire Single-Photon Detectors (SNSPDs)
D. Wang et al. Sensors 22(3)
Wide wavelength sensitivity.
High efficiency.
Low dark count and jitter.
Applications: quantum information, life science, imaging.
Standard readout setup
New architecture necessary to read out arrays of SNSPDs
2 μm
J. P. Allmaras, PhD Thesis CalTech (2020)
Notes: App: quantum infor, life science, low power optical comm, imaging,
Signal digitalized at room temp with scope or time-tagger

## Slide 5: Readout of SNSPD arrays
M. S. Allman et al. Appl. Phys. Lett. 106 (2015)
S. Doerner et al. Appl. Phys. Lett. 111 (2017)
Analog multiplexing
Frequency
multiplexing
Row-column
readout
Notes: Two kind of readout
On-chip digitalization (show image of a paper) Cost on chip complexity
Or analog multiplexing on cjip and then conventional electronic at room temp (show image of a paper)
Show row column readout 2sqrt(N) lines
Frequency multilexing
All this analog solutions limit some of the advantages of snspd (count rate, low jitter)

## Slide 6: Readout of SNSPD arrays
Digitized readout
M. Yabuno et al. Opt. Express 28 (2020)
The digitization is a key element for scaling up.
Multi-chip system.
JJs can not drive high loads.
M. S. Allman et al. Appl. Phys. Lett. 106 (2015)
S. Doerner et al. Appl. Phys. Lett. 111 (2017)
Analog multiplexing
Frequency
multiplexing
Row-column
readout
Notes: Two kind of readout
On-chip digitalization (show image of a paper) Cost on chip complexity
Or analog multiplexing on cjip and then conventional electronic at room temp (show image of a paper)
Show row column readout 2sqrt(N) lines
Frequency multilexing
All this analog solutions limit some of the advantages of snspd (count rate, low jitter)

## Slide 7: Readout of SNSPD arrays
Digitized readout
M. Yabuno et al. Opt. Express 28 (2020)
The digitization is a key element for scaling up.
Multi-chip system.
JJs can not drive high loads.
On-chip integration with electronics and higher signal levels can help scaling up
M. S. Allman et al. Appl. Phys. Lett. 106 (2015)
S. Doerner et al. Appl. Phys. Lett. 111 (2017)
Analog multiplexing
Frequency
multiplexing
Row-column
readout
Notes: Two kind of readout
On-chip digitalization (show image of a paper) Cost on chip complexity
Or analog multiplexing on cjip and then conventional electronic at room temp (show image of a paper)
Show row column readout 2sqrt(N) lines
Frequency multilexing
All this analog solutions limit some of the advantages of snspd (count rate, low jitter)

## Slide 8: Superconducting nanowire electronics: Nanocryotrons
A.N. McCaughan et al. Nano Lett. 14 (2014)
R. Baghdadi et al. Phys Rev. App. 14 (2020)
Nanocryotron (nTron)
Heater-Nanocryotron (hTron)
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 9: Superconducting nanowire electronics: Nanocryotrons
A.N. McCaughan et al. Nano Lett. 14 (2014)
R. Baghdadi et al. Phys Rev. App. 14 (2020)
Nanocryotron (nTron)
Heater-Nanocryotron (hTron)
Simple structure
Magnetic field robustness
High load driving
Coupling with CMOS, JJs
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 10: Superconducting nanowire electronics
B. A. Butters et al. SST 34 2021
Non-volatile memory
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 11: Superconducting nanowire electronics
OR gate
NOT gate
A. Buzzi et al. WOLTE 22
B. A. Butters et al. SST 34 2021
Non-volatile memory
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 12: Superconducting nanowire electronics
OR gate
NOT gate
A. Buzzi et al. WOLTE 22
R. A. Foster et al. WOLTE 22
B. A. Butters et al. SST 34 2021
Non-volatile memory
Shift-register
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 13: Superconducting nanowire electronics
OR gate
NOT gate
A. Buzzi et al. WOLTE 22
R. A. Foster et al. WOLTE 22
M. Onen et al. Nano Lett. 2020
B. A. Butters et al. SST 34 2021
Non-volatile memory
Shift-register
Integrator
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 14: Superconducting nanowire electronics
OR gate
NOT gate
A. Buzzi et al. WOLTE 22
R. A. Foster et al. WOLTE 22
M. Onen et al. Nano Lett. 2020
B. A. Butters et al. SST 34 2021
Non-volatile memory
Shift-register
Integrator
O. Medeiros et al. ASC 22
SNSPD: Physics, Measurement, Readout, Applications
Multiplexer
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 15: Megapixel SNSPD array for hyperspectral imaging
Count rates 105 - 107 cps per pixel (1012 per array) without losing any photons.
The timing information is not relevant.
Slide from Invisible Headlight DARPA project (2022)
Negligible dark counts and readout noise to support high frame rates.
High efficiency in MWIR (4-8 um), LWIR (8-12 um), and/or VLWIR (12-15 um).
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 16: Megapixel SNSPD array for hyperspectral imaging
Count rates 105 - 107 cps per pixel (1012 per array) without losing any photons.
The timing information is not relevant.
Slide from Invisible Headlight DARPA project (2022)
Negligible dark counts and readout noise to support high frame rates.
High efficiency in MWIR (4-8 um), LWIR (8-12 um), and/or VLWIR (12-15 um).
We need to count and store the exact number of photons in a certain time interval.
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 17: Superconducting nanowire pulse counter
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 18: Superconducting nanowire pulse counter
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 19: Superconducting nanowire pulse counter
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 20: Superconducting nanowire pulse counter
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 21: Superconducting nanowire pulse counter
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 22: Superconducting nanowire pulse counter
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 23: Superconducting nanowire pulse counter
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 24: Superconducting nanowire pulse counter
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 25: Superconducting nanowire pulse counter
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 26: Superconducting nanowire pulse counter
Simulations
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 27: Fabrication
300 nm SiO₂ on Si
15 nm sputtered NbN
ZEP530 spin coating
E-beam exposure
+ development
CF₄ reactive ion etching
Resist removing
A
B
C
D
E
F
A. Buzzi et al. WOLTE 22
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 28: Fabrication
L0 ≈ 150 nH
Rsh = 3 Ω
300 nm SiO₂ on Si
15 nm sputtered NbN
ZEP530 spin coating
E-beam exposure
+ development
CF₄ reactive ion etching
Resist removing
A
B
C
D
E
F
A. Buzzi et al. WOLTE 22
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 29: Single stage: measurements
Ib1
Tested at 4.2 K in helium dewar
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 30: Single stage: measurements
Ib1
Tested at 4.2 K in helium dewar
correct
operation
<
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 31: 2-digit counter: fabrication
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 32: 2-digit counter: measurements
Base 2
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 33: 2-digit counter: measurements
Base 2
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 34: 2-digit counter: measurements
< 2x10-4
Base 2
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 35: SNSPD + 2-digit counter
Tested at 1550 nm and 405 nm
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 36: SNSPD + 2-digit counter
Tested at 1550 nm and 405 nm
Base 2 at 405 nm
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 37: SNSPD + 2-digit counter
Tested at 1550 nm and 405 nm
Base 3 at 405 nm
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 38: SNSPD + 2-digit counter
<
Tested at 1550 nm and 405 nm
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 39: SNSPD + 2-digit counter
Base 3
Base 2
<
Tested at 1550 nm and 405 nm
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 40: SNSPD + 2-digit counter
Base 3
Base 2
<
Tested at 1550 nm and 405 nm
We still need to demonstrate how to read out the state of the counter
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 41: Read-out method: shift-register
Simulation
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 42: Read-out method: shift-register
Simulation
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 43: Read-out method: parallel
Simulation
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 44: Read-out method: parallel
Simulation
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 45: Megapixel SNSPD array
Output levels - parallel readout in base 6
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 46: Megapixel SNSPD array
With 3 digits in base 6 the maximum count is 215.
1012 cps if the array is read out every 200 us.
The rows are read out 10 at a time.
30-line ADC to read out
Output levels - parallel readout in base 6
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 47: Conclusions
We demonstrated a tunable pulse counter coupled to an SNSPD at 1150 nm and 405 nm.
We showed that both sensing and signal processing can be performed with the same technology on-chip.
The main application are SNSPD arrays, but it can be useful for quantum communications or cryogenic electronics generally.
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.
Integration with snspd of multi loops
Scaling up dimensions
Power consumption = 0.5 fJ/spike
Power = 25 nW per nTron
Area = 50x50 um2
Integration with resistors
Advantage of snspd is high count rate, the design must be optimize to have the same

## Slide 48: Conclusions
We demonstrated a tunable pulse counter coupled to an SNSPD at 1150 nm and 405 nm.
We showed that both sensing and signal processing can be performed with the same technology on-chip.
The main application are SNSPD arrays, but it can be useful for quantum communications or cryogenic electronics generally.
A
Maximum count rate: 5 x 107 cps
Energy consumption: 0.5 fJ/spike
Power: 25 nW/nTron
Cell footprint:
50x50 μm2
Operating temperature: 4.2 K
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.
Integration with snspd of multi loops
Scaling up dimensions
Power consumption = 0.5 fJ/spike
Power = 25 nW per nTron
Area = 50x50 um2
Integration with resistors
Advantage of snspd is high count rate, the design must be optimize to have the same

## Slide 49: Conclusions
We demonstrated a tunable pulse counter coupled to an SNSPD at 1150 nm and 405 nm.
We showed that both sensing and signal processing can be performed with the same technology on-chip.
The main application are SNSPD arrays, but it can be useful for quantum communications or cryogenic electronics generally.
A
Maximum count rate: 5 x 107 cps
Energy consumption: 0.5 fJ/spike
Power: 25 nW/nTron
Cell footprint:
50x50 μm2
1 m
Multi-layer process and on-chip resistors
Operating temperature: 4.2 K
Scaling down inductors
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.
Integration with snspd of multi loops
Scaling up dimensions
Power consumption = 0.5 fJ/spike
Power = 25 nW per nTron
Area = 50x50 um2
Integration with resistors
Advantage of snspd is high count rate, the design must be optimize to have the same

## Slide 50: Acknowledgement
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.

## Slide 51: Thank you!
Notes: Von Neumann architectures are reaching a performance plateau.
The system power consumption (J/bit) has been growing linearly over the years.